|  | Chemical composition (wt%) |  |  |  |  |  |  | Engineering properties |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Steel alloy | C | Mn | Si | S | P | Al | N | EL% | YS (MPa) | UTS (MPa) |
| Mild Steel | 0.15 | 0.60 | 0.13 | 0.04 | 0.05 | 0.04 | 0.0052 | 27 | 280 | 410 |
| IFHS 350 | 0.004 | 0.40 | 0.01 | 0.012 | 0.05 | 0.02 | 0.0018 | 40 | 220 | 450 |
| Elongation percentage (EL%), Yield Strength (YS), Ultimate Tensile Strength (UTS) |  |  |  |  |  |  |  |  |  |  |

Table 1: Chemical and Mechanical properties of steel materials being welded