Table 1. CO2 reduction coupled with 1-phenylethanol oxidation under LED light irradiationa.

| Catalyst | Gas Products (μmol·h-1) |  | Liquid Products (μmol·h-1) |  | e-/h+ |
| --- | --- | --- | --- | --- | --- |
|  | CO | H2 | Pinacol | Acetophenone |  |
| CdS-DETA | 467.1 | 78.4 | 553.9 | n.d.b | 0.98 |
| CdS | 0.2 | 112.7 | 2.57 | 113.0 | 0.98 |

aReaction conditions: 5 mg of catalyst and 500 μL of 1-phenylethanol were dispersed in 10 mL of acetonitrile and irradiated by a 395 nm LED light (74 mW·cm-2) for 1 hour at 25 °C and 1 atm CO2. bn.d. = not detected.