Production and characterization of transportation fuels from domestic plastic wastes and mixed virgin plastics by low- cost catalytic pyrolysis

Praveen Kumar Ghodkea  Krishna Moorthyb  Amit Kumar Sharmac, Wei-Hsin Chen,d,e,f

aDepartment of Chemical Engineering, National Institute of Technology Calicut, Kozhikode, Kerala, India.

bDepartment of Mechanical Engineering, University of Petroleum and Energy Studies (UPES), Dehradun, Uttarakhand, 248007, India.

cCentre for Alternate Energy Research (CAER) and Department of Chemistry, University of Petroleum and Energy Studies (UPES), Dehradun, Uttarakhand, 248007, India.

dDepartment of Aeronautics and Astronautics, National Cheng Kung University, Tainan 701, Taiwan

e Research Center for Smart Sustainable Circular Economy, Tunghai University, Taichung 407, Taiwan

f Department of Mechanical Engineering, National Chin-Yi University of Technology, Taichung 411, Taiwan

Corresponding author: Dr Amit Kumar Sharma, amit.orgchemistry@gmail.com, Mob. +91-9634800400

S1: Three-stage condensing system for liquid hydrocarbons production through pyrolysis

| Mineral Composition | SiO2 | Al2O3 | Fe2O3 | MgO | CaO | Na2O | K2O | MnO | TiO2 | P2O5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Wt % | 0.3 | 0.48 | 0.04 | 0.03 | 0.02 | 0.07 | 0.01 | 0.02 | 0.01 | 0.02 |

S2: XRF analysis of catalysts

S3: FTIR of catalyst

S4: XRD pattern of catalyst