Supporting information

Deterioration of contemporary Kaihua handmade paper: evolution of molecular, supermolecular and macroscopic structures

Jingjing Yao 1,2, Ruohong Zhang 1, Chan Luo 1, Yueer Yan3 *, Ning Bi 1 *, Yi Tang 2 *

1. Shanghai Institute of Quality Inspection and Technical Research, Shanghai 201114, PR China

2. Department of Chemistry, Fudan University, Shanghai 200433, PR China

3. Institute for Preservation and Conservation of Chinese Ancient Books, Fudan University Library, Fudan University, Shanghai 200433, PR China

*Corresponding authors.

Email addresses: yueeryan@fudan.edu.cn (Yueer Yan*), bining@sqi.org.cn (Ning Bi*), yitang@fudan.edu.cn (Yi Tang*)

Content

SI.1. Basic information for four typical kaihua handmade papers	1

SI.2. The change of FTIR spectra of four handmade papers in DH and WH condition	2

SI.3. The content of carboxyl group and reducing carbonyl group	3

SI.4. The Crystal-amorphous structure of four handmade papers in DH and WH aging process	4

SI.5 The change of hydrogen bond of four handmade papers in DH and WH aging process	5

SI.6 The change of DP of four handmade papers in DH and WH aging process	10

Reference	11

SI.1. Basic information for four typical kaihua handmade papers

Table S1. Description of four typical Kaihua handmade papers

| Sample |  | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- | --- |
| Raw Material |  | Wikstroemia monnula-A | Green wingceltis | Wikstroemia monnula/Green wingceltis | Wikstroemia monnula-B |
| Grammage（g/m2） |  | 21.09 | 23.81 | 25.24 | 3.25 |
| Thickness（μm） |  | 52.95 | 53.38 | 65.67 | 20.08 |
| Density （g/cm3） |  | 0.38 | 0.45 | 0.38 | 0.16 |
| Whiteness（%） |  | 67.41 | 74.45 | 71.48 | 41.63 |
| Content of cellulose （%） |  | 56.1 | 67.6 | 48.8 | 50.2 |
| Content of lignin（%） |  | 10.43 | 7.6 | 13.04 | 15.15 |
| pH |  | 6.86 | 6.87 | 6.92 | 7.02 |
| color | L | 89.18 | 91.42 | 90.62 | 79.11 |
|  | a | -0.47 | -0.13 | -0.03 | 1.72 |
|  | b | 7.56 | 3.94 | 5.65 | 15.65 |
| Folding endurance |  | 498.67 | 33.67 | 9 | - |
| Tear index (mN·m2/g) |  | 22.47 | 12.12 | 17.29 | 15.34 |
| Degree of polymerization |  | 1205.0 | 446.9 | 511.1 | 1392. |

Fig. S1. Microscopic images of four typical handmade papers

SI.2. The change of FTIR spectra of four handmade papers in DH and WH condition

Fig. S2. Time-dependent FTIR spectra of four handmade papers in DH and WH conditions.

SI.3. The content of carboxyl group and reducing carbonyl group

Fig. S3. Carboxyl group (a, b) and carbonyl group content (c, d) of four typical handmade papers at various aging days in DH and WH condition.

The content of reducing carbonyl group was determined according to the method proposed by Szabolcs and Matija (Kocar et al. 2004). Specifically, 2-10 mg sample was added into 0.5 mL of 0.5% TTC solution and 0.5 mL of 0.5 mol L−1 KOH. The reaction mixture was heated in a water bath at 80℃ for 6 min in an open 10 mL tube. The 9 ml methanol was added after reaction suspension immediate cooling to room temperature. Ultimately, the absorbance was measured at 482 nm by a UV spectrophotometer (UV-1800, Shimadzu Corp). Glucose was used as the standard for the construction of the calibration curve and all results were an average of three determination. Carboxylic acid group content was measured by using conductometric titration methodology. Air dry fibers equivalent to 150 mg of oven dry fibers were added to 50 mL H2O and 5 ml 0.01 M NaCl and stirred for one hour. Finally, the pulp was treated with 0.1 M HCl solution to adjust pH 2.5 and tested.

SI.4. The Crystal-amorphous structure of four handmade papers in DH and WH aging process

Fig. S4. The crystallinity (a), crystal size (b) and d-spacing (c) of four typical handmade papers at various aging days in DH and WH condition.

The crystallinity, crystal size and d-spacing were determined x-ray diffractometer (D8 Advance, Bruker). The crystalline index, crystal size and d-spacing of samples was calculated through the peak area method (Toba et al. 2013)

Cr=IcIc+Ia×100% (Eq. 1)

Ic is the area derived from the peak of crystalline region and Ia is the area derived from amorphous region.

The size of cellulose crystal was calculated via Scherrer equation:

D200= KλBCOSθ200   (Eq. 2)

Where D200 is crystal size (nm) in the direction of (200) plane, k is the Scherrer constant (0.94) of cellulose, λ is the X-ray wavelength (0.1542) nm, B is half bandwidth of (200) diffraction peak in radians and θ200 is the Bragg angle (°) for (200) plane.

Interplanar crystal spacing d was obtained by Bragg equation: d= nλ2sinθ200 (Eq. 3)

SI.5 The change of hydrogen bond of four handmade papers in DH and WH aging process. Table S2a The content of different hydrogen bond form obtained by FTIR Gaussian fitting in DH aging condition. 1#; Aging days; Wave number of peak 1 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å); Wave number of peak 2 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å); Wave number of peak 3 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å). 0; 3458.5; 13.734; 2.7978; 3315.9; 23.961; 2.7658; 3167.1; 34.633; 2.7322. 1; 3458; 13.770; 2.7979; 3316.2; 23.940; 2.7659; 3165.7; 34.734; 2.7319. 3; 3458.3; 13.748; 2.7980; 3316.6; 23.911; 2.7660; 3166.6; 34.669; 2.7321. 5; 3454.9; 13.992; 2.7972; 3315.6; 23.983; 2.7658; 3167.2; 34.626; 2.7323. 7; 3458.6; 13.727; 2.7980; 3316.1; 23.947; 2.7659; 3166.1; 34.705; 2.7320. 14; 3459.2; 13.684; 2.7982; 3316; 23.954; 2.7658; 3166.4; 34.884; 2.7321. 21; 3457.1; 13.834; 2.7977; 3315; 24.026; 2.7656; 3165.2; 34.770; 2.7318. 28; 3450.7; 14.294; 2.7962; 3311; 24.313; 2.7647; 3161.4; 35.042; 2.7309. 42; 3454.2; 14.043; 2.7971; 3313.4; 24.142; 2.7653; 3163.9; 34.863; 2.7315. 56; 3453.9; 14.064; 2.7970; 3313.3; 24.148; 2.7652; 3163.7; 34.877; 2.7315. 70; 3455.6; 13.942; 2.7974; 3314.5; 24.062; 2.7655; 3165; 34.784; 2.7318. 2#; Aging days; Wave number of peak 1 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å); Wave number of peak 2 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å); Wave number of peak 3 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å). 0; 3465.3; 13.246; 2.7996; 3316.1; 23.948; 2.7659; 3162.7; 34.949; 2.7312. 1; 3461.9; 13.490; 2.7988; 3313.2; 24.155; 2.7653; 3160; 35.143; 2.7306. 3; 3460.9; 13.562; 2.7986; 3311.2; 24.299; 2.7648; 3157.5; 35.322; 2.7301. 5; 3459.8; 13.641; 2.7984; 3311.8; 24.256; 2.7649; 3158.3; 35.265; 2.7303. 7; 3462; 13.483; 2.7988; 3312.2; 24.227; 2.7650; 3158.5; 35.251; 2.7303. 14; 3457.8; 13.784; 2.7979; 3309.7; 24.407; 2.7645; 3154.7; 35.523; 2.7295. 21; 3454.8; 14.000; 2.7972; 3307.2; 24.586; 2.7639; 3153.5; 35.609; 2.7292. 28; 3458; 13.770; 2.7979; 3311; 24.313; 2.7648; 3159; 35.214; 2.7304. 42; 3460; 13.627; 2.7984; 3313; 24.169; 2.7652; 3159; 35.215; 2.7304. 56; 3461; 13.555; 2.7986; 3313; 24.169; 2.7652; 3159; 35.215; 2.7304. 70; 3458.5; 13.734; 2.7980; 3310.9; 24.320; 2.7647; 3157; 35.358; 2.7300. 3#; Aging days; Wave number of peak 1 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å); Wave number of peak 2 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å); Wave number of peak 3 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å). 0; 3466.8; 13.139; 2.7999; 3314.9; 24.033; 2.7656; 3163.1; 34.920; 2.7313. 1; 3462.1; 13.476; 2.7988; 3311.1; 24.307; 2.7647; 3159.1; 35.207; 2.7304. 3; 3464; 13.340; 2.7993; 3314.2; 24.084; 2.7654; 3162.9; 34.935; 2.7313. 5; 3457.5; 13.806; 2.7978; 3309.3; 24.435; 2.7643; 3159.2; 35.200; 2.7304. 7; 3462; 13.483; 2.7988; 3314; 24.098; 2.7654; 3161.7; 35.021; 2.7310. 14; 3458.4; 13.741; 2.7980; 3310.5; 24.349; 2.7646; 3159.8; 35.157; 2.7306. 21; 3457.5; 13.806; 2.7978; 3310.9; 24.320; 2.7647; 3159.3; 35.193; 2.7305. 28; 3459; 13.698; 2.7981; 3312; 24.241; 2.7649; 3160; 35.143; 2.7306. 42; 3458.1; 13.763; 2.7979; 3311.2; 24.298; 2.7648; 3160.6; 35.100; 2.7308. 56; 3459; 13.698; 2.7981; 3312; 24.241; 2.7649; 3162; 34.999; 2.7311. 70; 3458; 13.770; 2.7979; 3312; 24.241; 2.7649; 3161; 35.071; 2.730903. Aging days; Wave number of peak 1 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å); Wave number of peak 2 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å); Wave number of peak 3 (cm-1); Hydrogen bond energy (kJ/mol); Hydrogen bond distance (Å). 0; 3476.8; 12.422; 2.8021; 3325.4; 23.281; 2.7680; 3171.3; 34.332; 2.7332. 1; 3474.8; 12.565; 2.8017; 3323.4; 23.423; 2.7675; 3169.9; 34.433; 2.7329. 3; 3475.2; 12.536; 2.8018; 3323.7; 23.402; 2.7676; 3169.5; 34.462; 2.7328. 4#; 5; 3476.9; 12.414; 2.8022; 3324.8; 23.323; 2.7678; 3170; 34.425; 2.7330. 7; 3474.3; 12.601; 2.8016; 3323.5; 23.416; 2.7675; 3170.1; 34.418; 2.7329. 14; 3474.7; 12.572; 2.8017; 3324.7; 23.330; 2.7678; 3169.3; 34.476; 2.7327. 21; 3476.6; 12.436; 2.8021; 3326.8; 23.180; 2.7683; 3173.3; 34.189; 2.7336. 28; 3473.6; 12.651; 2.8014; 3322.2; 23.510; 2.7672; 3167.7; 34.591; 2.7324. 42; 3474; 12.622; 2.8015; 3323.8; 23.395; 2.7676; 3169.5; 34.462; 2.7328. 56; 3473.7; 12.644; 2.8014; 3321.2; 23.581; 2.7670; 3164.9; 34.792; 2.7317. 70; 3473; 12.694; 2.8013; 3321.9; 23.531; 2.7672; 3167.4; 34.612; 2.7323.

| Table S2b The content of different hydrogen bond form obtained by FTIR Gaussian fitting in WH aging condition |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1# | Aging days | Wave number of peak 1 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) | Wave number of peak 2 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) | Wave number of peak 3 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) |
|  | 0 | 3462.6 | 13.440 | 2.7989 | 3316.9 | 23.890 | 2.7660 | 3160.7 | 35.092 | 2.7308 |
|  | 1 | 3463.9 | 13.347 | 2.7992 | 3317.5 | 23.847 | 2.7663 | 3162.7 | 34.949 | 2.7312 |
|  | 3 | 3461.6 | 13.512 | 2.7987 | 3314.9 | 24.033 | 2.7656 | 3160.9 | 35.078 | 2.7308 |
|  | 5 | 3463 | 13.411 | 2.7990 | 3317.7 | 23.832 | 2.7662 | 3164.8 | 34.798 | 2.7317 |
|  | 7 | 3463 | 13.411 | 2.7990 | 3318.6 | 23.768 | 2.7664 | 3165.9 | 34.719 | 2.7320 |
|  | 14 | 3461.7 | 13.504 | 2.7987 | 3316.5 | 23.918 | 2.7660 | 3163.9 | 34.863 | 2.7315 |
|  | 21 | 3461.7 | 13.504 | 2.7987 | 3316.4 | 23.926 | 2.7659 | 3163.7 | 34.877 | 2.7315 |
|  | 28 | 3463.7 | 13.361 | 2.7992 | 3318 | 23.811 | 2.7663 | 3164 | 34.856 | 2.7316 |
|  | 42 | 3463 | 13.411 | 2.7990 | 3318 | 23.811 | 2.7663 | 3165 | 34.784 | 2.7318 |
|  | 56 | 3463 | 13.411 | 2.7990 | 3318 | 23.811 | 2.7663 | 3166 | 34.712 | 2.7320 |
|  | 70 | 3463.5 | 13.375 | 2.7992 | 3318.5 | 23.775 | 2.7664 | 3166 | 34.713 | 2.7320 |
| 2# | Aging days | Wave number of peak 1 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) | Wave number of peak 2 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) | Wave number of peak 3 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) |
|  | 0 | 3460.6 | 13.583 | 2.7985 | 3311.1 | 24.306 | 2.7647 | 3155.5 | 35.465 | 2.7296 |
|  | 1 | 3457 | 13.842 | 2.7977 | 3310.2 | 24.371 | 2.7645 | 3157.4 | 35.329 | 2.7300 |
|  | 3 | 3457.4 | 13.813 | 2.7978 | 3308.8 | 24.471 | 2.7642 | 3156.6 | 35.386 | 2.7299 |
|  | 5 | 3461.5 | 13.519 | 2.7987 | 3312.2 | 24.227 | 2.7650 | 3158.4 | 35.257 | 2.7303 |
|  | 7 | 3457.3 | 13.820 | 2.7977 | 3310.1 | 24.377 | 2.7645 | 3159.4 | 35.186 | 2.7305 |
|  | 14 | 3457.5 | 13.806 | 2.7978 | 3310.9 | 24.320 | 2.7647 | 3160.4 | 35.114 | 2.7307 |
|  | 21 | 3457.5 | 13.806 | 2.7978 | 3309.3 | 24.435 | 2.7643 | 3158.2 | 35.272 | 2.7302 |
|  | 28 | 3457.2 | 13.827 | 2.7977 | 3310.2 | 24.371 | 2.7645 | 3160.4 | 35.114 | 2.7307 |
|  | 42 | 3461.9 | 13.491 | 2.7988 | 3312.4 | 24.213 | 2.7650 | 3159.2 | 35.200 | 2.7304 |
|  | 56 | 3457.1 | 13.835 | 2.7977 | 3310.5 | 24.349 | 2.7646 | 3158.9 | 35.221 | 2.7304 |
|  | 70 | 3459 | 13.699 | 2.7981 | 3313.1 | 24.162 | 2.7652 | 3160.6 | 35.100 | 2.7308 |
| 3# | Aging days | Wave number of peak 1 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) | Wave number of peak 2 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) | Wave number of peak 3 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) |
|  | 0 | 3461.7 | 13.505 | 2.7987 | 3315.3 | 24.004 | 2.7657 | 3166.8 | 34.655 | 2.7322 |
|  | 1 | 3461.7 | 13.505 | 2.7987 | 3315.3 | 24.004 | 2.7657 | 3167.8 | 34.583 | 2.7324 |
|  | 3 | 3456.1 | 13.907 | 2.7975 | 3315.9 | 23.961 | 2.7658 | 3175 | 34.067 | 2.7340 |
|  | 5 | 3461 | 13.555 | 2.7986 | 3315.7 | 23.976 | 2.7658 | 3164.1 | 34.849 | 2.7316 |
|  | 7 | 3455.7 | 13.935 | 2.7974 | 3315.4 | 23.997 | 2.7657 | 3276.5 | 26.787 | 2.7569 |
|  | 14 | 3456.4 | 13.885 | 2.7975 | 3314.9 | 24.033 | 2.7656 | 3174.3 | 34.117 | 2.7339 |
|  | 21 | 3454.6 | 14.014 | 2.7971 | 3312.7 | 24.191 | 2.76514 | 3172.4 | 34.253 | 2.7334 |
|  | 28 | 3454.5 | 14.021 | 2.7971 | 3312.6 | 24.198 | 2.76512 | 3170.1 | 34.418 | 2.7329 |
|  | 42 | 3462 | 13.483 | 2.7988 | 3314.3 | 24.076 | 2.7655 | 3175.8 | 34.009 | 2.7342 |
|  | 56 | 3462 | 13.483 | 2.7988 | 3313.5 | 24.133 | 2.7653 | 3169.7 | 34.447 | 2.7328 |
|  | 70 | 3461.5 | 13.519 | 2.7987 | 3314.6 | 24.055 | 2.7655 | 3171.6 | 34.311 | 2.7332 |
|  | Aging days | Wave number of peak 1 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) | Wave number of peak 2 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) | Wave number of peak 3 (cm-1) | Hydrogen bond energy (kJ/mol) | Hydrogen bond distance (Å) |
|  | 0 | 3470.7 | 12.859 | 2.8008 | 3322.6 | 23.481 | 2.7673 | 3168.3 | 34.547 | 2.7325 |
|  | 1 | 3466.7 | 13.146 | 2.7999 | 3320.4 | 23.639 | 2.7668 | 3168.4 | 34.540 | 2.7325 |
|  | 3 | 3467.5 | 13.089 | 2.8001 | 3320.1 | 23.660 | 2.7668 | 3168.6 | 34.526 | 2.7326 |
| 4# | 5 | 3470.3 | 12.888 | 2.8007 | 3323.2 | 23.438 | 2.7675 | 3171.6 | 34.311 | 2.7332 |
|  | 7 | 3471.5 | 12.802 | 2.8009 | 3323.7 | 23.402 | 2.7676 | 3170.6 | 34.382 | 2.7330 |
|  | 14 | 3470.4 | 12.881 | 2.8007 | 3322.9 | 23.459 | 2.7674 | 3169.7 | 34.447 | 2.7328 |
|  | 21 | 3466.2 | 13.182 | 2.7997 | 3320.3 | 23.646 | 2.7668 | 3167.3 | 34.619 | 2.7323 |
|  | 28 | 3465.2 | 13.253 | 2.7995 | 3320.8 | 23.610 | 2.7669 | 3168.4 | 34.540 | 2.7325 |
|  | 42 | 3464.5 | 13.304 | 2.7994 | 3317.6 | 23.839 | 2.7662 | 3164.4 | 34.827 | 2.7316 |
|  | 56 | 3466.9 | 13.132 | 2.7999 | 3316.1 | 23.947 | 2.7659 | 3164.7 | 34.806 | 2.7317 |
|  | 70 | 3469 | 12.981 | 2.8004 | 3322 | 23.524 | 2.7672 | 3170 | 34.426 | 2.7329 |

We obtained energy and distance of hydrogen bond in DH (Table S2a) and in WH (Table S2b) condition. The hydrogen bonds peaks were obtained by deconvolution and peak-fitting from FTIR spectrum. Specifically, the hydrogen bond energy was calculated using following equation (PimentelSederholm 1956; Yuan et al. 2013):

EH=1K[V0-VV0]   (Eq. 4)

V0 - the frequency of standard free hydroxyl group（3650 cm-1）；

V- the frequency of the hydroxyl group calculated in the sample (cm-1)

K - constant（3.82×103 Kj-1）

The hydrogen bond distance D was calculated using the Sederholm equation:

△v (cm-1) = 4.43×103 (2.82-D)  (Eq. 5)

△v=v0-v

v0 - the stretching vibration frequency of single hydroxyl group（3600 cm-1）

v - the frequency of the hydroxyl group calculated in the sample（cm-1）

SI.6 The change of DP of four handmade papers in DH and WH aging process

Fig. S5. The DP values of various aging time for four handmade papers in DH (a) and WH (b) condition.

Reference

Kocar D, Pedersoli J L, Strlic M, Kolar J, Rychly J, Matisova-Rychla L (2004) Chemiluminescence from paper II. The effect of sample crystallinity, morphology and size. Polymer Degradation and Stability 86(2): 269-274.

Pimentel G C, Sederholm C H (1956) Correlation of infrared stretching frequencies and hydrogen bond distances in crystals. Journal of Chemical Physics 24(4): 639-641.

Toba K, Yamamoto H, Yoshida M (2013) Crystallization of cellulose microfibrils in wood cell wall by repeated dry-and-wet treatment, using X-ray diffraction technique. Cellulose 20(2): 633-643.

Yuan L, Wan J, Ma Y, Wang Y, Huang M, Chen Y (2013) The content of different hydrogen bond models and crystal structure of eucalyptus fibers during beating. BioResources 8(1): 717-734.