Table 1 General characteristics of oxytetracycline hydrochloride

Synonym: 5-Hydroxytetracycline hydrochloride   Molecular formula: C22H24N2O9.HCl

Molecular structure:

Chemical class: Antibiotic                                   Molecular weight:  496.9 g/mol

pKa: 3.22; 7.46; 8.94                                            Ionization: Acidic, basic, zwitter ion

Molecular volume (nm3): 0.413                          Molecular dimensions (nm): 1.26 ×0.82 ×0.53

Maximum wavelength: 274 nm

Table 2 Pore, surface chemical, and magnetic properties of BAC (Teymur et al. 2023) and CuF@BAC

Pore properties                                  Surface chemical properties             Magnetic properties

BAC    CuF@BAC

_____   __________

SBET (m2/g)   	 2211     455              Carboxylic (mEq/g)          0.5312       Ms (emu/g)   15.01

VT (cm3/g)       1.262    0.280           Phenolic (mEq/g)              0.0124       Mr (emu/g)   0.73

Vm (cm3/g)       0.502    0.099           Lactonic (mEq/g)              0.5014       Hc   (Oe)       80.0

VM (cm3/g)      0.760    0.181           Total acidity (mEq/g)        1.0450

Vm (%)             39.8      35.5             Total basicity (mEq/g)      1.1838

VM (%)             60.2      64.5             pHZPC                                8.24

DP (nm)            2.8        2.5

† SBET: Brunauer-Emmett-Teller surface area; VT: total pore volume; Vm: micropore volume; VM: mesopore volume (VT-Vm); Vm (%): micropore contribution ((Vm/VT) × 100); VM (%): mesopore contribution (100-Vm%); DP: average pore diameter; pHZPC: point of zero charge; Ms: saturation magnetization; Mr: residual magnetization; Hc: intrinsic coercivity.

Table 3 Linearized form of the kinetic and isotherm models, and thermodynamics equations used in this study

Classification                 Equation                                  Plot                       Slope        Intercept

Kinetic models

Pseudo-first-order:                  vs t       k1              lnQe

Pseudo-second-order:                          vs t

Isotherm models

Freundlich:                               lnQe vs lnCe                        lnKF

Langmuir:                                    vs Ce

Thermodynamic

Gibbs-Helmholtz

;

vs

† k1 (1/min): constant rate for the pseudo-first-order model; k2 (g/mg min): rate constant for the  pseudo-second-order model; Qm (mg/g): the maximum sorption capacity;  KL: sorption equilibrium constant; KF: sorption equilibrium constant related to sorption capacity; n: Freundlich constant related to sorption density; ΔGo (kJ/mol): Gibbs free energy change;  ΔHo (kJ/mol): average enthalpy change; ΔSo (kJ/mol K): average entropy change; R (8.314 J/mol/K): the universal gas constant and T (K): the absolute temperature; : the dimensionless equilibrium constant;  Mw(g/mol): the molecular weight of the sorbate; γ: the dimensionless activity coefficient of the sorbate, which is assumed to be 1.0 for dilute solutions under standard conditions; Co: the standard sorbate concentration taken as 1 mol/L; ge: an equilibrium coefficient equal to 1 for diluted solutions.

Table 4 Kinetic parameters for sorption at different OTC concentrations onto CuF@BAC

Models:                  Pseudo-first-order                                  Pseudo-second-order

____________________________        _____________________________

C0          Qe,exp        Qe,cal       k1x10-2   R2                Δq%               Qe,cal         k2 x10-3       R2               Δq%

650       150.5        20.78      1.45        0.9645    3.87           151.5        2.72         0.9998    1.91

700       205.9        89.94      1.40        0.9449    3.41           212.8        4.26         0.9981    1.22

800       225.8        55.81      1.01        0.9673    3.22           226.9        7.08         0.9993    0.74

† (C0: mg/L; Qe,exp: mg/g; Qe,cal: mg/g; k1: 1/min; k2: g/mg min); kid: mg/g min1/2; I: mg/g.

Table 5 Isotherm and thermodynamics parameters for OTC sorption onto CuF@BAC at different temperatures

Models: Freundlich                           Langmuir                                            Thermodynamic

_____________________  _____________________________   ________________

T (K)   KF     1/n      R2          Δq%      Qm   KL          R2         Δq%    RL        ΔGo    ΔHo     ΔSo

293      17.0   0.79   0.8975   2.98       588   0.0018   0.9778   2.02   0.632    -16.5   23.1   0.130

303      23.0   0.46   0.8776   2.55       615   0.0024   0.9864   1.54   0.546    -17.8

313      26.6   0.41   0.8365   1.89       669   0.0033   0.9935   1.01   0.447    -18.9

†KF: (mg/g)(L/mg)1/n; Qm: mg/g;  KL: L/mg; ∆Go: kJ/mol; ∆Ho: kJ/mol; ∆So: kJ/mol K.

Table 6 Comparison of maximum OTC sorption capacity of CuF@BAC with some nanocomposite sorbents reported in the literature

Sorbent                                  Sorption conditions        Qm (mg/g)     References

Fe3O4@Graphene                  pH:2.9; T: 313 K            336                 Zhang et al. (2017)

MnO2/Corn stalks BC            pH:7.0; T: 303 K             40                  Gao et al. (2018)

CuF/NiMgAl-LDH               pH:4.0; T: 323 K             192                 Eniola et al. (2020)

FeCl3/garlic skin BC             pH: 6.5; T:298 K            822                  Feng et al. (2022)

MnF@BAC                           pH:2.9; T: 313 K            592                 Teymur and Güzel (2024)

Mg-Fe/suaeda salsa BC         pH: -; T: 303 K                83                 Jiang et al. (2024)

CuF@BAC                                    pH:2.9; T: 313 K            669                 Present study

†CuF: CuFe2O4; MnF: MnFe2O4; AC: Activated carbon; BC: Biochar; LDH: Layered double hydroxide.