Table 2: Scope of various arylamines reacting with dimedone in presence of MnMoO4 as catalyst

| 3a Yield: 95% | 3b Yield:92% | 3c Yield:93% |
| --- | --- | --- |
| 3d Yield:91% | 3e Yield:89% | 3f Yield: 85% |
| 3g Yield: 83% | 3h Yield:84% | 3i Yield: 81% |
| 3j Yield: 81% | 3k Yield: 75% | 3l Yield: 86% |
| Reaction condition: 1.0 mmol of Arylamine, 1.2 mmol of dimedone in 10 mL acetonitrile, 20 mg of MnMoO4catalyst and stirred for 20 min at room temperature |  |  |