Non-wetting and Conductive Janus Structure for High-Performance Electronics Enabled by Gradient Polarity Driven Hierarchical Spatial Assembly
Shanshan Jiaa,1, Shijie Daia,1, Yiqiang Wub,*, Guoxi Chena, Bin Zhoua, Qi Chena, Shaobo Zhanga, Yao Luc,*, Zhiping Sua,*, Yan Qingb
a College of Forestry, Sichuan Agricultural University, Chengdu 611130, P.R. China
b College of Materials Science and Engineering, Central South University of Forestry and Technology, Changsha 410004, P. R. China

c Department of Chemistry, School of Physical and Chemical Sciences, Queen Mary University of London, London E1 4NS, UK. 
Corresponding Authors

Email address: qingyan0429@163.com, yao.lu@qmul.ac.uk, suzp@sicau.edu.cn. 
[image: image1.jpg]Treated

Treated

Cottoh

Treated

50um





Fig. S1. The Janus-HC-NW on wood, paper, textile, sponge, cotton and glass.

[image: image2.png]155

150

145

140

Contact angle (°)

135

0.4 % MWCNTs

0.0 0.2 0.4 0.6 0.8

MWCNT content (wt%)




Fig. S2. Effect of MWCNT on electrical conductivity and hydrophobicity of this coating.

[image: image3.png]Janus-HC-NW Conventional
@ 154,10 b 139,70





Fig. S3. Water contact angle of Janus-HC-NW coated wood surface (a) and conventionally coated wood surface (b).

[image: image4.png]RO OR
VTES




Fig. S4. The process of VTES combining with hydrophilic TiO2。
[image: image5.png]VTES Tio, MWCNT
P
¥ 3 e 2
':‘ﬁ 4 ‘? ;j..a {( j
¢ Pite/ 11155
J.
VTES@VTES VTES@TIO, VTES@MWCNT
. .
J!
J. g & :"4 o oﬁ’
2 e vees i
J*¢J ot D 1 ?/#ij ¥ .a”‘
¢ -f e., &’q - gﬁg‘;&
AE=2819.34 kcal/mol AE=7303.6 kcal/mol AE=1533.86kcal/mol
®o @ H ®si é®C




Fig. S5. Models of VTES, TiO2, MWCNT, VTES@VTES, VTES@TiO2 and VTES@MWCNT.

[image: image6.png]a ., Janus-HC-NW

00

o0

Cycle

ARR,

Conventional

) 20 o & 8 100
Cycle




Fig. S6. Stability of Janus-HC-NW coated wood sponge (a) and conventionally coated wood sponge (b) under 30% shape variable.

[image: image7.png]



Fig. S7. The conversion result by mathematical analysis.
Table. S1. Binding energy and total energy of different combinations.

	Material
	Total energy (kcal/mol)
	Binding energy ((kcal/mol))

	MWCNT
	-191.3788507
	-

	VTES
	-21.36391671
	-

	TiO2
	-103.9802909
	-

	VTES@VTES
	-47.220812
	-4.492978578

	VTES@TiO2
	-136.9834081
	-11.6392004

	VTES@MWCNT
	-215.2397623
	-2.496994825


