# Appendix

Appendix 1: Experimental data of experiments with activated DLC; P1…period 1; P3…period 3

| Test | DLC | Viscosity / mPas | sp3 content / % | Wear Rate nm/h | Lubricant Type | Hydro-genated | OX- number | COF | Roughness Sa / µm | Hardness GPa |  | Initial Hertzian Pressure MPa |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | ta-C | 0.94 | 69 | 64.5 (P1) | 1 | 0 | 0 | 0.109 | 171 |  | 27 | 986 |
| 2 | ta-C | 0.94 | 69 | 31.5 (P3) | 1 | 0 | 0 | 0.158 | 171 |  | 27 | 986 |
| 3 | ta-C | 0.94 | 69 | 18 (P1) | 1 | 0 | 0 | 0.098 | 171 |  | 27 | 986 |
| 4 | ta-C | 0.94 | 69 | 12 (P3) | 1 | 0 | 0 | 0.145 | 171 |  | 27 | 986 |
| 5 | ta-C | 2.17 | 69 | 29.5 (P1) | 0 | 0 | 0 | 0.185 | 171 |  | 27 | 986 |
| 6 | ta-C | 2.17 | 69 | 22.5 (P3) | 0 | 0 | 0 | 0.238 | 171 |  | 27 | 986 |
| 7 | ta-C | 2.17 | 69 | 18 (P1) | 0 | 0 | 0 | 0.219 | 171 |  | 27 | 986 |
| 8 | ta-C | 2.17 | 69 | 28.5 (P3) | 0 | 0 | 0 | 0.249 | 171 |  | 27 | 986 |
| 9 | ta-C | 2.92 | 69 | 15 (P1) | 0 | 0 | 10 | 0.131 | 171 |  | 27 | 986 |
| 10 | ta-C | 2.92 | 69 | 2.5 (P3) | 0 | 0 | 10 | 0.069 | 171 |  | 27 | 986 |
| 11 | ta-C | 2.92 | 69 | 28 (P1) | 0 | 0 | 10 | 0.133 | 171 |  | 27 | 986 |
| 12 | ta-C | 2.92 | 69 | 3 (P3) | 0 | 0 | 10 | 0.14 | 171 |  | 27 | 986 |
| 13 | a-C | 0.94 | 56 | 30.5 (P1) | 1 | 0 | 0 | 0.275 | 60 |  | 29 | 1010 |
| 14 | a-C | 0.94 | 56 | 32 (P3) | 1 | 0 | 0 | 0.263 | 60 |  | 29 | 1010 |
| 15 | a-C | 2.17 | 56 | 15 (P1) | 0 | 0 | 0 | 0.139 | 60 |  | 29 | 1010 |
| 16 | a-C | 2.92 | 56 | 6 (P3) | 0 | 0 | 10 | 0.187 | 60 |  | 29 | 1010 |
| 17 | a-C | 2.92 | 56 | 10 (P1) | 0 | 0 | 10 | 0.182 | 60 |  | 29 | 1010 |
| 18 | a-C:H | 0.94 | 54 | 59 (P3) | 1 | 1 | 0 | 0.188 | 73 |  | 19 | 899 |
| 19 | a-C:H | 0.94 | 54 | 19.5 (P1) | 1 | 1 | 0 | 0.192 | 73 |  | 19 | 899 |
| 20 | a-C:H | 0.94 | 54 | 23.5 (P3) | 1 | 1 | 0 | 0.257 | 73 |  | 19 | 899 |
| 21 | a-C:H | 2.17 | 54 | 15.5 (P1) | 0 | 1 | 0 | 0.286 | 73 |  | 19 | 899 |
| 22 | a-C:H | 2.17 | 54 | 4.5 (P3) | 0 | 1 | 0 | 0.286 | 73 |  | 19 | 899 |
| 23 | a-C:H | 2.92 | 54 | 3.5 (P1) | 0 | 1 | 10 | 0.098 | 73 |  | 19 | 899 |
| 24 | a-C:H | 2.92 | 54 | 6 (P3) | 0 | 1 | 10 | 0.09 | 73 |  | 19 | 899 |
| 25 | a-C:H(CrN) | 0.94 | 46 | 46 (P1) | 1 | 1 | 0 | 0.189 | 354 |  | 16 | 852 |
| 26 | a-C:H(CrN) | 0.94 | 46 | 23.5 (P3) | 1 | 1 | 0 | 0.235 | 354 |  | 16 | 852 |
| 27 | a-C:H(CrN) | 2.17 | 46 | 5.5 (P1) | 0 | 1 | 0 | 0.163 | 354 |  | 16 | 852 |
| 28 | a-C:H(CrN) | 2.17 | 46 | 2 (P3) | 0 | 1 | 0 | 0.166 | 354 |  | 16 | 852 |
| 29 | a-C:H(CrN) | 2.92 | 46 | 5 (P1) | 0 | 1 | 10 | 0.126 | 354 |  | 16 | 852 |
| 30 | a-C:H(CrN) | 2.92 | 46 | 1.5 (P3) | 0 | 1 | 10 | 0.095 | 354 |  | 16 | 852 |

Appendix 2: Wear rates of DLC and counter body during the different periods and with different lubricants. The uncertainty is roughly ± 40% including tribological testing, averaging over test periods with the same loading conditions, as well as measurement uncertainties. [39]

| Group | DLC coating label | Lubricant | Activated material / body | DLC-wear rate in nm/h |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Period 1 | Period 2 | Period 3 | Averaged wear rate Period 1 Period 2 Period 3 |
| A | ta-C | Water | DLC coating | 41 | 20 | 22 | Water lubricant 40 9 25 |
| B | a-C | Water |  | 30 | 6 | 31 |  |
| C | a-C:H(1) | Water |  | 44 | 8 | 23 |  |
| D | a-C:H(2) | Water |  | 46 | 1 | 23 |  |
| E | ta-C | Diesel |  | 24 | 0 | 25 | Diesel lubricant 16 0 10 |
| F | a-C | Diesel |  | 20 | 0 | 9 |  |
| G | a-C:H(1) | Diesel |  | 15 | 0 | 4 |  |
| H | a-C:H(2) | Diesel |  | 5 | 1 | 2 |  |
| I | ta-C | OX10 |  | 21 | 4 | 3 | Diesel OX10 lubricant 9 2 5 |
| J | a-C | OX10 |  | 6 | 0 | 10 |  |
| K | a-C:H(1) | OX10 |  | 4 | 0 | 6 |  |
| L | a-C:H(2) | OX10 |  | 5 | 4 | 2 |  |
|  |  |  |  | Counter body running-in wear depth in nm |  |  | Counter body wear-rate in nm/h |
| M | a-C:H(3) | Water | Steel counter body | 1050 |  |  | 1224 |
| N | a-C:H(3) | Diesel |  | 1838 |  |  | 80 |
| O | a-C:H(3) | OX2 |  | 848 |  |  | 38 |
| P | a-C:H(3) | OX10 |  | 790 |  |  | 30 |

Appendix 3: Content in atomic percent (%) of C1s und O1s Peaks of the XPS analysis ±12 % from ta-C and a-C:H(1).

| C1s peak |  | Reference |  | Water |  | Diesel |  | Aged Diesel OX10 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | ta-C | a-C:H | ta-C | a-C:H | ta-C | a-C:H | ta-C | a-C:H |
| Not sputtered | O=C-O | 3 | 4 | 4 | 2 | 4 | 2 | 4 | 3 |
|  | C-O | 91 | 31 | 54 | 62 | 61 | 64 | 52 | 72 |
|  | sp³ | 6 | 40 | 30 | 7 | 23 | 9 | 31 | 8 |
|  | sp² | 1 | 25 | 12 | 29 | 12 | 25 | 13 | 18 |
|  | sp³ content (sp³+sp²=100%) | 82 | 61 | 72 | 20 | 66 | 26 | 70 | 31 |
| Sputtered | O=C-O | 2 | 1 | 3 | 0 | 3 | 0 | 2 | 1 |
|  | C-O | 15 | 2 | 7 | 1 | 7 | 1 | 6 | 2 |
|  | sp³ | 33 | 15 | 21 | 16 | 21 | 12 | 25 | 10 |
|  | sp² | 50 | 83 | 70 | 83 | 69 | 87 | 67 | 87 |
|  | sp³ content (sp³+sp²=100%) | 40 | 15 | 23 | 16 | 23 | 12 | 27 | 10 |

| O1s peak |  | Reference |  | Water |  | Diesel |  | Aged Diesel OX10 |  |  | Deposit a-C:H |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | ta-C | a-C:H | ta-C | a-C:H | ta-C | a-C:H | ta-C | a-C:H | in DLC wear track |  | on DLC |
| Not sputtered | C-O | 7 | 28 | 14 | 8 | 22 | 3 | 9 | 3 | 20 |  | 13 |
|  | MeOx | 1 | 2 | 2 | 1 | 2 | 1 | 3 | 1 | 3 |  | 7 |
|  | OH | 30 | 1 | 6 | 2 | 6 | 0 | 4 | 2 | 2 |  | 6 |
|  | C-OH | 62 | 69 | 79 | 89 | 69 | 94 | 84 | 94 | 76 |  | 73 |
| Sputtered | C-O | 50 | 46 | 75 | 50 | 74 | 54 | 73 | 57 |  |  |  |
|  | MeOx | 13 | 20 | 7 | 5 | 8 | 7 | 3 | 6 |  |  |  |
|  | OH | 5 | 3 | 5 | 5 | 5 | 7 | 5 | 5 |  |  |  |
|  | C-OH | 31 | 30 | 13 | 40 | 14 | 30 | 20 | 32 |  |  |  |