Supporting Information

Copolyfluorenes containing polymethine dyes in the main chain: synthesis and photophysical properties

Elena V. Zhukova, Alexander M. Mitroshin, Ksenia I. Kaskevich, Serguei A. Miltsov, Larisa S. Litvinova, Tatiana G. Chulkova, Alexander V. Yakimansky

Branch of Petersburg Nuclear Physics Institute Named by B.P. Konstantinov of National Research Centre “Kurchatov Institute” – Institute of Macromolecular Compounds, 31 Bolshoy pr. V.O., St. Petersburg, 199004 Russia

Synthesis of polymethine dyes

Preparation of  5-bromo-1-ethyl-2,3,3-trimethylindoleninium iodide 11, N-(3-anilino-2-propenylidene)aniline hydroperchlorate 22, 1-ethyl-2,3,3-trimethylindoleninium iodide  43, 2-[4-(acetylphenylamino)-1,3-butadien-1-yl]-1-ethyl-3,3-dimethyl-3H-indolium  perchlorate 54 and 2,5-bis-dimethylaminomethylenecyclopentanone 85 was performed according to the published protocols.

1. M. V. Reddington. Synthesis and properties of phosphonic acid containing cyanine and squaraine dyes for use as fluorescent labels. Bioconjugate Chem. 2007, 18 (6), 2178–2190.

DOI: 10.1021/bc070090y

2. D. Lloyd, H. McNab, D. R. Marshall. Diazepines. XVII. Simple preparation of 2,3-dihydro-1H-1,4-diazepinium perchlorate. Synthesis 1973, (12), 791.

DOI: 10.1055/s-1973-22305

3. J. S. Lindsey,  P. A. Brown,  D. A. Siesel. Visible light-harvesting in covalently-linked porphyrin-cyanine dyes. Tetrahedron. 1989, 45(15), 4845-4866.

DOI: 10.1016/s0040-4020(01)85156-5

4.  S. Miltsov, M. Goikhman, A. Yakimansky, A. Misharev, M. Puyol, J. Alonso. N-Bromosuccinimide-mediated dimerization of unsymmetrical indodicarbocyanine dyes. Tetrahedron Lett. 2019, 60, 151005.

DOI: 10.1016/j.tetlet.2019.151005

5. Yu. L. Slominskii, I. D. Radchenko,  S. V. Popov, A. I.  Tolmachev. Polymethine dyes with hydrocarbon bridges. Enamine ketones in the chemistry of cyanine dyes. Zh. Org. Khim. 1983,

19(10), 2134-2142.

3H-Indolium, 2-[5-(1-ethyl-1,3-dihydro-5-bromo-3,3-dimethyl-2H-indol-2-ylidene)-1,3-pentadien-1-yl]-1-ethyl-5-bromo-3,3-dimethyl-, perchlorate 3

Acetic anhydride (200 mg, 2 mmol) was added dropwise to a solution of N-(3-anilino-3-propenylidene)aniline perchlorate 2 (323 mg, 1 mmol) and diisopropylethylamine (DIEA, 0.38 ml, 2 mmol) in 7 ml of CH2Cl2.  The mixture was kept at room temperature for 3 hours and added to the solution of salt 1 (788 mg, 2 mmol) and anhydrous sodium acetate (430 mg, 5.2 mmol) in 25 ml of methanol. Methylene chloride was distilled off and the remaining methanol solution was heated at reflux for 8 hours. After reducing to 10 ml the solution was kept at -15 0C overnight. The resulted crystals were washed with ether, water and ether again, and dried on air. Yield 486 mg (73%).

1H NMR (400 MHz, DMSO-d6) 1.26 (m, 6H), 1.68 (s, 12), 4.13 (m, 4H), 6.30 (d, J = 14 Hz, 2H), 6.58 (m, 1H), 7.36 (d, J =  8.5 Hz, 2H),  7.58 (dd, J  =  8.5 Hz, J  =  2 Hz, 2H),  7.92 (d, J = 2 Hz, 2H),  8.33 (m, 2H). 13C NMR (100 MHz, DMSO-d6) 12.6, 27.3, 39.2, 49.6, 103.6, 113.2, 117.5, 126.3, 126.4, 131.6, 141.4, 144.1, 155.1, 172.5. HRMS (ESI+), m/z: 567.0991 (calcd. 567.1010 for C29H33Br2N2). UV-Vis: λabs (EtOH) = 651.5 nm (ε = 2.50∙105 M1cm1).  Fluor.: λem (EtOH) = 668 nm.

1-Ethyl-2-[(1E,3E,5E)-5-(1-ethyl-1,3-dihydro-5-bromo-3,3-dimethyl-2H-indol-2-ylidene)-1,3-pentadien-1-yl]-3,3-dimethyl-3H-indolium perchlorate (6)

Acetylated hemicyanine 5 (1.836 g, 4 mmol), indoleninium salt 1 (4 mmol) and anhydrous sodium acetate (400 mg, 4.82 mmol) in 30 ml of MeOH were heated at reflux for 1 hour. After evaporation to dryness in vacuo the residue was triturated with water (50 ml) filtered and dried on air. The dye was purified by column chromatography on silica (0 – 5% MeOH in CH2Cl2).  Yield 1.86 g (79%).

1H NMR (400 MHz, DMSO-d6)   1.20 – 1.35 (m, 6H), 1.69 (s, 12 H),  4.03 – 4.15 (m, 2H), 4.15 – 4.27 (m, 2H),   6.24 (d, J = 13 Hz, 1H), 6.39 (d, J = 13 Hz, 1H), 6.58 (m, 1H),), 7.25 – 7.36 (m, 2H),  7.39 – 7.50 (m, 2H),  7.57 (d, J = 8 Hz, 1H) 7.67 (d, J = 8 Hz, 1H),  7.91 (s, 1H), 8.26 – 8.44 (m, 4H).  13C NMR (100 MHz, DMSO-d6) 12.4, 12.8, 27.4, 27.4, 39.9, 49.2, 49.7, 102.7, 103.3, 111.8, 112.8, 116.9, 123.0, 125.7, 126.2, 129.0, 131.5, 141.6, 141.9, 141.9, 142.0, 143.9, 154.2, 155.4, 171.3, 173.9. HRMS (ESI+), m/z: 489.1908 [M]+ (calcd. 489.1905 for C29H34BrN2). UV-Vis: λmax (EtOH) = 647 nm.

10,10-Bis(5-bromo-1,1′-diethyl-3,3,3′,3′-tetramethylindodicarbocyanine) diiodide (7)

Dicarbocyanine 6 (589 mg, 1 mmol) was dissolved in CHCl3 (30 ml), heated to reflux and NIS (337 mg, 1.5 mmol) were added in three portions during 15 min. and reflux was continued for 1 h more. After evaporation to dryness in vacuo, the residue was triturated with water (50 ml), filtered and dried on air. The product was purified by column chromatography on silica (0 – 5% MeOH in CH2Cl2), resulting in 432 mg (73%) of 7.

1H NMR (400 MHz, DMSO-d6) 0.95 – 1.15 (m, 12H), 1.81 (s, 24 H),  3.88 (m, 4H), 3.98 (m, 4H), 5.66 (d, J = 14 Hz, 2H),  5.78 (d, J = 14 Hz, 2H),  7.24 – 7.37 (m, 4H),  7.38 – 7.48 (m, 4H),  7.55 (d, J = 8 Hz, 2H),  7.71 (d, J = 8 Hz, 2H), 7.99 (s, 2H), 8.52 – 8.72 (m, 4H).  13C NMR (100 MHz, DMSO-d6) 12.3, 12.6, 27.4, 27.4, 39.1,  49.6, 45.0, 100.5, 101.8, 112.0, 113.1,  117.6, 123.2,  126.1, 126.4,  127.5,  129.1, 131.6, 141.3,  141.7, 142.0, 144.0, 153.1,  154.2, 172.1, 174.2. HRMS (ESI+), m/z: 488.1828 [M2+] (calcd. 488.1827 for C58H66Br2N4/2).  UV-Vis: λabs (EtOH) = 640 nm (ε = 2.16∙105 M1cm1); 597 nm (ε = 1.65∙105 M1cm1).

2,5-Bis-[2-(1-ethyl-1,3-dihydro-5-bromo-3,3-dimethyl-2H-indol-2-ylidene)ethylydene]-cyclopentanone  9

Salt 1 (788 mg, 2 mmol) и 2,5-bis-dimethylaminomethylenecyclopentanone 8 (194 mg, 1 mmol) in pyridine (10 ml) were heated to reflux for 2 h. cooling the mixture was poured in ice-water (100 ml), the precipitate formed was filtered, dried and recrystallized from MeOH. Yield: 507 mg (82%).

1H NMR (400 MHz, DMSO-d6)   1.16 (t, J = 7 Hz, 6H), 1.57 (s, 12), 2.68 s, 6H), 3.79 (q, J = 7 Hz, 4H), 5.42 (d, J = 13 Hz, 2H),  6.89 (d, J  =  8 Hz, 2H),  7.37 (dd, J  =  8 Hz, J  =  1.5 Hz, 2H),  7.47 (d, J  =  13 Hz, 2H), 7.56 (d, J = 1.5 Hz, 2H). 13C NMR (100 MHz, DMSO-d6)  11.3, 23.5, 28.3,  37.1, 46.6, 93.8, 109.4, 112.5, 125.5, 127.5, 131.0, 132.8, 141.9, 143.1, 161.0. UV-Vis: λabs(base) (EtOH) = 540 nm.  Fluor.: λem(base) (EtOH) = 638 nm. UV-Vis: λabs(acid) (EtOH) = 719 nm.  Fluor.: λem(acid) (EtOH) = 747 nm.

3H-Indolium, 5-bromo-2-[[3-[(5-bromo-1-ethyl-1,3-dihydro-3,3-dimethyl-2H-indol-2-ylidene)methyl]-2-hydroxy-4-oxo-2-cyclobuten-1-ylidene]methyl]-1-ethyl-3,3-dimethyl-, inner salt 10

Squaric acid (114 mg, 1 mmol), salt 1 (788 mg, 2 mmol) and quinoline (516 mg, 8 mmol) in the mixture of benzene (20 ml)  and n-butanol (20 ml) were kept at reflux with Dean-Stark trap for 6 h. After removal of solvents the product was recrystallized from MeOH. Yield: 480 mg (79 %).

1H NMR (400 MHz, DMSO-d6)   1.27 (t, J = 7 Hz, 6H), 1.70 (s, 12H), 4.12 (q, J = 7 Hz, 4H), 5.80 (s, 2H), 7.32 (d, J  =  8.5 Hz, 2H),  7.55 (dd, J  =  8.5 Hz, J  =  1.5 Hz, 2H),  7.81 (d, J  =  2 Hz, 2H). 13С NMR was not measured because of low solubility. UV-Vis: λmax (EtOH) = 638 nm. Fluor.: λem (EtOH) = 646 nm.

Fig. S1 The 1H NMR (400 MHz, DMSO-d6) spectrum of 3

Fig. S2 The 13C NMR (100 MHz, DMSO-d6) spectrum of 3

Fig. S3 The 1H NMR (400 MHz, DMSO-d6) spectrum of 6

Fig. S4 The 13C NMR (100 MHz, DMSO-d6) spectrum of 6

Fig. S5 The 1H NMR (400 MHz, DMSO-d6) spectrum of 7

Fig. S6 The 13C NMR (100 MHz, DMSO-d6) spectrum of 7

Fig. S7 The 1H NMR (400 MHz, DMSO-d6) spectrum of 9

Fig. S8 The 13C NMR (100 MHz, DMSO-d6) spectrum of 9

Fig. S9 The 1H NMR (400 MHz, DMSO-d6) spectrum of 10

Fig. S10 The IR (ATR) spectrum of CPFPM1

Fig. S11 The IR (ATR) spectrum of CPFPM2

Fig. S12 The IR (ATR) spectrum of CPFPM3

Fig. S13 The IR (ATR) spectrum of CPFPM4

Fig. S14 The IR (ATR) spectrum of CPFPM5

Fig. S15 The UV-Vis spectra of CPFPM1 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S16 The UV-Vis spectra of CPFPM1 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S17 The fluorescence spectra of CPFPM1 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S18 The UV-Vis absorption and fluorescence spectra of CPFPM1 in film (blue and black lines, respectively)

Fig. S19 The UV-Vis spectra of CPFPM2 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S20 The fluorescence spectra of CPFPM2 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S21 The UV-Vis absorption and fluorescence spectra of CPFPM2 in film (blue and black lines, respectively)

Fig. S22 The UV-Vis spectra of CPFPM3 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S23 The UV-Vis spectra of CPFPM3 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S24 The fluorescence spectra of CPFPM3 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S25 The fluorescence spectra of CPFPM3 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S26 The UV-Vis absorption and fluorescence spectra of CPFPM3 in film (blue and black lines, respectively)

Fig. S27 The UV-Vis spectrum of CPFPM4 in chloroform

Fig. S28 The fluorescence spectrum of CPFPM4 in chloroform (black line), in chloroform with TFA (red line)

Fig. S29 The UV-Vis absorption and fluorescence spectra of CPFPM4 in film (blue and black lines, respectively)

Fig. S30 The UV-Vis spectra of CPFPM5 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S31 The fluorescence spectra of CPFPM5 in chloroform (black line), in chloroform with TFA (red line), in chloroform with TEA (blue line)

Fig. S32 The UV-Vis absorption and fluorescence spectra of CPFPM5 in film (blue and black lines, respectively)

Fig. S33 Plot of of the integral intensity of the luminescence of the long-wavelength band of CPFPM2 against varying logarithm of TFA concentrations

Fig. S34 Luminescence intensites of CPFPM5 in chloroform solution changed with different concentrations of TFA (CTFA = 0 – 1.7103 M)

Fig. S35 Plot of of the integral intensity of the luminescence of the long-wavelength band of CPFPM5 against varying logarithm of TFA concentrations

| a) | b) |
| --- | --- |
| c) | d) |

Fig. S36 The color of the CPFPM5 solution in chloroform (a), in chloroform with the addition of TFA (b) and luminescence of the CPFPM5 solution in chloroform (c), in chloroform with the addition of TFA (d)