Appendix A (Supplementary Materials)

Soil Responses to Nano-enhanced Bioremediation Techniques: Comparative Analysis of Bio-based Vermicompost, Fe3O4 Nanoparticles, and Their Novel Synergistic Effects against Phthalate Contamination

Laleh Ghafghazi 1. Lobat Taghavi 1. Behnam Rasekh 2. Hadi Farahani 2. Mahyar Safa 3

1 Department of Natural Resources and Environment, SR.C., Islamic Azad University, P. O. Box 14515-775, Tehran, Iran.

laleh.ghafghazi@gmail.com; laleh.ghafghazi@srbiau.ac.ir

taghavi_lobat@yahoo.com; l.taghavi@srbiau.ac.ir

2 Environment & Biotechnology Division, Research Institute of Petroleum Industry (RIPI), P.O. Box: 14665-137 Tehran, Iran.

b.rasekh@gmail.com

hadifarahani@gmail.com

3 Department of Environmental Engineering (Solid Waste), Faculty of Environment, University of Tehran, Iran.

mahyarsafa77@yahoo.com

Contents

| Supplementary Figures | Pages | Supplementary Tables | Pages |
| --- | --- | --- | --- |
| Fig. S1 Fig. S2 Fig. S3 Fig. S4 | 3 4 5 6 | Table S1 Table S2 Table S3 Table S4 Table S5 Table S6 Table S7 Table S8 Table S9 Table S10 | 7 8 8 9 10 11 12 13 14 15 |

| Eisenia Fetida in compost media |  |  |  |
| --- | --- | --- | --- |
| Final Vermicompost |  |  |  |

Fig. S1  Vermicompost preparation in a decay-resistant wooden reactor with Eisenia Fetida post-treatment.

Fig. S2   Prepared group's treatments in the incubation/exposure study.

| a FT-IR Peaks. Vibrations; ν (cm-1). Fe2O3, Fe3O4; 514, 518. C-H bending (Alkyne); 620 ,649. C-H bending (Aromatic); 781, 873. RCOOH (O-H) bending; 924. RCOOH (C-O) bending; 1015, 1044. Alcohol (C-O); 1101. CO32- or C-C Aromatic in ring; 1418. N=O (Nitroso); 1574. C=N, N-H; 1625. C-H stretching; 2935. O-H (with hydrogen bonding (; 3445. | b |
| --- | --- |

Fig. S3  a) Possible bonds in the structure of Vermicompost added by Fe3O4 NPs and b) FTIR infra-red spectrum after DEHP absorption.

| a | b | c |
| --- | --- | --- |

Fig. S4  a) Gel electrophoresis image of PCR product and gene fragment amplification, the DNA size marker on the left, and samples L1 to L5 on the right side; b) Gel electrophoresis image of PCR pure product of L1 to L5; c) Related microbial plate samples.

Table S1   Physicochemical and microbial characteristics of selected soil and vermicompost (Mean ± SD, n=3).

| Parameter/ Media | Density (Bulk) (Kg.m3) | pH | EC (mS/cm) | OM (%) | TC (%) dw | TN (%) dw | C:N | AP (%) dw | EK (%) dw | CEC (meq/100g) | DEHP Background dose(mg.kg-1) | Total Plate Count (CFU/ml) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Agricultural Soil (0-20 cm depth) Vermicompost (85 day process) | 950 ± 0.15 373 ± 0.18 | 6.12 ±0.07 (1:5/H2O) (24°C) 8.18 ± 0.01 (1:10/H2O) (25°C) | 1.28 ± 1.30 (1:5/H2O) (23°C) 4.08 ± 1.55 (1:10/H2O) | 4.35 ± 2.15 41.20 ± 0.65 (100g) | 7.14 ± 1.08 38.12 ± 1.06 | 0.94 ± 0.75 3.23 ± 0.07 | 7.59 11.8 | 0.38 ± 1.80 1.32 ± 2.06 | 8.0 ± 0.55 1.10 ± 0.02 | 31 74 | 1.49 ±1.45 0.57 ± 0.15 | 106 × 8.4 ± 7.17 108× 7.9 ± 11.53 |

Table S2  Numeric independent variables, actual factors and their coded levels (α =1.68).

| Factor | Name | Units | Type | Minimum | Maximum | Coded Low | Coded High | Mean | Std. Dev. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A (X1) | Time | days | Numeric | 4.45 | 51.55 | -1 ↔ 14.00 | +1 ↔ 42.00 | 28.00 | 11.87 |
| B (X2) | Fe3O4 NPs dose | g.kg-1 (media) | Numeric | 0.6636 | 1.34 | -1 ↔ 0.80 | +1 ↔ 1.20 | 1.0000 | 0.1696 |
| C (X3) | DEHP Concentration | mg.kg-1 (dw.soil) | Numeric | 3.18 | 36.82 | -1 ↔ 10.00 | +1 ↔ 30.00 | 20.00 | 8.48 |

Table S3   DEHP removal efficiency in treatments of nano and bioremediation comparative experiments (Mean ± SD).

| Subset/ DEHP Concentration | Groups | DEHP removal efficiency |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Time 1 (7 days, n=24) |  | Time 2 (21 days, n=24) |  | Time 3 (42 days, n=24) |  |
|  |  | Mean | STDEV | Mean | STDEV | Mean | STDEV |
| 10 mg/kg | S1 (control) | 12.43 | 0.58 | 12.70 | 0.91 | 14.45 | 0.5 |
|  | S1V (Soil+ Vermicompost) | 34.8 | 2.13 | 54.79 | 4.99 | 69.34 | 3.15 |
|  | S1VN (Soil+ Vermicompost+ Fe3O4NP) | 43.47 | 1.06 | 66.75 | 3.12 | 94.58 | 2.65 |
|  | S1N (Soil + Fe3O4NP) | 54.28 | 5.30 | 67.09 | 4.77 | 80.90 | 2.20 |
| 30 mg/kg | S2 (control) | 13.34 | 1.11 | 14.15 | 0.13 | 15.10 | 0.48 |
|  | S2V (Soil+ Vermicompost) | 40.87 | 2.42 | 48.99 | 2.03 | 65.25 | 2.45 |
|  | S2VN (Soil+ Vermicompost+ Fe3O4NP) | 48.22 | 1.80 | 61.50 | 1.41 | 91.16 | 2.60 |
|  | S2N (Soil+ Fe3O4NP) | 33.77 | 4.65 | 52.38 | 2.28 | 75.76 | 0.98 |

Table S4   Two-way ANOVA comparisons test for DEHP Removal Efficiency analogy.

| Table Analyzed | DEHP Removal Efficiency,% |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Two-way ANOVA | Ordinary |  |  |  |  |
| Alpha | 0.05 |  |  |  |  |
| Source of Variation | % of total variation | P value | P value summary | Significant? |  |
| Row Factor | 0.2583 | 0.0987 | ns | No |  |
| Column Factor | 99.60 | <0.0001 | **** | Yes |  |
| ANOVA table | SS | DF | MS | F (DFn, DFd) | P value |
| Row Factor | 18.00 | 1 | 18.00 | F (1, 3) = 5.606 | P=0.0987 |
| Column Factor | 6942 | 3 | 2314 | F (3, 3) = 720.6 | P<0.0001 |
| Residual | 9.633 | 3 | 3.211 |  |  |
| Difference between row means |  |  |  |  |  |
| Mean of Time 49 (10 mg/kg) | 64.82 |  |  |  |  |
| Mean of Time 49 (30 mg/kg) | 61.82 |  |  |  |  |
| Difference between means | 3.000 |  |  |  |  |
| SE of difference | 1.267 |  |  |  |  |
| 95% CI of difference | -1.032 to 7.032 |  |  |  |  |
| Data summary |  |  |  |  |  |
| Number of columns (Column Factor) | 4 |  |  |  |  |
| Number of rows (Row Factor) | 2 |  |  |  |  |
| Number of values | 8 |  |  |  |  |

Table S5   The results of two-way ANOVA for TN and AP changes (%) in all treatments.

| Two-way ANOVA, TN (%) |  | Ordinary |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Alpha |  | 0.05 |  |  |  |  |  |  |  |  |
| Source of Variation |  | % of total variation | P value |  | summary |  |  | Significant? |  |  |
| Row Factor (Different Times) |  | 13.12 | 0.0031 |  | ** |  |  | Yes |  |  |
| Column Factor (Different Treatment) |  | 76.69 | <0.0001 |  | **** |  |  | Yes |  |  |
| ANOVA table |  | SS | DF |  | MS |  |  | F (DFn, DFd) | P value |  |
| Row Factor |  | 24.16 | 2 |  | 12.08 |  |  | F (2, 14) = 9.011 | P=0.0031 |  |
| Column Factor |  | 141.3 | 7 |  | 20.18 |  |  | F (7, 14) = 15.05 | P<0.0001 |  |
| Residual |  | 18.77 | 14 |  | 1.341 |  |  |  |  |  |
| Number of columns |  | 8 |  |  |  |  |  |  |  |  |
| Number of rows (Row Factor) |  | 3 |  |  |  |  |  |  |  |  |
| Number of values |  | 24 |  |  |  |  |  |  |  |  |
| Two-way ANOVA, AP (%) | Ordinary |  |  |  |  |  |  |  |  |  |
| Source of Variation (Alpha=0.05) | % of total variation |  |  | P value |  | summary | Significant? |  |  |  |
| Row Factor | 45 |  |  | 0.0025 |  | ** | Yes |  |  |  |
| Column Factor | 22 |  |  | 0.3219 |  | ns | No |  |  |  |
| ANOVA table | SS |  |  | DF |  | MS | F (DFn, DFd) |  |  | P value |
| Row Factor | 11 |  |  | 2 |  | 5.6 | F (2, 14) = 9.5 |  |  | P=0.0025 |
| Column Factor | 5.3 |  |  | 7 |  | 0.76 | F (7, 14) = 1.3 |  |  | P=0.3219 |
| Residual | 8.3 |  |  | 14 |  | 0.59 |  |  |  |  |
| Number of columns (Column Factor) | 8 |  |  |  |  |  |  |  |  |  |
| Number of rows (Row Factor) | 3 |  |  |  |  |  |  |  |  |  |
| Number of values | 24 |  |  |  |  |  |  |  |  |  |

Table S6   The results of two-way ANOVA for EK and SOM changes in all treatments.

| Two-way ANOVA, EK (%) | Ordinary |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Source of Variation (Alpha=0.05) | % of total variation | P value | summary | Significant? |  |
| Row Factor | 15 | 0.0018 | ** | Yes |  |
| Column Factor | 74 | <0.0001 | **** | Yes |  |
| ANOVA table | SS | DF | MS | F (DFn, DFd) | P value |
| Row Factor | 12 | 2 | 6.2 | F (2, 14) = 10 | P=0.0018 |
| Column Factor | 59 | 7 | 8.5 | F (7, 14) = 14 | P<0.0001 |
| Residual | 8.5 | 14 | 0.61 |  |  |
| Number of columns (Column Factor) | 8 |  |  |  |  |
| Number of rows (Row Factor) | 3 |  |  |  |  |
| Number of values | 24 |  |  |  |  |
| Two-way ANOVA, SOM(%); Ordinary. Alpha; 0.05. Source of Variation; % of total variation; P value; P value summary; Significant?. Row Factor; 4.847; 0.0033; **; Yes. Column Factor; 91.30; <0.0001; ****; Yes. ANOVA table; SS; DF; MS; F (DFn, DFd); P value. Row Factor; 253.7; 2; 126.9; F (2, 14) = 8.815; P=0.0033. Column Factor; 4779; 7; 682.8; F (7, 14) = 47.44; P<0.0001. Residual; 201.5; 14; 14.39. Data summary. Number of columns (Column Factor); 8. Number of rows (Row Factor); 3. Number of values; 24. |

Table S7  The results of two-way ANOVA for pH, CEC and EC changes in all treatments.

| Two-way ANOVA (pH) (Alpha=0.05) | % of total variation | P value | P value summary | Significant? |  |
| --- | --- | --- | --- | --- | --- |
| Interaction | 1.8 | <0.0001 | **** | Yes |  |
| Row Factor | 0.41 | <0.0001 | **** | Yes |  |
| Column Factor | 97 | <0.0001 | **** | Yes |  |
| ANOVA table | SS | DF | MS | F (DFn, DFd) | P value |
| Interaction | 1.7 | 21 | 0.081 | F (21, 64) = 7.2 | P<0.0001 |
| Row Factor | 0.38 | 3 | 0.13 | F (3, 64) = 11 | P<0.0001 |
| Column Factor | 90 | 7 | 13 | F (7, 64) = 1139 | P<0.0001 |
| Residual | 0.72 | 64 | 0.011 |  |  |
| Number of values | 96 |  |  |  |  |
| Two-way ANOVA (CEC) (Alpha=0.05); % of total variation; P value; P value summary; Significant?. Interaction; 6.3; <0.0001; ****; Yes. Row Factor; 4.6; <0.0001; ****; Yes. Column Factor; 88; <0.0001; ****; Yes. ANOVA table; SS; DF; MS; F (DFn, DFd); P value. Interaction; 908; 21; 43; F (21, 64) = 25; P<0.0001. Row Factor; 674; 3; 225; F (3, 64) = 129; P<0.0001. Column Factor; 12824; 7; 1832; F (7, 64) = 1050; P<0.0001. Residual; 112; 64; 1.7. Two-way ANOVA (EC) (Alpha=0.05); % of total variation; P value; P value summary; Significant?. Interaction; 7.0; <0.0001; ****; Yes. Row Factor; 5.0; <0.0001; ****; Yes. Column Factor; 88; <0.0001; ****; Yes. ANOVA table; SS; DF; MS; F (DFn, DFd); P value. Interaction; 6804354; 21; 324017; F (21, 64) = 5032; P<0.0001. Row Factor; 4845108; 3; 1615036; F (3, 64) = 25080; P<0.0001. Column Factor; 84900247; 7; 12128607; F (7, 64) = 188345; P<0.0001. Residual; 4121; 64; 64.. |

Table S8  The results of Tukey's multiple comparisons test based on the ordinary one-way ANOVA for microbial colony count assay.

| Ordinary one-way ANOVA (In groups with spiked soil treatment at 10 mg.kg-1) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Number of comparisons per 1 family | 6 | Alpha |  |  | 0.05 |  |  |  |  |  |  |  |  |  |
| Tukey's multiple comparisons test | Mean Diff. | 95.00% CI of diff. |  |  | Significant? |  | Summary |  | Adjusted P Value |  |  |  |  |  |
| Control (S1) vs. S1V | -5.040 | -7.065 to -3.015 |  |  | Yes |  | **** |  | <0.0001 |  | A-B |  |  |  |
| Control (S1) vs. S1VN | -5.108 | -7.133 to -3.082 |  |  | Yes |  | **** |  | <0.0001 |  | A-C |  |  |  |
| Control (S1) vs. S1N | -1.785 | -3.810 to 0.2402 |  |  | No |  | ns |  | 0.0910 |  | A-D |  |  |  |
| S1V vs. S1VN | -0.06750 | -2.093 to 1.958 |  |  | No |  | ns |  | 0.9996 |  | B-C |  |  |  |
| S1V vs. S1N | 3.255 | 1.230 to 5.280 |  |  | Yes |  | ** |  | 0.0022 |  | B-D |  |  |  |
| S1VN vs. S1N | 3.323 | 1.297 to 5.348 |  |  | Yes |  | ** |  | 0.0019 |  | C-D |  |  |  |
| Ordinary one-way ANOVA (In groups with spiked soil at 100 mg.kg-1) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Number of comparisons per 1 family | 6 |  | Alpha | 0.05 |  |  |  |  |  |  |  |  |  |  |
| Tukey's multiple comparisons test | Mean Diff. |  | 95.00% CI of diff. | Significant? |  | Summary |  | Adjusted P Value |  |  |  |  |  |  |
| Control (S2) vs. S2V | -4.978 |  | -6.673 to -3.282 | Yes |  | **** |  | <0.0001 |  | A-B |  |  |  |  |
| Control (S2) vs. S2VN | -4.190 |  | -5.886 to -2.494 | Yes |  | **** |  | <0.0001 |  | A-C |  |  |  |  |
| Control (S2) vs. S2N | 0.2500 |  | -1.446 to 1.946 | No |  | ns |  | 0.9866 |  | A-D |  |  |  |  |
| S2V vs. S2VN | 0.7875 |  | -0.9081 to 2.483 | No |  | ns |  | 0.5251 |  | B-C |  |  |  |  |
| S2V vs. S2N | 5.228 |  | 3.532 to 6.923 | Yes |  | **** |  | <0.0001 |  | B-D |  |  |  |  |
| S2VN vs. S2N | 4.440 |  | 2.744 to 6.136 | Yes |  | **** |  | <0.0001 |  | C-D |  |  |  |  |

Table S9  RSM model summary statistics and ANOVA/ Fit statistics parameters

### Model Summary Statistics. Source; Std. Dev.; Sequential p-value; R²; Adjusted R²; Predicted R²; PRESS. Linear; 0.9914; 0.2444; 0.2233; 0.0776; -0.2021; 24.34. 2FI; 1.06; 0.7857; 0.2822; -0.0491; -0.8815; 38.09. Quadratic; 0.3048; < 0.0001; 0.9541; 0.9128; 0.7006; 6.06; Suggested. Cubic; 0.2143; 0.0811; 0.9864; 0.9569; -0.1400; 23.08; Aliased.

ANOVA/Fit Statistics. Std. Dev.; 0.2883; R²; 0.9507. Mean; 11.09; Adjusted R²; 0.9220. C.V. %; 2.60; Predicted R²; 0.7937. Adeq Precision; 19.4572.

Table S10   ANOVA for Reduced Quadratic model (Response: log10 Total Colony Count)

| ANOVA for Reduced Quadratic model |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| Model | 19.25 | 7 | 2.75 | 33.07 | < 0.0001 | significant |
| A-Time (X1) | 3.84 | 1 | 3.84 | 46.25 | < 0.0001 |  |
| B-Fe3O4 NPs dose (X2) | 0.3601 | 1 | 0.3601 | 4.33 | 0.0595 |  |
| C-DEHP Concentration (X3) | 0.3149 | 1 | 0.3149 | 3.79 | 0.0754 |  |
| AB | 1.12 | 1 | 1.12 | 13.53 | 0.0032 |  |
| A² | 12.71 | 1 | 12.71 | 152.83 | < 0.0001 |  |
| B² | 0.7866 | 1 | 0.7866 | 9.46 | 0.0096 |  |
| C² | 1.38 | 1 | 1.38 | 16.62 | 0.0015 |  |
| Residual | 0.9976 | 12 | 0.0831 |  |  |  |
| Lack of Fit | 0.8257 | 7 | 0.1180 | 3.43 | 0.0967 | not significant |
| Pure Error | 0.1719 | 5 | 0.0344 |  |  |  |
| Cor Total | 20.24 | 19 |  |  |  |  |

Corresponding Author

taghavi_lobat@yahoo.com; l.taghavi@srbiau.ac.ir (L. Taghavi)