Supplementary Information

Effect of geometric structures on initial filtration and dust loading performance of bimodal coarse fibrous filter media: a numerical study

Yu Song *, Min Du, Yuhai Yan, Jiawei Liu, and Rongwu Wang

Engineering Research Center of Technical Textiles, Ministry of Education, College of Textiles, Donghua University, Shanghai 201620, China

*Corresponding author.

E-mail address: songyu@dhu.edu.cn (Y. Song)

This supplementary information includes:

Fig. S1 to S9, and Table S1 to S5.

Table S1 Collision model parameters.

| Parameter | Values |
| --- | --- |
| Boltzmann constant, kB (J/K) | 1.38×10-23 |
| Temperature, T (K) | 300 |
| Relative permittivity, Ɛ | 3.8 (A2), 2.3 (PET), 3.8 (Nylon), 1.0 (Air) |
| Plank's constant, h (J*s) | 6.63×10-34 |
| Main electronic absorption frequency, ve (s-1) | 3.00×1015 |
| Refractive index, n | 1.45 (A2), 1.6 (PET), 1.54 (Nylon), 1.0 (Air) |
| Hamaker constant, H (×10-20) | 7.55 (PET-A2), 6.96 (Nylon-A2), 7.26 (Fiber-A2), 5.97 (A2-A2) |

Table S2 Simulation parameters.

| Parameter | Values |
| --- | --- |
| Face velocity, u (cm/s) | 20 |
| Particle concentration, c (mg/m3) | 150 |
| Particle density, ρ (kg/m3) | 1808 |
| Air density, ρair (kg/m3) | 1.204 |
| Air dynamic viscosity, μ (kg/ms) | 1.834×10-5 |
| Simulation time per batch, t (s) | 45 |
| Number of particles per batch | 108970 |

Fig. S1. Particle size distribution [1].

Fig. S2. Simulated fractional efficiency using the restitution coefficient from our previous work [1] based on the generated 3D structure in (a) Fig. S5a-8.5μm and (b) Fig. S5a-6μm.

Fig. S3. Virtual 3D structures of filter media with various geometric parameters. (a) Fine fiber diameter, (b) mass blend ratio, (c) filter basis weight, (d) filter solidity, and (e) filter bulkiness. (* Indicates the same filter structure in Fig. 1a without inflow/outflow region.)

Fig. S4. Virtual 3D filter media structures with various geometric parameters (continued). (a) Fine fiber diameter distribution, (b) fine fiber cross-section shape, (c) in-plane fiber orientation. (* Indicates the same filter structure in Fig. 1a without inflow/outflow region.)

Fig. S5. (a) Creating a statistical digital twin from a non-uniform 3D filter structure [2] assisted by deep learning. (b) Comparison of PF restitution coefficients in our previous work [1] and this work. Initial fractional efficiency based on (c) the statistical digital twin, (d) the generated 3D structure in Fig. S5a-8.5μm, and (e) Fig. S5a-6μm. (The involved experimental results in Fig. S3c were conducted and reported in the previous work [2]; dimensions, Fig. S5a-(i): 660*660*723 μm3, Fig. S5a-(ii): 600*600*619 μm3; slices with filter solidity <1% were ignored in digital twin generation, leaving a thickness of 619 μm)

Table S3 Key structural characteristics of virtual filters with various fiber diameter distributions of the fine fibers.

| Case | dfine, μm | dcoarse, μm | D50, μm | Specific surface area, m2/m3 |
| --- | --- | --- | --- | --- |
| S1-1* | 8.5 ± 0 | 20 | 68.61 | 8849 |
| S1-2 | 8.5 ± 1 | 20 | 67.94 | 8728 |
| S1-3 | 8.5 ± 2 | 20 | 70.53 | 8467 |
| S1-4 | 8.5 ± 3 | 20 | 72.14 | 8072 |
| S1-5 | 8.5 ± 4 | 20 | 72.73 | 7680 |
| S1-6 | 8.5 ± 5 | 20 | 72.86 | 7687 |

* Indicates the case of the filter structure in Fig. 1a/Fig. S3a-8.5μm.

Fig. S6. Effect of fine fiber diameter distribution. (a) Initial filtration efficiency and pressure drop, (b) initial fractional efficiency. (c) Dust holding capacity and gravimetric total efficiency at 120 Pa, (d) pressure drop evolution, and (e) filtration efficiency evolution during dust loading, and (f) particle deposition profile across filter depth.

Table S4 Key structural characteristics of virtual filters with various cross-section shapes of fine fibers.

| Case | Fine fiber cross-section shape | Coarse fiber cross-section shape | D50, μm | Specific surface area, m2/m3 |
| --- | --- | --- | --- | --- |
| S2-1* | Circular | Circular | 68.61 | 8849 |
| S2-2 | Elliptical | Circular | 67.94 | 9550 |
| S2-3 | Rectangular | Circular | 70.53 | 9959 |
| S2-4 | Angular | Circular | 72.14 | 10462 |
| S2-5 | Trilobal | Circular | 72.73 | 10810 |
| S2-6 | Quadrilobal | Circular | 72.86 | 12196 |

* Indicates the case of the filter structure in Fig. 1a/Fig. S3a-8.5μm.

Fig. S7. Effect of fine fiber cross-section shape. (a) Initial filtration efficiency and pressure drop, (b) initial fractional efficiency. (c) Dust holding capacity and gravimetric total efficiency at 120 Pa, (d) pressure drop evolution, and (e) filtration efficiency evolution during dust loading, and (f) particle deposition profile across filter depth.

Table S5 Key structural characteristics of virtual filters with various in-plane fiber orientations of the fine fibers.

| Case | Fiber Orientation | Fraction | D50, μm |
| --- | --- | --- | --- |
| S3-1* | Isotropic | 100% | 68.61 |
| S3-2 | 0°/90° | 50%/50% | 63.97 |
| S3-3 | 30°/90° | 50%/50% | 54.31 |
| S3-4 | 45°/90° | 50%/50% | 62.08 |
| S3-5 | 60°/90° | 50%/50% | 54.13 |
| S3-6 | 90° | 100% | 42.86 |

* Indicates the case of the filter structure in Fig. 1a/Fig. S3a-8.5μm.

Fig. S8. Effect of in-plane fiber orientation. (a) Initial filtration efficiency and pressure drop, (b) initial fractional efficiency. (c) Dust holding capacity and gravimetric total efficiency at 120 Pa, (d) pressure drop evolution, and (e) filtration efficiency evolution during dust loading, and (f) particle deposition profile across filter depth.

Fig. S9. D10, D50, and D90 of filter structures with various fiber orientations.

References

[1]	Y. Song, E. Shim, High-fidelity 3D simulation of dust-loading behavior and clogging process of coarse nonwoven filter media considering collision effect, Sep. Purif. Technol. 344 (2024) 127046. https://doi.org/10.1016/j.seppur.2024.127046.

[2]	Y. Song, E. Shim, 3D X-ray tomographic microstructure analysis of dust-clogging inside nonwoven fibrous filter media, J. Memb. Sci. 664 (2022) 121067. https://doi.org/10.1016/j.memsci.2022.121067.