
CuCrO2/Cr2O3 heterojunction gas sensor for low-temperature and high response H2S detection and applied for meat freshness evaluation
Baoyu Songa, *, 1, Jinghan Wangc, 1, Xiaona Zhangb, Kuo Linb, Wenxiao Lia, Fei Yea, Ying Fua,*, Yingming Xub
aDepartment of Chemistry, College of Arts and Sciences, Northeast Agricultural University, Harbin 150030, China.
bKey Laboratory of Functional Inorganic Material Chemistry, Ministry of Education, School of Chemistry and Materials Science, Heilongjiang University, Harbin 150080, People's Republic of China
cCollege of Horticulture and Landscaoe Architecture, Northeast Agricultural University, Harbin 150030, China.
________________

*Correspondence author E-mail: songbaoyu1026@163.com (B. Y. Song); fuying@neau.edu.cn (Y. Fu)
1 These authors contribute equally.
Table S1 Comparison for gas-sensing performance of Cr2O3-based sensors towards H2S gas.
	Sensing Materials
	T. (oC)
	Conc. (ppm)
	Response
	Refs.

	Cr2O3 nanocylinders/ellipsoids
	170
	100
	42.8
	1

	Cr2O3 monotubes
	133
	50
	24.4
	2

	Cr2O3 nanofilms
	100
	5
	~4.64
	3

	CuCrO2/Cr2O3 heterojunction
	92
	50
	200
	This work


Note: T: Working temperature; Conc.: Concentration; a: (Ra-Rg)/Ra × 100%.
[image: image1.png]



Fig. S1. SEM images of Cu-Cr2O3-1 (a), Cu-Cr2O3-2 (b), Cu-Cr2O3-3 (c), Cu-Cr2O3-4 (d) and Cu-Cr2O3-5 (e)
[image: image2.png]Intensity (a.u.)

Sat.

Cu-Cr,0.-1|

Cr 2py,

Cu-Cr,0,-1 I

Cu-Cr,0,-2 Cu-Cr,0,2|
3
C
2
0n

Cu-Cr,0,3| 5 Cu-Cr,0.3|
=

Cu-Cr,0,-4 Cu-Cr203-4I
Cu-Cr,0,-5 Cu-Cr,0,5|
T T T T T T T T T T T T T
960 955 950 945 940 935 930 595 590 585 580 575 570

Binding Energy (eV)

Binding Energy (eV)




Fig. S2. High-resolution XPS spectra of Cu-Cr2O3 samples: (a) Cu 2p, (b) Cr 2p.
[image: image3.png]00

6501 Cu-Cr,0,-1 ——100 ppm 550 CU-Cr,0;5-1 ——50 ppm Cu-Cr,0,-1 ——30 ppm
600 500 -
g ss0 c
=3 = 450 1
§ 500 - §
S 450 5400
Q 7]
[ 7]
@ 400 D350
g 8350
350 -
300 3001
300
0 500 1000 1500 2000 0 500 1000 1500 2000 2500 3000 -200 O 200 400 600 800 1000 1200 1400
Time (s) Time (s) Time (s)
550 Cu-Cr,0,-1 ——10 ppm 550] Cu-Cr,0,-1 ——5ppm Cu-Cr,0,-1 ——3 ppm
550
500 L
a G500 -
£ =
450
8 9450
[= c
3 1S
0 400+ 400 -
0 7]
& r
3501 350
300 3004 300
0 200 400 600 800 1000 1200 0 200 400 600 800 1000 0 200 400 600 800 1000 12
Time (s) Time (s) Time (s)
1
550, CU-Cr04-1 —— 1ppm 8001 cu-cr,0,-1 ——0.8 ppm Cu-Cr,0,-1
550 - 8
~ 5004 =
[e] [e]
s 2500- o
75450- jg 3 o
g §45°' g
£ 400+ 7 S 4
L == 400 - 12 £ £
X 350 - x 2 5 5§ & 2 & o @2
350 2o 2 & a S £ 5 8
o - ™ L - ™ L -
. r . r . . . . . . r 0
0 200 400 600 800 1000 1200 0 200 400 600 800 1 2 3 4 5 6 7 8
Time (s) Time (s)





Fig. S3. Dynamic resistance change curves of Cu-Cr2O3-1 sensor towards different H2S concentrations gas 92 °C, (c) Response histogram of towards different kinds of H2S at 92 °C.
[image: image4.png]Resistance (MQ) Resistance (MQ)

Resistance (MQ)

Cu-Cr,0,-2 ——100 ppm 1004 Cu-Cr,0;-2 ——50 ppm 100 Cu-Cr,0,-2 ——30 ppm
100 _ _
[] [e]
= 10 =105
10 3 g
3 c c
8 8
K] K
0w 1 n 14
1 [} [}
1 o 12
0.14 J 0.1 0.14
0 500 1000 1500 2000 0 500 1000 1500 2000 2500 3000 -200 O 200 400 600 800 1000 1200 1400
Time (s) Time (s) Time (s)
Cu-Cr,0,-2 ——10 ppm Cu-Cr,0,-2 ——5ppm Cu-Cr,0,-2 ——3 ppm
14
g g
£ £
14 ] ]
f= f=
3 3
0 0
0n 0n
Q Q
14 114
0.1
0.1 0.1
0 200 400 600 800 1000 1200 0 200 400 600 800 1000 0 200 400 600 800 1000 1200
Time (s) Time (s) Time (s)
03
Cu-Cr,0,-2 —— 1ppm Cu-Cr,0,-2 ——0.8 ppm Cu-Cr,0,-2
024 { .
[e]
= 0.2
[
[}
f=
8
2
n
[}
©
0 200 400 600 800 1000 1200 0 200 400 600 800
Time (s) Time (s)




Fig. S4. Dynamic resistance change curves of Cu-Cr2O3-2 sensor towards different H2S concentrations gas at 92 °C, (c) Response histogram of towards different kinds of H2S at 92 °C.
[image: image5.png]Resistance (MQ)

Resistance (MQ)

Resistance (MQ)

Cu-Cr,0,-4 ——100 ppm Cu-Cr,0,-4 ——50 ppm Cu-Cr,0,-4 ——30 ppm
1000 1 .
- 100+
[e] (]
= 100+ =
[ [
100 4 2 2
[1} [}
ol ol
0 |2
[7] [7]
& & 10
104 E
10
0 500 1000 1500 2000 0 500 1000 1500 2000 2500 3000 -200 O 200 400 600 800 1000 1200 1400
Time (s) Time (s) Time (s)
.
Cu-Cr,0,4 ——10 ppm Cu-Cr,0,-4 ——5ppm Cu-Cr,0,-4 ——3ppm
<) <)
= 2
[} [}
e e
@ @ 10
%107 o
104 i o
[] []
o 15
0 200 400 600 800 1000 1200 0 200 400 600 800 1000 0 200 400 600 800 1000 1200
Time (s) Time (s) Time (s)
p— —0. 3
Cu-Cr,0,-4 1ppm Cu-Cr,0,-4 0.8 ppm 1000 CU-Cr05-4 &
[=3
o
g 10- T
2
104 @
(%]
c
[
8
0
7]
(]
o
0 200 400 600 800 1000 1200 100 O 100 200 300 400 500 600 700 8

Time (s) Time (s)




Fig. S5. Dynamic resistance change curves of Cu-Cr2O3-4 sensor towards different H2S concentrations gas at 92 °C, (c) Response histogram of towards different kinds of H2S at 92 °C.
[image: image6.png]Resistance (MQ)

Resistance (MQ)

Resistance (MQ)

100 CU-Cr,05-5 100 ppm Cu-Cr,0,-5 ——50 ppm Cu-Cr,0,-5 —— 30 ppm
10 ]
— 10- —
o] o]
104 £ £
[ [
Q (%]
f = f =
© o 11
- 14 -
K2 0
1 n 7}
[} [}
4 4
0.1 - 0.1 0.1+
0 500 1000 1500 2000 0 500 1000 1500 2000 0 500 1000 1500 2000 2500 3000
Time (s) Time (s) Time (s)
.
Cu-Cr,0,5 ——10 ppm Cu-Cr,0,-5 ——5ppm 04 cu-cr,0,5 ——3ppm
a g
1 g g
] o 2021
Q (%]
f = c
[y} [}
Rl R
K2 0
] (7]
[} [}
¢ 14
014
0.14
200 0 200 400 600 800 1000 1200 1400 0 200 400 600 800 1000 1200 0 200 400 600 800 1000
Time (s) Time (s) Time (s)
0.15 10000 4
Cu-Cr,0,-5 —— 1ppm Cu-Cr,0,-5 —— 0.8 ppm Cu-Cr,0,-5
g
02 5 1000 - s
= E o
= o s ©
@ g o
g g1004 )
[y}
@ 3
@ 01 4
10
011 x
1
0 200 400 600 800 1000 1200  -100 O 100 200 300 400 500 600 700 800

Time (s) Time (s)




Fig. S6. Dynamic resistance change curves of Cu-Cr2O3-5 sensor towards different H2S concentrations gas at 92 °C, (c) Response histogram of towards different kinds of H2S at 92 °C.
[image: image7.png]SO,

80

70

50 60

Mass

40

H,S

(‘n-e) Ayisuajuy

20




Fig. S7. MS spectra of gaseous product after contacting with H2S at 92 °C.
Song BY, Zhang XF, Huang J, Cheng XL, Deng ZP, Xu YM, Huo LH, Gao S (2022) Porous Cr2O3 architecture assembled by nano-sized cylinders/ellipsoids for enhanced sensing to trace H2S gas, ACS Appl Mater Interfaces 14: 22302-22312. https://doi.org/10.1021/acsami.2c03154.
Song BY, Liu LH, Yang M, Zhang XF, Deng ZP, Xu YM, Huo LH, Gao S (2022) Biotemplate-directed synthesis of Cr2O3 mesoporous monotubes for enhanced sensing to trace H2S gas, Sens Actuat B Chem 369: 132294. https://doi.org/10.1016/j.snb.2022.132294.
Balouria V, Kumar A, Singh A, Samanta S, Debnath AK, Mahajan A, Bedi RK, Aswal DK, Gupta SK, Yakhmi JV ( 2011) Temperature dependent H2S and Cl2 sensing selectivity of Cr2O3 thin films, Sens Actuat B Chem 157: 466-472. https://doi.org/10.1016/j.snb.2011.05.002.

