Supplementary Materials

Table S1. Unit area content of bendiocarb in microencapsulated fabrics with different washing cycles

| Number of washes | Peak area of C2 | Content per unit area (mg/m2) |
| --- | --- | --- |
| 0 | 20319 | 127.64 |
| 5 | 10745 | 67.50 |
| 10 | 6136 | 38.55 |
| 15 | 5990 | 37.63 |
| 20 | 5485 | 34.46 |

Table S2. Content of glufosinate bendiocarb per unit area in microencapsulated fabrics with different slow-release cycles

| Number of washes | Peak area of C2 | Content per unit area (mg/m2) |
| --- | --- | --- |
| 0 | 20603 | 131.51 |
| 7 | 17854 | 113.96 |
| 14 | 12259 | 78.25 |
| 21 | 8037 | 51.30 |
| 28 | 6336 | 40.44 |

Figure S1. Plot of liquid phase test for bendiocarb content in microencapsulated fabrics with different washing cycles

Fig. S1. Liquid phase test of oxamethonium content in microencapsulated fabrics with different slow-release cycles