Table 1. Parameters of the kinetic models for the adsorption of Pb2+ andCu2+.

| Model | pH | Parameter | Pb2+ |  | Cu2+ |
| --- | --- | --- | --- | --- | --- |
| Pseudo-second order | 2.0 | qe, cal (mmol/g) | 0.0594 |  | 0.0530 |
|  |  | k2 (g/(mmol·h)) | 91.9243 |  | 128.2262 |
|  |  | k2q2e, cal (mmol/(g·h)) | 0.3249 |  | 0.3605 |
|  |  | R2 | 0.9897 |  | 0.9983 |
|  | 4.0 | qe, cal (mmol/g) | 0.0613 |  | 0.05934 |
|  |  | k2 (g/(mmol·h)) | 132.1275 |  | 111.1203 |
|  |  | k2q2e, cal (mmol/(g·h)) | 0.4950 |  | 0.3912 |
|  |  | R2 | 0.9991 |  | 0.9909 |
| Pseudo-first order | 2.0 | qe, cal (mmol/g) | 0.0266 |  | 0.03258 |
|  |  | K1 (g/(mmol·h)) | 0.0317 |  | 0.772 |
|  |  | R2 | 0.8128 |  | 0.977 |
|  | 4.0 | qe, cal (mmol/g) | 0.0220 |  | 0.0320 |
|  |  | k2 (g/(mmol·h)) | 0.296 |  | 0.517 |
|  |  | R2 | 0.6966 |  | 0.9034 |
| Weber-Morris intraparticle diffusion | 2.0 | Kid 1 (mmol/g·min1/2) | 0.00623 |  | 0.0034 |
|  |  | I1 (mmol/g) | 0.00121 |  | 0.01345 |
|  |  | R2 | 0.964 |  | 0.899 |
|  |  | Kid 2 (mol/g·min1/2) | 0.00015 |  | 0.00026 |
|  |  | I2 (mmol/g) | 0.0541 |  | 0.05351 |
|  |  | R2 | 0.57 |  | 0.693 |
|  | 4.0 | Kid 1 (mmol/g·min1/2) | 0.00625 |  | 0.0039 |
|  |  | I1 (mmol/g) | 0.00626 |  | 0.0141 |
|  |  | R2 | 0.979 |  | 0.881 |
|  |  | Kid 2 (mol/g·min1/2) | 0.0001 |  | 0.00007 |
|  |  | I2 (mmol/g) | 0.0575 | 0.0587 |  |
|  |  | R2 | 0.681 | 0.643 |  |

Table 2. Parameters of the Langmuir and Freundlich models.

| Model | Parameter | Cu2+ (pH=2) | Pb2+(pH=2) |  | Cu2+ (pH=4) | Pb2+(pH=4) |
| --- | --- | --- | --- | --- | --- | --- |
| Langmuir |  |  |  |  |  |  |
|  | kL(L/mg) | 28.62 | 4.17 |  | 15.28 | 2.213 |
|  | qm (mmol/g) | 0.035 | 0.127 |  | 0.051 | 0.168 |
|  | R2 | 0.968 | 0.995 |  | 0.978 | 0.994 |
| Freundlich |  |  |  |  |  |  |
|  | KF(mg/L(1-1/n)·g) | 0.053 | 0.216 |  | 0.083 | 0.212 |
|  | n | 2.905 | 1.167 |  | 2.160 | 1.307 |
|  | R2 | 0.989 | 0.989 |  | 0.083 | 0.984 |

Table 3.  2D-IR-COS results on the assignment and sign of each peak in synchronous (Φ) and asynchronous (Ψ, in parentheses) maps.

| System | Position (cm-1) | Assignment | Signa |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cu2+-2 |  |  | 1637 | 1104 | 1032/1008/914 | 778/795/694 | 536 |
|  | 1632 | N-H stretching vibration of amino acid[1] | + | + (+) | + (+) | + (+) | - (+) |
|  | 1104 | SO42-asymmetric stretching vibration[2] |  | + | + (+) | + (-) | + (+) |
|  | 1034/1008/914 | Si-O-Si (clay) stretching vibration[3] |  |  | + | - (-) /+ (+) | + (+) |
|  | 778/7950/692 | Si-O (kaolinite) symmetric stretching/bending [4] |  |  |  | + | + (-) |
|  | 537 | Fe-O stretching vibration of hematite[4] |  |  |  |  | + |
| Cu2+-4 |  |  | 1637 | 1104 | 1032/1008/914 | 778/795/694 | 536 |
|  | 1632 | N-H stretching vibration of amino acid | + | - (-) | - (-) | - (-) | - (-) |
|  | 1104 | SO42-asymmetric stretching vibration |  | + | + (-) | + (-) | + (-) |
|  | 1034/1008/914 | Si-O-Si (clay) stretching vibration |  |  | + | +(+) | + (-) |
|  | 778/7950/692 | Si-O (kaolinite) symmetric stretching/bending |  |  |  | + | + (-) |
|  | 537 | Fe-O stretching vibration of hematite |  |  |  |  | + |
| Pb2+-2 |  |  | 1637 | 1104 | 1032/1008/914 | 778/795/694 | 536 |
|  | 1632 | N-H stretching vibration of amino acid | + | - (+) | - (+) | + (-) | - (+) |
|  | 1104 | SO42-asymmetric stretching vibration |  | + | + (+) | - (-)/+ (+) | + (+) |
|  | 1034/1008/914 | Si-O-Si (clay) stretching vibration |  |  | + | - (-) /+ (+) | + (-) |
|  | 778/7950/692 | Si-O (kaolinite) symmetric stretching/bending |  |  |  | + | + (-) |
|  | 537 | Fe-O stretching vibration of hematite |  |  |  |  | + |
| Pb2+-4 |  |  | 1637 | 1104 | 1032/1008/914 | 778/795/694 | 536 |
|  | 1632 | N-H stretching vibration of amino acid | + | + (-) | + (-) | + (-) | + (-) |
|  | 1104 | SO42-asymmetric stretching vibration |  | + | + (-) | + (+) | + (-) |
|  | 1034/1008/914 | Si-O-Si (clay) stretching vibration |  |  | + | +(+) | + (-) |
|  | 778/7950/692 | Si-O (kaolinite) symmetric stretching/bending |  |  |  | + | + (-) |
|  | 537 | Fe-O stretching vibration of hematite |  |  |  |  | + |
| note | Signs were obtained in the synchronous (Ф) and asynchronous (Ψ) maps: +, positive; −, negative. |  |  |  |  |  |  |

Reference

- [1] Wang, Y.Q., Wei, R.Q., Liu. X.N., Liu, Y., 2007. Adsorption of polystyrene diethanolamine resin for cupric ion. The Chinese Journal of Process Engineering.7(1), 49-53. https://www.jproeng.com/EN/Y2007/V7/I1/49

- [2] Yin, Y., Yin, J., Zhang, W., Tian, H., Hu, Z., Ruan, M., 2017. FT-IR and micro-Raman spectroscopic characterization of minerals in high-calcium coal ashes. Journal of the Energy Institute. 91(3), 389-396.

- https://doi.org/10.1016/j.joei.2017.02.003

- [3] Jiang, G.Y., Zhang, Y.J., Wei, X., Zhang, D.X., Liu, S.L., Liu, K.L., 2018. The Soil Infrared Spectral Characteristics of Soil Organic Matter under Different Carbon Saturation Levels. Scientia Agricultura Sinica. 51(16), 13.  https://www.chinaagrisci.com/CN/Y2018/V51/I16/3117

- [4] Manoharan, C., Sutharsan, P., Dhanapandian, S., Venkatachalapathy, R., 2012. Spectroscopic and thermal analysis of red clay for industrial applications from tamilnadu, India. Journal of Molecular Structure. 1027, 99-103.

- https://doi.org/10.1016/j.molstruc.2012.05.079