Supplementary Materials

Tong Ye1, Hongzhi Shen1, Junwen Ren1, Dehui Li1,2*

1School of Optical and Electronic Information, Huazhong University of Science and Technology, Wuhan 430074, China.

2Wuhan National Laboratory for Optoelectronics, Huazhong University of Science and Technology, Wuhan 430074, China.

Fig. S1|Gate-dependent PL spectra for a stacking-order inversed HS (WSe2/WS2) on a hydrophilic substrate. The device shows contrary behaviors to that of WS2/WSe2 HS shown in Fig. 2a, thus proving the Stark effect. However, this device exhibits no excitonic hysteresis during the cyclic-Vg sweeping. This might be resulted from the Coulomb screening of electrons that are transferred from WSe2 due to the type-II band alignment.

Fig. S2|PL spectra of the WSe2 monolayer under gate voltages from 0 V to −60 V shown in Fig. 3a. The trion peak (X-/X+) and the neutral exciton (X0) evolve non-monotonously as Vg changes. The X- peak is gradually suppressed while the X+ peak is enhanced. Meanwhile, the X0 peak is abnormally strengthened at first and then weakened gradually. Such peculiar features strongly suggest that the WSe2 is preliminarily n-doped, and gradually become p-doped by the efficient gate control.

Fig. S3|Gate-dependent PL spectra for a WS2/WSe2 HS on a hydrophobic substrate. The device shows similar behaviors to that of WS2/WSe2 on hydrophilic substrate shown in Fig. 2a, but with no hysteresis, thus proving the importance role of O2/H2O molecules.

Fig. S4|Gate-dependent PL spectra of a WS2/WSe2/BN HS. The WS2/WSe2 HS was transferred on a hydrophilic SiO2/Si substrate with a region insulated by a thin layer BN as a and d shows. b-c, Gate-dependent PL spectra of the WS2/WSe2 HS region. e-f, Gate-dependent PL spectra of the WS2/WSe2/BN HS region.

The hysteresis was observed only in the region where WS2/WSe2 HS is directly contacted with the hydrophilic substrate, other than the region that is insulated by BN, thus proving the important role of O2/H2O molecules.

Fig. S5|Helicity–resolved PL spectra of the WS2/WSe2 HS. The valley-polarized degree can be efficiently modulated by Vg, and shows a strong hysteresis. a-d, The helicty-resolved PL spectra upon Vg sweeping from 0 V ~ −60 V, −60 V ~ 0 V, 0 V ~ 60 V, 60 V ~ 0 V, respectively.

Fig. S6|Electrically controlled memory operation in the HS. a, Fig. 5b that is replot in logarithmic timescale; b, Leakage current and PL intensity upon Vg varied with time. The retention time should be much longer than 60 minutes, because both the energy and intensity of IX emission gradually level off as time went by. The leakage current changes exponentially near the edges of writing and reading Vg, suggesting that the dynamic evolution of IX emission is resulted from charging and discharging processes.

Fig. S7|Memory performance of the WS2/WSe2 HS under different temperatures. a, Contour plot of the PL spectra under cyclic writing/reading/erasing operations at 150 K, 200 K, 250 K and 300 K, respectively. b, Circularly polarized PL spectra of IX under different temperatures. c, Absolute circular polarization degree of IX upon temperature.

The memory performance of IX degrades as the temperature increases. Intriguingly, the information encoding ability of the device can host up to 250 K with good energy difference of the 1 and 0 bits.