Supporting information

Table S1 The instruments used in the catalyst characteristic and performance evaluation

| Technology and method | Instrument | Information |
| --- | --- | --- |
| X-ray Diffraction (XRD) Raman spectrometer Scanning Electron Microscope (SEM) Energy Dispersive X-ray Spectroscopy (EDX) Field emission transmission electron microscope (FETEM) Brunauere-Emmette-Teller (BET) X-ray Photoelectron Spectroscopy (XPS) The UV-vis diffuse reflectance spectra (DRS) The photoluminescence spectra(PL) The CHI-660E electrochemical system Total Organic Carbon (TOC) Electronspin resonance spectra (ESR) | Bruker D8–Advance, Bruker VERTEX 70-RAM II type spectrometer Hitachi S-4800 microscope (acceleration voltage 20000 V) Hitachi H-7500, Japan Quantacrome Instruments Kubo X1000 PHI 5000 Versaprobe Instrument UV-550, JASCO, Japan Hitachi F-4600, Hitachi, Japan The CHI-660E lquiTOC II Elementar Analytik analyzer MS-5000 (Germany) spectrometer | Phase structure Surface functional groups Morphology, EDX spectrum, Elemental mapping Morphology Specific surface area Surface composition/chemical state Absorption of light Photoresponse properties Electrochemical property Mineralization efficiency Species of ROS |

Fig.S1 SEM morphologies of g-C3N4 (a) and g-C3N4NS (b)

Fig.S2 EDX spectra and the corresponding elemental mapping of CTC-4:1

Fig.S3 XPS survey spectrum of the CTN-4:1 composite

Fig.S4 Nitrogen adsorption–desorption isotherms of the samples (a: CdS, b: Ti3C2, c: g-C3N4, d: g-C3N4NS, e: Ti3C2/g-C3N4NS, f: CTC-2:1, g: CTC-3:1, h: CTC-4:1, and i: CTC-5:1)

Fig.S5 (A) Adsorptin, (B) degradation curves of orange II versus time in the g-C3N4 and g-C3N4NS systems (a: g-C3N4, b: g-C3N4NS)

Fig.S6 (A) TOC removal efficiency of orange II versus time in the CTN-4:1 system, (B) Cycle test for the CTN-4:1 catalyst, (C) XRD patterns of the CTN-4:1 catalyst before (a) and after (b) the photocatalytic reaction

Fig.S7 (A) UV–vis absorption spectra, (B) band-gap energy of g-C3N4 (a) and g-C3N4NS (b)

Fig.S8 (A) PL spectra, (B) transient photocurrent responses of the different composites

Fig.S9 ESR spectra of DMPO-•OH in the CTN-4:1 and CdS/g-C3N4NS degradation different systems

Fig. S10 (A) Degradation curves of orange II in the CTN-4:1 and CdS/g-C3N4NS. (B) Reactive species trapping experiments for the CdS/g-C3N4NS degradation system. (C) ESR spectra of DMPO-•O2− in the CTN-4:1 and CdS/g-C3N4NS systems

Fig.S11 Mott–Schottky plots of samples (A: g-C3N4NS, B: Ti3C2, and C: CdS)