Host–Guest Recognition in the Crystalline State: Selective Inclusion of 1,4-Dibromobutane by Bromoethoxy-Functionalized Pillar[5]arenes

Mickey Vinodh, Fatemeh H. Alipour and Talal F. Al-Azemi*

Chemistry Department, Kuwait University, P.O. Box 5969, Safat 13060, Kuwait

e-mail: t.alazemi@ku.edu.kw

Supporting information

Table of Contents                                                                                                              Page No

| Table S1. Summary on the nature and various crystallographic parameters of PBr1.ButBr2 and PBr2.ButBr2 | 2 |
| --- | --- |
| Table S2. Summary on the nature and various crystallographic parameters of PBr4.ButBr2 and PBr6.ButBr2 | 3 |
| Fig. S1. Crystal structure of PBr1.ButBr2 with displacement ellipsoids | 4 |
| Fig. S2. Symmetry expanded structure of PBr2.ButBr2 with displacement ellipsoids | 5 |
| Fig. S3. Crystal structure of PBr4.ButBr2 with displacement ellipsoids | 6 |
| Fig. S4. Crystal structure of PBr6.ButBr2 with displacement ellipsoids | 7 |
| Table S3: Non-bonding interactions between pillar[5]arene host and dibromobutane guest in the PBr1.ButBr2 crystals | 8 |
| Table S4: Non-bonding interactions between pillar[5]arene host and dibromobutane guest in the PBr2.ButBr2 crystals | 8 |
| Table S5: Non-bonding interactions between pillar[5]arene host and dibromobutane guest in the PBr4.ButBr2 crystals | 8 |
| Table S6: Non-bonding interactions between pillar[5]arene host and dibromobutane guest in the PBr6.ButBr2 crystals | 9 |
| Fig. S5. Packing pattern of PBr1.ButBr2 crystals | 10 |
| Fig. S6. Packing pattern of PBr2.ButBr2 crystals | 11 |
| Fig. S7. Packing pattern of PBr4.ButBr2 crystals | 12 |
| Fig. S8. Packing pattern of PBr6.ButBr2 crystals | 13 |
| CheckCIF_ PBr1.ButBr2 | 14 |
| CheckCIF_ PBr2.ButBr2 | 17 |
| CheckCIF_ PBr4.ButBr2 | 20 |
| CheckCIF_ PBr6.ButBr2 | 23 |

Table S1.  Summary on the nature and various crystallographic parameters of PBr1.ButBr2 and PBr2.ButBr2

| Crystal sample | PBr1.ButBr2 | PBr2.ButBr2 |
| --- | --- | --- |
| Chemical formula | C51H61Br4O10 | C51H60Br4O10 |
| Mr | 1153.63 | 1152.63 |
| Crystal system, space group | Triclinic, P-1 | Monoclinic, C2/c |
| Temperature (K) | 293 | 293 |
| a, b, c (Å) | 11.9504 (6), 12.3790 (5), 19.820 (1) | 11.147 (6), 21.854 (14), 21.609 (13) |
| α, β, γ (°) | 87.229 (6), 85.730 (6), 61.925 (4) | 104.819 (9) |
| V (Å3) | 2579.6 (2) | 5089 (5) |
| Z | 2 | 4 |
| Radiation type | Mo Kα | Mo Kα |
| µ (mm−1) | 3.18 | 3.22 |
| Crystal size (mm) | 0.15 × 0.12 × 0.08 | 0.20 × 0.20 × 0.11 |
| Diffractometer | Rigaku R-AXIS RAPID | Rigaku R-AXIS RAPID |
| Absorption correction | Multi-scan ABSCOR (Rigaku, 1995) | Multi-scan ABSCOR (Rigaku, 1995) |
| Tmin, Tmax | 0.464, 0.789 | 0.444, 0.749 |
| No. of measured, independent & observed [I > 2σ(I)] reflections | 30699, 9065, 4185 | 14748, 4465, 1888 |
| Rint | 0.068 | 0.096 |
| (sin θ/λ)max (Å−1) | 0.595 | 0.595 |
| R[F2 > 2σ(F2)], wR(F2), S | 0.096, 0.333, 1.02 | 0.077, 0.303, 0.93 |
| No. of reflections | 9065 | 4465 |
| No. of parameters | 649 | 372 |
| No. of restraints | 174 | 205 |
| H-atom treatment | Constrained | Constrained |
| Δρmax, Δρmin (e Å−3) | 1.15, −0.96 | 0.50, −0.63 |

Table S2.  Summary on the nature and various crystallographic parameters of PBr4.ButBr2 and PBr6.ButBr2

| Crystal sample | PBr4.ButBr2 | PBr6.ButBr2 |
| --- | --- | --- |
| Chemical formula | C56H68Br7O10 | C55H64Br8O10 |
| Mr | 1460.47 | 1524.34 |
| Crystal system, space group | Triclinic, P-1 | Orthorhombic, Aba2 |
| Temperature (K) | 296 | 296 |
| a, b, c (Å) | 12.491 (2), 12.859 (3), 19.944 (4) | 41.472 (5), 17.4570 (17), 16.6459 (17) |
| α, β, γ (°) | 94.148 (10), 93.140 (9), 111.521 (8) |  |
| V (Å3) | 2961.0 (10) | 12051 (2) |
| Z | 2 | 8 |
| Radiation type | Cu Kα | Cu Kα |
| µ (mm−1) | 6.13 | 6.80 |
| Crystal size (mm) | 0.21 × 0.19 × 0.17 | 0.21 × 0.17 × 0.11 |
| Diffractometer | Bruker APEX-II CCD | Bruker APEX-II CCD |
| Absorption correction | Multi-scan SADABS2016/2 - Bruker AXS area detector scaling and absorption correction | Multi-scan SADABS2016/2 - Bruker AXS area detector scaling and absorption correction |
| Tmin, Tmax | 0.31, 0.62 | 0.33, 0.64 |
| No. of measured, independent & observed [I > 2σ(I)] reflections | 43527, 10517, 7640 | 17083, 9315, 8406 |
| Rint | 0.054 | 0.041 |
| (sin θ/λ)max (Å−1) | 0.599 | 0.596 |
| R[F2 > 2σ(F2)], wR(F2), S | 0.091, 0.293, 1.04 | 0.075, 0.225, 1.04 |
| No. of reflections | 10517 | 9315 |
| No. of parameters | 706 | 659 |
| No. of restraints | 197 | 49 |
| H-atom treatment | Constrained | Constrained |
| Δρmax, Δρmin (e Å−3) | 1.46, −1.21 | 1.32, −0.64 |

Fig. S1. Crystal structure of PBr1.ButBr2 with displacement ellipsoids (30% probability). Hydrogen atoms are omitted for clarity.

Fig. S2. Symmetry expanded crystal structure of PBr2.ButBr2 with displacement ellipsoids (30% probability; labeled only the symmetry independent atoms). Hydrogen atoms are omitted for clarity.

Fig. S3. Crystal structure of PBr4.ButBr2 with displacement ellipsoids (30% probability). Hydrogen atoms are omitted for clarity.

Fig. S4. Crystal structure of PBr6.ButBr2 with displacement ellipsoids (30% probability). Hydrogen atoms are omitted for clarity.

Table 3: Non-bonding interactions between pillar[5]arene host and dibromobutane guest   in the PBr1_ButBr2 crystals ( Å, o).

| A-B...C |  | A-B |  | B...C |  | B....C |  | A-B...C |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C39-H39C…Br2A | 0.96 |  | 3.133 |  | 4.01(1) |  | 152.1 |  |
| C47A-H47A… O5 | 0.97 |  | 3.011 |  | 3.95(3) |  | 162 |  |
| C47A-H47B… O3 | 0.97 |  | 2.946 |  | 3.66(5) |  | 131 |  |
| C48A-H48A…O7 | 0.97 |  | 3.208 |  | 4.12(3) |  | 159 |  |
| C48A-H48B…O9 | 0.97 |  | 3.325 |  | 4.16(3) |  | 145 |  |
| C49A-H49A…3 | 0.97 |  | 2.879 |  | 3.840 |  | 170.09 |  |
| C49A-H49B…2 | 0.97 |  | 3.013 |  | 3.723 |  | 130.88 |  |
| C50A-H50A…4 | 0.97 |  | 2.890 |  | 3.840 |  | 167.03 |  |
| C50A-H50B…5 | 0.97 |  | 2.850 |  | 3.673 |  | 143.10 |  |
| C42-H42B…Br3A | 0.96 |  | 3.227 |  | 4.08(1) |  | 148.4 |  |

2 - 5 are the centroid of the pillar[5]arene phenyl rings constitute C8-13,C15-C20, C22-C27 & C29-C34 respectively.

Table 4: Non-bonding interactions between pillar[5]arene host and dibromobutane guest   in the PBr2_ButBr2 crystals ( Å, o).

| A-B...C |  | A-B |  | B...C |  | B....C |  | A-B...C |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C23-H23B…Br2A | 0.959 |  | 3.12 |  | 3.97(1) |  | 147.3 |  |
| C25A-H25A… O5 | 0.97 |  | 2.847 |  | 3.68(2) |  | 145 |  |
| C25A-H25B… O3 | 0.97 |  | 2.964 |  | 3.86(2) |  | 155 |  |
| C26A-H26A…2 | 0.97 |  | 3.152 |  | 3.841 |  | 129.44 |  |
| C26A-H26B…3 | 0.97 |  | 2.944 |  | 3.875 |  | 161.05 |  |

2 and 3 are the centroid of the pillar[5]arene phenyl rings constitute C5-10 & C12-C17 respectively.

Table 5: Non-bonding interactions between pillar[5]arene host and dibromobutane guest   in the PBr4_ButBr2 crystals ( Å, o).

| A-B...C |  | A-B |  | B...C |  | B....C |  | A-B...C |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C44-H44C…Br5 | 0.96 |  | 3.048 |  | 3.99(1) |  | 166.4 |  |
| C50-H50A … O9 | 0.97 |  | 3.159 |  | 4.00(2) |  | 146 |  |
| C50-H50B …2 | 0.97 |  | 3.313 |  | 4.026 |  | 148.84 |  |
| C51-H51A …4 | 0.97 |  | 3.125 |  | 3.826 |  | 130.46 |  |
| C51-H51B…3 | 0.97 |  | 3.009 |  | 3.942 |  | 161.89 |  |
| C52-H52A…5 | 0.97 |  | 3.209 |  | 3.954 |  | 134.92 |  |
| C52-H52B…2 | 0.97 |  | 3.098 |  | 4.000 |  | 155.47 |  |
| C53-H53A…4 | 0.97 |  | 2.927 |  | 3.633 |  | 130.66 |  |
| C53-H53B…3 | 0.97 |  | 3.101 |  | 4.040 |  | 162.26 |  |
| C42-H42A…Br6 | 0.97 |  | 3.218 |  | 4.138(8) |  | 158.9 |  |

2 - 5 are the centroid of the pillar[5]arene phenyl rings constitute C8-13,C15-C20, C22-C27 & C29-C34 respectively.

Table 6: Non-bonding interactions between pillar[5]arene host and dibromobutane guest   in the PBr6_ButBr2 crystals ( Å, o).

| A-B...C |  | A-B |  | B...C |  | B....C |  | A-B...C |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C36-H36A…Br7 | 0.97 |  | 3.285 |  | 3.98(1) |  | 129.9 |  |
| C52-H52A… O5 | 0.96 |  | 2.727 |  | 3.64(3) |  | 149 |  |
| C52-H52B …O3 | 0.97 |  | 3.225 |  | 4.03(3) |  | 141 |  |
| C53-H53A…4 | 0.97 |  | 3.265 |  | 3.924 |  | 126.94 |  |
| C53-H53B…5 | 0.97 |  | 3.072 |  | 3.796 |  | 132.40 |  |
| C54-H54A…4 | 0.97 |  | 2.854 |  | 3.714 |  | 148.19 |  |
| C54-H54B…3 | 0.97 |  | 2.772 |  | 3.503 |  | 132.77 |  |
| C55-H55A…O10 | 0.97 |  | 3.205 |  | 4.08(3) |  | 151 |  |
| C55-H55B…1 | 0.97 |  | 3.232 |  | 3.842 |  | 122.54 |  |
| C49-H49C…Br8 | 0.96 |  | 3.208 |  | 4.12(1) |  | 158.5 |  |

1 - 5 are the centroid of the pillar[5]arene phenyl rings constitute C1-6,C15-C20,C22-C27 & C29-C34 respectively.

Fig. S5. Packing pattern of PBr1.ButBr2 crystals viewed from two different orientations.

Fig. S6. Packing pattern of PBr2.ButBr2 crystals viewed from two different orientations.

Fig. S7. Packing pattern of PBr4.ButBr2 crystals viewed from two different orientations.

Fig. S8. Packing pattern of PBr6.ButBr2 crystals viewed from two different orientations.

CheckCIF_ PBr1.ButBr2

# checkCIF (basic structural check) running

Checking for embedded fcf data in CIF ...
Found embedded fcf data in CIF. Extracting fcf data from uploaded CIF, please wait . . . .

# checkCIF/PLATON (basic structural check)

Structure factors have been supplied for datablock(s) PBr1_ButBr2

THIS REPORT IS FOR GUIDANCE ONLY. IF USED AS PART OF A REVIEW PROCEDURE FOR PUBLICATION, IT SHOULD NOT REPLACE THE EXPERTISE OF AN EXPERIENCED CRYSTALLOGRAPHIC REFEREE.

No syntax errors found. CIF dictionary
Please wait while processing ....  Interpreting this report

Structure factor report

Datablock: PBr1_ButBr2

| Bond precision: | C-C = 0.0115 A | Wavelength=0.71075 |
| --- | --- | --- |

| Cell: | a=11.9504(6) | b=12.3790(5) | c=19.820(1) |
| --- | --- | --- | --- |
|  | alpha=87.229(6) | beta=85.730(6) | gamma=61.925(4) |
| Temperature: | 293 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 2579.6(2) | 2579.6(2) |
| Space group | P -1 | P -1 |
| Hall group | -P 1 | -P 1 |
| Moiety formula | C46 H51 Br O10, C4 H8 Br2, 0.5(C2 H4 Br2) | ? |
| Sum formula | C51 H61 Br4 O10 | C51 H61 Br4 O10 |
| Mr | 1153.60 | 1153.63 |
| Dx,g cm-3 | 1.485 | 1.485 |
| Z | 2 | 2 |
| Mu (mm-1) | 3.175 | 3.175 |
| F000 | 1174.0 | 1174.0 |
| F000' | 1172.24 |  |
| h,k,lmax | 14,14,23 | 14,14,23 |
| Nref | 9119 | 9065 |
| Tmin,Tmax | 0.639,0.776 | 0.464,0.789 |
| Tmin' | 0.615 |  |

| Correction method= # Reported T Limits: Tmin=0.464 Tmax=0.789 AbsCorr = MULTI-SCAN |  |
| --- | --- |

| Data completeness= 0.994 | Theta(max)= 25.026 |
| --- | --- |

| R(reflections)= 0.0961( 4185) | wR2(reflections)= 0.3330( 9065) |
| --- | --- |
| S = 1.016; Npar= 649. |  |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level B

PLAT910_ALERT_3_B Missing # of FCF Reflection(s) Below Theta(Min).         17 Note

1  0  0,   0  1  0,   1  1  0,  -1 -1  1,   0 -1  1,  -1  0  1,

0  0  1,   1  0  1,   0  1  1,   1  1  1,  -1 -1  2,   0 -1  2,

-1  0  2,   0  0  2,   1  0  2,   0  1  2,   1  1  2,

RESPONSE: The unit cell is reasonable large and these low angle reflections are probably missing due to the beamstop. This occurs rather frequently with our goniometer's geometry, especially for larger unit cells.

Alert level C

PLAT026_ALERT_3_C Ratio Observed / Unique Reflections (too) Low ..        46% Check

PLAT084_ALERT_3_C High wR2 Value (i.e. > 0.25) ...................       0.33 Report

PLAT234_ALERT_4_C Large Hirshfeld Difference O5       --C41      .       0.19 Ang.

And 4 other PLAT234 Alerts

More ...

PLAT260_ALERT_2_C Large Average Ueq of Residue Including      Br2A      0.175 Check

And 2 other PLAT260 Alerts

More ...

PLAT341_ALERT_3_C Low Bond Precision on  C-C Bonds ...............    0.01145 Ang.

PLAT906_ALERT_3_C Large K Value in the Analysis of Variance ......     17.262 Check

And 2 other PLAT906 Alerts

More ...

PLAT911_ALERT_3_C Missing FCF Refl Between Thmin & STh/L=    0.595         37 Report

-1  3  0,   3  4  0,   4  5  0, -10-14  1,  -3 -2  2,  -4-14  3,

-2 -5  3,   6  5  3,  14  9  3,  -9-14  4,  -6-14  4,  -5-14  4,

-4-14  4, -11-13  4,   0  0  4,  10 14  4,  -7-14  5,  -6-14  5,

-5-14  5,  -4-14  5,  -7-14  6,  -6-14  6,  -7-13  7,  -8-13  8,

-7-13  8,  -1  0  8,  -8-13  9,  -7-13  9,  -6-13 10,  -5-13 10,

4 -9 11,   8 12 14,   9 -2 15,  -4 -7 20,   1 -4 22,  -2  0 23,

4  3 23,

Alert level G

PLAT002_ALERT_2_G Number of Distance or Angle Restraints on AtSite         12 Note

PLAT003_ALERT_2_G Number of Uiso or U(i,j)  Restrained non-H-Atoms         12 Report

PLAT172_ALERT_4_G The CIF-Embedded .res File Contains DFIX Records          3 Report

PLAT173_ALERT_4_G The CIF-Embedded .res File Contains DANG Records          2 Report

PLAT177_ALERT_4_G The CIF-Embedded .res File Contains DELU Records          1 Report

PLAT178_ALERT_4_G The CIF-Embedded .res File Contains SIMU Records          1 Report

PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K)        293 Check

PLAT200_ALERT_1_G Reported   _diffrn_ambient_temperature ..... (K)        293 Check

PLAT302_ALERT_4_G Anion/Solvent/Minor-Residue Disorder (Resd    2)       100% Note

PLAT302_ALERT_4_G Anion/Solvent/Minor-Residue Disorder (Resd    3)       100% Note

PLAT304_ALERT_4_G Non-Integer Number of Atoms in ..... (Resd    2)       7.50 Check

PLAT304_ALERT_4_G Non-Integer Number of Atoms in ..... (Resd    3)       6.50 Check

PLAT434_ALERT_2_G Short Inter HL..HL Contact Br4      ..Br3B     .       3.40 Ang.

-1+x,y,z  =      1_455 Check

PLAT860_ALERT_3_G Number of Least-Squares Restraints .............        174 Note

PLAT883_ALERT_1_G Absent Datum for _atom_sites_solution_primary ..     Please Do !

PLAT933_ALERT_2_G Number of HKL-OMIT Records in Embedded .res File          6 Note

0  0  4,  -2 -5  3,  -1  3  0,  -3 -2  2,   6  5  3,  -1  0  8,

PLAT941_ALERT_3_G Average HKL Measurement Multiplicity ...........        3.4 Low

PLAT969_ALERT_5_G The 'Henn et al.' R-Factor-gap value ...........      7.475 Note

Predicted wR2: Based on SigI**2  4.46 or SHELX Weight 32.78

PLAT978_ALERT_2_G Number C-C Bonds with Positive Residual Density.          6 Info

0 ALERT level A = Most likely a serious problem - resolve or explain

1 ALERT level B = A potentially serious problem, consider carefully

15 ALERT level C = Check. Ensure it is not caused by an omission or oversight

19 ALERT level G = General information/check it is not something unexpected

3 ALERT type 1 CIF construction/syntax error, inconsistent or missing data

8 ALERT type 2 Indicator that the structure model may be wrong or deficient

10 ALERT type 3 Indicator that the structure quality may be low

13 ALERT type 4 Improvement, methodology, query or suggestion

1 ALERT type 5 Informative message, check

PLATON version of 02/02/2025; check.def file version of 02/02/2025

Datablock PBr1_ButBr2 - ellipsoid plot

CheckCIF_ PBr2.ButBr2

# checkCIF (basic structural check) running

Checking for embedded fcf data in CIF ...
Found embedded fcf data in CIF. Extracting fcf data from uploaded CIF, please wait . . .

# checkCIF/PLATON (basic structural check)

Structure factors have been supplied for datablock(s) PBr2_ButBr2

THIS REPORT IS FOR GUIDANCE ONLY. IF USED AS PART OF A REVIEW PROCEDURE FOR PUBLICATION, IT SHOULD NOT REPLACE THE EXPERTISE OF AN EXPERIENCED CRYSTALLOGRAPHIC REFEREE.

No syntax errors found. CIF dictionary
Please wait while processing ....  Interpreting this report

Structure factor report

Datablock: PBr2_ButBr2

| Bond precision: | C-C = 0.0091 A | Wavelength=0.71075 |
| --- | --- | --- |

| Cell: | a=11.147(6) | b=21.854(14) | c=21.609(13) |
| --- | --- | --- | --- |
|  | alpha=90 | beta=104.819(9) | gamma=90 |
| Temperature: | 293 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 5089(5) | 5089(5) |
| Space group | C 2/c | C 2/c |
| Hall group | -C 2yc | -C 2yc |
| Moiety formula | C47 H52 Br2 O10, C4 H8 Br2 | ? |
| Sum formula | C51 H60 Br4 O10 | C51 H60 Br4 O10 |
| Mr | 1152.59 | 1152.63 |
| Dx,g cm-3 | 1.504 | 1.504 |
| Z | 4 | 4 |
| Mu (mm-1) | 3.219 | 3.219 |
| F000 | 2344.0 | 2344.0 |
| F000' | 2340.49 |  |
| h,k,lmax | 13,26,25 | 13,26,25 |
| Nref | 4500 | 4465 |
| Tmin,Tmax | 0.531,0.702 | 0.444,0.749 |
| Tmin' | 0.520 |  |

| Correction method= # Reported T Limits: Tmin=0.444 Tmax=0.749 AbsCorr = MULTI-SCAN |  |
| --- | --- |

| Data completeness= 0.992 | Theta(max)= 25.028 |
| --- | --- |

| R(reflections)= 0.0772( 1888) | wR2(reflections)= 0.3031( 4465) |
| --- | --- |
| S = 0.927; Npar= 372. |  |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level C

PLAT026_ALERT_3_C Ratio Observed / Unique Reflections (too) Low ..        42% Check

PLAT084_ALERT_3_C High wR2 Value (i.e. > 0.25) ...................       0.30 Report

PLAT242_ALERT_2_C Low    'MainMol' Ueq as Compared to Neighbors of         O5 Check

PLAT260_ALERT_2_C Large Average Ueq of Residue Including      Br2A      0.182 Check

PLAT260_ALERT_2_C Large Average Ueq of Residue Including      Br2B      0.181 Check

PLAT334_ALERT_2_C Small <C-C> Benzene Dist.   C1       -C3_a     .       1.37 Ang.

PLAT341_ALERT_3_C Low Bond Precision on  C-C Bonds ...............     0.0091 Ang.

PLAT906_ALERT_3_C Large K Value in the Analysis of Variance ......     10.974 Check

PLAT906_ALERT_3_C Large K Value in the Analysis of Variance ......      2.615 Check

PLAT910_ALERT_3_C Missing # of FCF Reflection(s) Below Theta(Min).          8 Note

1  1  0,   0  2  0,  -1  1  1,   1  1  1,   0  2  1,   0  0  2,

-1  1  2,   0  2  2,

PLAT911_ALERT_3_C Missing FCF Refl Between Thmin & STh/L=    0.595         27 Report

12  0  2,  12  2  3,  12  0  4,  12  2  4,  11  1  5, -12  0  6,

11  1  6,  11  3  6,  11  1  7,  11  3  7,   8  6  7,  10  0  8,

11  1  8,  11  3  8,  10  2  9,  10  0 10,  10  2 10,   7  3 10,

10  4 10,   9  1 11,  10  2 11,   9  5 11,   9  1 12,   9  1 13,

9  3 13,   8  0 14,   8  2 15,

PLAT918_ALERT_3_C Reflection(s) with I(obs) much Smaller I(calc) .          1 Check

Alert level G

PLAT002_ALERT_2_G Number of Distance or Angle Restraints on AtSite         17 Note

PLAT003_ALERT_2_G Number of Uiso or U(i,j)  Restrained non-H-Atoms         17 Report

PLAT172_ALERT_4_G The CIF-Embedded .res File Contains DFIX Records          2 Report

PLAT173_ALERT_4_G The CIF-Embedded .res File Contains DANG Records          1 Report

PLAT175_ALERT_4_G The CIF-Embedded .res File Contains SAME Records          2 Report

PLAT176_ALERT_4_G The CIF-Embedded .res File Contains SADI Records          6 Report

PLAT177_ALERT_4_G The CIF-Embedded .res File Contains DELU Records          3 Report

PLAT178_ALERT_4_G The CIF-Embedded .res File Contains SIMU Records          3 Report

PLAT188_ALERT_3_G A Non-default SIMU Restraint Value has been used     0.0200 Report

PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K)        293 Check

PLAT200_ALERT_1_G Reported   _diffrn_ambient_temperature ..... (K)        293 Check

PLAT299_ALERT_4_G Atom Site Occupancy Constrained at .............        0.5 Check

H18A    H18B

PLAT301_ALERT_3_G Main Residue  Disorder ..............(Resd    1)        17% Note

PLAT302_ALERT_4_G Anion/Solvent/Minor-Residue Disorder (Resd    2)       100% Note

PLAT302_ALERT_4_G Anion/Solvent/Minor-Residue Disorder (Resd    3)       100% Note

PLAT304_ALERT_4_G Non-Integer Number of Atoms in ..... (Resd    2)       7.56 Check

PLAT304_ALERT_4_G Non-Integer Number of Atoms in ..... (Resd    3)       6.44 Check

PLAT367_ALERT_2_G Long?  C(sp?)-C(sp?) Bond  C15      - C18      .       1.51 Ang.

PLAT410_ALERT_2_G Short Intra H...H Contact  H3       ..H19D     .       1.78 Ang.

1-x,y,3/2-z  =      2_656 Check

PLAT721_ALERT_1_G Bond    Calc     0.97000, Rep     0.96000 Dev...       0.01 Ang.

C24A     -H24C            1_555   1_555 ........     #   38 Check

PLAT860_ALERT_3_G Number of Least-Squares Restraints .............        205 Note

PLAT883_ALERT_1_G Absent Datum for _atom_sites_solution_primary ..     Please Do !

PLAT941_ALERT_3_G Average HKL Measurement Multiplicity ...........        3.3 Low

PLAT969_ALERT_5_G The 'Henn et al.' R-Factor-gap value ...........      3.188 Note

Predicted wR2: Based on SigI**2  9.51 or SHELX Weight 32.69

PLAT978_ALERT_2_G Number C-C Bonds with Positive Residual Density.          2 Info

0 ALERT level A = Most likely a serious problem - resolve or explain

0 ALERT level B = A potentially serious problem, consider carefully

12 ALERT level C = Check. Ensure it is not caused by an omission or oversight

25 ALERT level G = General information/check it is not something unexpected

4 ALERT type 1 CIF construction/syntax error, inconsistent or missing data

9 ALERT type 2 Indicator that the structure model may be wrong or deficient

12 ALERT type 3 Indicator that the structure quality may be low

11 ALERT type 4 Improvement, methodology, query or suggestion

1 ALERT type 5 Informative message, check

PLATON version of 02/02/2025; check.def file version of 02/02/2025

Datablock PBr2_ButBr2 - ellipsoid plot

CheckCIF_ PBr4.ButBr2

# checkCIF (basic structural check) running

Checking for embedded fcf data in CIF ...
Found embedded fcf data in CIF. Extracting fcf data from uploaded CIF, please wait . . . .checkCIF/PLATON (basic structural check)Structure factors have been supplied for datablock(s) PBr4_ButBr2

THIS REPORT IS FOR GUIDANCE ONLY. IF USED AS PART OF A REVIEW PROCEDURE FOR PUBLICATION, IT SHOULD NOT REPLACE THE EXPERTISE OF AN EXPERIENCED CRYSTALLOGRAPHIC REFEREE.

No syntax errors found. CIF dictionary
Please wait while processing ....  Interpreting this report

Structure factor report

Datablock: PBr4_ButBr2

| Bond precision: | C-C = 0.0101 A | Wavelength=1.54178 |
| --- | --- | --- |

| Cell: | a=12.491(2) | b=12.859(3) | c=19.944(4) |
| --- | --- | --- | --- |
|  | alpha=94.148(10) | beta=93.140(9) | gamma=111.521(8) |
| Temperature: | 296 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 2960.9(10) | 2961.0(10) |
| Space group | P -1 | P -1 |
| Hall group | -P 1 | -P 1 |
| Moiety formula | C49 H54 Br4 O10, 0.5(C6 H12 Br2), C4 H8 Br2 | ? |
| Sum formula | C56 H68 Br7 O10 | C56 H68 Br7 O10 |
| Mr | 1460.41 | 1460.47 |
| Dx,g cm-3 | 1.638 | 1.638 |
| Z | 2 | 2 |
| Mu (mm-1) | 6.128 | 6.128 |
| F000 | 1458.0 | 1458.0 |
| F000' | 1451.47 |  |
| h,k,lmax | 14,15,23 | 14,15,23 |
| Nref | 10645 | 10517 |
| Tmin,Tmax | 0.318,0.353 | 0.310,0.620 |
| Tmin' | 0.240 |  |

| Correction method= # Reported T Limits: Tmin=0.310 Tmax=0.620 AbsCorr = MULTI-SCAN |  |
| --- | --- |

| Data completeness= 0.988 | Theta(max)= 67.387 |
| --- | --- |

| R(reflections)= 0.0914( 7640) | wR2(reflections)= 0.2927( 10517) |
| --- | --- |
| S = 1.043; Npar= 706. |  |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level C

PLAT084_ALERT_3_C High wR2 Value (i.e. > 0.25) ...................       0.29 Report

PLAT220_ALERT_2_C NonSolvent   Resd 1  C   Ueq(max)/Ueq(min) Range        3.8 Ratio

PLAT222_ALERT_3_C NonSolvent Resd 1  H   Uiso(max)/Uiso(min) Range        4.6 Ratio

PLAT234_ALERT_4_C Large Hirshfeld Difference Br4B     --C43      .       0.20 Ang.

PLAT242_ALERT_2_C Low    'MainMol' Ueq as Compared to Neighbors of         O6 Check

And 2 other PLAT242 Alerts

More ...

PLAT243_ALERT_4_C High   'Solvent' Ueq as Compared to Neighbors of        C50 Check

PLAT243_ALERT_4_C High   'Solvent' Ueq as Compared to Neighbors of        C53 Check

PLAT244_ALERT_4_C Low    'Solvent' Ueq as Compared to Neighbors of        C51 Check

PLAT244_ALERT_4_C Low    'Solvent' Ueq as Compared to Neighbors of        C52 Check

PLAT260_ALERT_2_C Large Average Ueq of Residue Including      Br7A      0.233 Check

PLAT260_ALERT_2_C Large Average Ueq of Residue Including       Br5      0.207 Check

PLAT341_ALERT_3_C Low Bond Precision on  C-C Bonds ...............    0.01015 Ang.

PLAT906_ALERT_3_C Large K Value in the Analysis of Variance ......      2.909 Check

PLAT911_ALERT_3_C Missing FCF Refl Between Thmin & STh/L=    0.599        130 Report

13  2  0, -12 13  0,  12-13  1, -12 13  1,  -8 15  1,  12-13  2,

-7-10  2,  14-10  2, -12 -4  2,  14 -1  2,   4 12  2,  -7-10  3,

-12 -4  3,   4 -4  3, -14 10  3,  -7 15  3,   8-15  4,  -9 -8  4,

-13 -2  4,   7  0  4, -12 11  4, -10 14  4,  10-14  5,  -8 -9  5,

14 -9  5,   5 -4  5, -11 13  5,  14 -8  6, -14  1  6,   0  3  6,

-14  9  6, -13 11  6, -11 13  6,  -9 14  6,   5-15  7,   9-14  7,

11-13  7,  12-12  7,  14 -6  7,  14 -5  7,   4 -3  7,  12  2  7,

9-14  8,  13 -1  8, -14  2  8,  -4 14  8,  10-13  9,  11-12  9,

12-11  9,  13 -9  9, -12 -3  9,  13 -2  9, -14  3  9, -11 12  9,

13 -5 10,  13 -4 10,  12  0 10, -13  9 10,   3-14 11,   6-14 11,

9-13 11,  11-11 11, -11 -4 11, -12 -2 11, -13  8 11, -12 10 11,

-4 13 11,   0-13 12,  -4-11 12,  12 -2 12, -13  7 12,   3 10 12,

1-13 13,   7-13 13,   9-12 13,  10-11 13,  -5-10 13,  12 -6 13,

12 -5 13,  12 -4 13, -11 -3 13,   3-13 14,   5-13 14,   8-12 14,

10  1 14,   7-12 15,  11 -6 15,  -9 -5 15,  11 -5 15,  11 -4 15,

10  0 15, -12  2 15,   9  2 15,   2-12 16,   5-12 16,  10 -8 16,

PLAT975_ALERT_2_C Check Calcd Resid. Dens.  0.65Ang From C56     .       0.69 eA-3

PLAT977_ALERT_2_C Check Negative Difference Density on H50B      .      -0.34 eA-3

And 4 other PLAT977 Alerts

More ...

Alert level G

PLAT002_ALERT_2_G Number of Distance or Angle Restraints on AtSite         21 Note

PLAT003_ALERT_2_G Number of Uiso or U(i,j)  Restrained non-H-Atoms         21 Report

PLAT083_ALERT_2_G SHELXL Second Parameter in WGHT  Unusually Large       9.38 Why ?

PLAT172_ALERT_4_G The CIF-Embedded .res File Contains DFIX Records          6 Report

PLAT173_ALERT_4_G The CIF-Embedded .res File Contains DANG Records          4 Report

PLAT175_ALERT_4_G The CIF-Embedded .res File Contains SAME Records          2 Report

PLAT177_ALERT_4_G The CIF-Embedded .res File Contains DELU Records          4 Report

PLAT178_ALERT_4_G The CIF-Embedded .res File Contains SIMU Records          4 Report

PLAT301_ALERT_3_G Main Residue  Disorder ..............(Resd    1)         3% Note

PLAT302_ALERT_4_G Anion/Solvent/Minor-Residue Disorder (Resd    2)        75% Note

PLAT411_ALERT_2_G Short Inter H...H Contact  H28B     ..H54D     .       1.76 Ang.

-x,1-y,1-z  =      2_566 Check

PLAT413_ALERT_2_G Short Inter XH3 .. XHn     H49A     ..H54C     .       2.06 Ang.

-x,1-y,1-z  =      2_566 Check

PLAT432_ALERT_2_G Short Inter X...Y Contact  O10      ..C54B     .       2.58 Ang.

-x,1-y,1-z  =      2_566 Check

PLAT432_ALERT_2_G Short Inter X...Y Contact  C49      ..C54B     .       3.04 Ang.

-x,1-y,1-z  =      2_566 Check

PLAT434_ALERT_2_G Short Inter HL..HL Contact Br6      ..Br7B     .       3.41 Ang.

x,y,z  =      1_555 Check

PLAT860_ALERT_3_G Number of Least-Squares Restraints .............        197 Note

PLAT883_ALERT_1_G Absent Datum for _atom_sites_solution_primary ..     Please Do !

PLAT909_ALERT_3_G Percentage of I>2sig(I) Data at Theta(Max) Still        40% Note

PLAT941_ALERT_3_G Average HKL Measurement Multiplicity ...........        4.1 Low

PLAT965_ALERT_2_G The SHELXL WEIGHT Optimisation has not Converged     Please Check

PLAT969_ALERT_5_G The 'Henn et al.' R-Factor-gap value ...........      4.922 Note

Predicted wR2: Based on SigI**2  5.95 or SHELX Weight 28.05

PLAT978_ALERT_2_G Number C-C Bonds with Positive Residual Density.          2 Info

PLAT992_ALERT_5_G Repd & Actual _reflns_number_gt Values Differ by          2 Check

0 ALERT level A = Most likely a serious problem - resolve or explain

0 ALERT level B = A potentially serious problem, consider carefully

22 ALERT level C = Check. Ensure it is not caused by an omission or oversight

23 ALERT level G = General information/check it is not something unexpected

1 ALERT type 1 CIF construction/syntax error, inconsistent or missing data

22 ALERT type 2 Indicator that the structure model may be wrong or deficient

9 ALERT type 3 Indicator that the structure quality may be low

11 ALERT type 4 Improvement, methodology, query or suggestion

2 ALERT type 5 Informative message, check

PLATON version of 02/02/2025; check.def file version of 02/02/2025

Datablock PBr4_ButBr2 - ellipsoid plot

CheckCIF_ PBr6.ButBr2

# checkCIF (basic structural check) running

Checking for embedded fcf data in CIF ...
Found embedded fcf data in CIF. Extracting fcf data from uploaded CIF, please wait . . . . . .

# checkCIF/PLATON (basic structural check)

Structure factors have been supplied for datablock(s) PBr6_ButBr2

THIS REPORT IS FOR GUIDANCE ONLY. IF USED AS PART OF A REVIEW PROCEDURE FOR PUBLICATION, IT SHOULD NOT REPLACE THE EXPERTISE OF AN EXPERIENCED CRYSTALLOGRAPHIC REFEREE.

No syntax errors found. CIF dictionary
Please wait while processing ....  Interpreting this report

Structure factor report

Datablock: PBr6_ButBr2

| Bond precision: | C-C = 0.0148 A | Wavelength=1.54178 |
| --- | --- | --- |

| Cell: | a=41.472(5) | b=17.4570(17) | c=16.6459(17) |
| --- | --- | --- | --- |
|  | alpha=90 | beta=90 | gamma=90 |
| Temperature: | 296 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 12051(2) | 12051(2) |
| Space group | A b a 2 | A b a 2 |
| Hall group | A 2 -2ac | A 2 -2ac |
| Moiety formula | C51 H56 Br6 O10, C4 H8 Br2 | ? |
| Sum formula | C55 H64 Br8 O10 | C55 H64 Br8 O10 |
| Mr | 1524.27 | 1524.34 |
| Dx,g cm-3 | 1.680 | 1.680 |
| Z | 8 | 8 |
| Mu (mm-1) | 6.800 | 6.799 |
| F000 | 6032.0 | 6032.0 |
| F000' | 6000.41 |  |
| h,k,lmax | 49,20,19 | 49,20,19 |
| Nref | 10714[ 5562] | 9315 |
| Tmin,Tmax | 0.287,0.473 | 0.330,0.640 |
| Tmin' | 0.209 |  |

| Correction method= # Reported T Limits: Tmin=0.330 Tmax=0.640 AbsCorr = MULTI-SCAN |  |
| --- | --- |

| Data completeness= 1.67/0.87 | Theta(max)= 66.794 |
| --- | --- |

| R(reflections)= 0.0750( 8406) | wR2(reflections)= 0.2245( 9315) |
| --- | --- |
| S = 1.038; Npar= 659. |  |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level B

PLAT910_ALERT_3_B Missing # of FCF Reflection(s) Below Theta(Min).         45 Note

0  2  0,   0  4  0,   1  2  0,   1  4  0,   2  0  0,   2  2  0,

3  2  0,   4  0  0,   4  2  0,   5  2  0,   6  0  0,   6  2  0,

7  2  0,   8  0  0,   8  2  0,   1  1  1,   1  3  1,   2  1  1,

2  3  1,   3  1  1,   3  3  1,   4  1  1,   4  3  1,   5  1  1,

RESPONSE: The unit cell is reasonable large and these low angle reflections are probably missing due to the beamstop. This occurs rather frequently with our goniometer's geometry, especially for larger unit cells.

Alert level C

PLAT094_ALERT_2_C Ratio of Maximum / Minimum Residual Density ....       2.06 Report

PLAT234_ALERT_4_C Large Hirshfeld Difference C44      --C45      .       0.18 Ang.

PLAT242_ALERT_2_C Low    'MainMol' Ueq as Compared to Neighbors of        C37 Check

And 3 other PLAT242 Alerts

More ...

PLAT243_ALERT_4_C High   'Solvent' Ueq as Compared to Neighbors of        C55 Check

PLAT260_ALERT_2_C Large Average Ueq of Residue Including       Br7      0.186 Check

PLAT341_ALERT_3_C Low Bond Precision on  C-C Bonds ...............    0.01476 Ang.

PLAT601_ALERT_2_C Unit Cell Contains Solvent Accessible VOIDS   <=         54 Ang**3

PLAT911_ALERT_3_C Missing FCF Refl Between Thmin & STh/L=    0.596         63 Report

0  6  0,   0  8  0,   0 10  0,   1  6  0,   1  8  0,   2  4  0,

2  6  0,  17 12  0,  22 18  0,  23 18  0,  24 18  0,  25  8  0,

26  8  0,  27  8  0,  39 12  0,  40 10  0,  40 12  0,  41 10  0,

42 10  0,  43 10  0,   1  5  1,   1  7  1,   2  5  1,  20 19  1,

41 11  1,   0  4  2,   0  6  2,   0  8  2,   1  4  2,   1  6  2,

23 18  2,  24 18  2,   6  1  3,   0  0  4,   0  2  4,   1  2  4,

2  0  4,   2  2  4,   4  0  4,  30 16  4,   1  1  5,   2  1  5,

3  1  5,   0  0  6,   2  0  6,  10 19  7,  10 16 12,  21 14 12,

11 15 13,  21 13 13,  11 14 14,  22  0 14,  32  6 14,  19 11 15,

0  0 16,   6 12 16,  17 10 16,  22  8 16,   0  0 18,   8  8 18,

15  6 18,  12  3 19,  14  1 19,

Alert level G

PLAT002_ALERT_2_G Number of Distance or Angle Restraints on AtSite          6 Note

PLAT003_ALERT_2_G Number of Uiso or U(i,j)  Restrained non-H-Atoms          6 Report

PLAT083_ALERT_2_G SHELXL Second Parameter in WGHT  Unusually Large      13.76 Why ?

PLAT172_ALERT_4_G The CIF-Embedded .res File Contains DFIX Records          2 Report

PLAT173_ALERT_4_G The CIF-Embedded .res File Contains DANG Records          2 Report

PLAT177_ALERT_4_G The CIF-Embedded .res File Contains DELU Records          1 Report

PLAT178_ALERT_4_G The CIF-Embedded .res File Contains SIMU Records          1 Report

PLAT188_ALERT_3_G A Non-default SIMU Restraint Value has been used     0.0100 Report

PLAT434_ALERT_2_G Short Inter HL..HL Contact Br2      ..Br3      .       3.43 Ang.

x,-1/2+y,-1/2+z  =      5_544 Check

PLAT860_ALERT_3_G Number of Least-Squares Restraints .............         49 Note

PLAT883_ALERT_1_G Absent Datum for _atom_sites_solution_primary ..     Please Do !

PLAT909_ALERT_3_G Percentage of I>2sig(I) Data at Theta(Max) Still        73% Note

PLAT915_ALERT_3_G No Flack x Check Done: Low Friedel Pair Coverage         75 %

PLAT941_ALERT_3_G Average HKL Measurement Multiplicity ...........        3.1 Low

PLAT965_ALERT_2_G The SHELXL WEIGHT Optimisation has not Converged     Please Check

PLAT969_ALERT_5_G The 'Henn et al.' R-Factor-gap value ...........      2.716 Note

Predicted wR2: Based on SigI**2  8.27 or SHELX Weight 21.63

PLAT978_ALERT_2_G Number C-C Bonds with Positive Residual Density.          0 Info

PLAT992_ALERT_5_G Repd & Actual _reflns_number_gt Values Differ by          5 Check

0 ALERT level A = Most likely a serious problem - resolve or explain

1 ALERT level B = A potentially serious problem, consider carefully

11 ALERT level C = Check. Ensure it is not caused by an omission or oversight

18 ALERT level G = General information/check it is not something unexpected

1 ALERT type 1 CIF construction/syntax error, inconsistent or missing data

13 ALERT type 2 Indicator that the structure model may be wrong or deficient

8 ALERT type 3 Indicator that the structure quality may be low

6 ALERT type 4 Improvement, methodology, query or suggestion

2 ALERT type 5 Informative message, check

PLATON version of 02/02/2025; check.def file version of 02/02/2025

Datablock PBr6_ButBr2 - ellipsoid plot