Supporting Information

Redox-Responsive Polymeric Micelles with Aggregation-Induced Emission for Bioimaging and Delivery of Anticancer Drug

Changzhen Sun,†a,b Ji Lu,†a Jun Wang,a Ping Hao,c Chunhong Li,a Lu Qi,a Lin Yang,a Bin He,d Zhirong Zhong*a and Na Hao*a

aDepartment of Pharmaceutical Sciences, School of Pharmacy, Southwest Medical University, Luzhou 646000, China.

bAffiliated Traditional Chinese Medicine Hospital, Southwest Medical University, Luzhou 646000, China.

cBiological group, Beijing Huimin School, Beijing 100032, China.

dNational Engineering Research Center for Biomaterials, Sichuan University, Chengdu 610064, China.

Synthesis of mPEG-Tripp

The mPEG (0.2 g, 0.1 mmol), DMAP (0.01 g, 0.1 mmol) and Tripp-COOH (0.34 g, 1.0 mmol) were dissolved in 30 mL of anhydrous CH2Cl2 with vigorous stirring under nitrogen. A solution of DCC (0.412 g, 2.0 mmol) in CH2Cl2 (10 mL) was added dropwise to the mixture on an ice bath. The mixture was stirred at room temperature for 48 h. The white solid dicyclohexylurea (DCU) precipitate was removed by filtration, and the filtrate was concentrated and precipitated with a large volume of cold diethyl ether. This purification procedure was repeated several times, and the product was vacuum-dried at 40 °C.

Figure S1. 1H NMR spectra of mPEG-Tripp (DMSO-d6).

Figure S2. Fluorescence spectra of micelles in aqueous solution at 485 nm excitation wavelength.