Supplementary Materials for

Lattice oxygen oxidation in Oxygen Vacancy-rich Co3O4 for the Electrooxidation of 5-Hydroxymethyfurfural

Yuxuan Lu,[a],+ Tianyang Liu,[b],+ Chunming Yang,[a,c],+ Chung-Li Dong,[d],+ Yucheng Huang,[d],+ Yafei Li,[b],+ Bo Zhou,[a] Ling Zhou,[a] Yujie Wu,[a] Zhijie Kong,[a] Ming Yang,[a] Yandong Wu,[a] Weixing Zhao,[a] Yuqin Zou,*[a] Shuangyin Wang*[a]

+Y.H.L., T.Y.L, C.M.Y, C.L.D, Y.C.H and Y.F.L equally contributed to this work.

*Correspondence to: yuqin_zou@hnu.edu.cn

Supporting Figures

Supplementary Fig. 1 SEM images of (a-c) Co3O4; (d-f) Vo-Co3O4.

Supplementary Fig. 2 (a-b) TEM images of Co3O4.

Supplementary Fig. 3 (a-b) HR-TEM image of Co3O4 .

Supplementary Fig. 4 XANES spectra of Co3O4 and Vo-Co3O4;

Supplementary Fig. 5 (a) The Cdl of Vo-Co3O4 and Co3O4; (b) The LSV curves of the Vo-Co3O4 and Co3O4 after normalized by ECSA area; (c) N2 adsorption-desorption isotherms of Vo-Co3O4 and Co3O4. (d) The LSV curves of the Vo-Co3O4 and Co3O4 after normalized by BET area.

Supplementary Fig. 6 Tafel slope of Vo-Co3O4 and Co3O4.

Supplementary Fig. 7 The reaction intermediate state models for Co3O4 during HMFOR process.

Supplementary Fig. 8 The XRD pattern of (a) Co3O4 and (b) Vo-Co3O4. The peak which marked by orange is attributed to Ti mesh.

Supplementary Fig. 9 (a-b) The TEM images of Co3O4 after HMFOR; (c-d) The HRTEM images of Co3O4 after HMFOR; (e-f) The TEM images of Vo-Co3O4 after HMFOR; (g-h) The HRTEM images of Vo-Co3O4 after HMFOR;

Supplementary Fig. 10 The XPS spectra for (a) Co3O4 and (b) Vo-Co3O4 at various applied potentials.

Supplementary Fig. 11 XPS spectra of Co 2p for (a) Co3O4 and (b) Vo-Co3O4 at various applied potentials.

Supplementary Fig. 12 Operando EXAFS spectra and the corresponding fitting for Vo-Co3O4 and Co3O4 at critical potentials.

Supplementary Fig. 13 O 1s XPS spectra fitting for (a) Co3O4 and (b) Vo-Co3O4 at various applied potential.

Supplementary Fig. 14 Bode phase plots of the in-situ EIS on Co3O4 in 1 M KOH (a) with and without (b) 50 mM HMF.

Supplementary Fig. 15 The equivalent circuit used for modeling the measured electrochemical response. The equivalent circuit image. Rs stands for the solution resistance, CPE1 represents double layer capacitance, Rct has contact with the interfacial charge transfer reaction, CPE2 and Rp are related to the dielectric properties and the resistance of the electrode inner film.

Supplementary Fig. 16 (a-b) HPLC standard curve measurements of pure HMF, HMFCA, FFCA, DFF and FDCA.

Supplementary Fig. 17 The HPLC chromatogram traces of the various products for  (a) Vo-Co3O4 and (b) Co3O4 at different reaction times following an HMF electrochemical oxidation reaction in 1 M KOH; (c) The concentration of substrates, intermediates and products during the HMFOR for Co3O4.

Supplementary Fig. 18 The yield (%) of FDCA and faradaic efficiency on Vo-Co3O4 under six successive electrolysis cycles.

Supplementary Fig. 19 The HPLC chromatogram traces of the various products for (a) Co3O4 and (b) Vo-Co3O4 at different reaction times following an HMF electrochemical oxidation reaction in 1 M PBS.

Supporting Table.

Supplementary Table 1. Structural parameters of Vo-Co3O4 and Co3O4 extracted from the EXAFS fitting. (S02=0.738)

| Potential | Sample | Path | CN | R(Å) | σ2(×10-3Å2) | △E0 (eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- | --- |
| OCP | Co3O4 | Co-O | 4.32 | 1.92 | 0.00242 | -4.744 | 0.005 |
|  |  | Co-Co（Oh） | 4.06 | 2.85 | 0.00491 | -8.532 |  |
|  |  | Co-Co（Td） | 9.72 | 3.35 | 0.00948 | -9.201 |  |
| OCP | Vo-Co3O4 | Co-O | 4.08 | 1.91 | 0.00205 | -7.335 | 0.009 |
|  |  | Co-Co（Oh） | 3.83 | 2.84 | 0.00447 | -9.703 |  |
|  |  | Co-Co（Td） | 8.22 | 3.35 | 0.00822 | -9.509 |  |
| 1.3V | Vo-Co3O4 | Co-O | 4.43 | 1.91 | 0.00281 | -6.046 | 0.007 |
|  |  | Co-Co（Oh） | 4.47 | 2.86 | 0.00448 | -6.797 |  |
|  |  | Co-Co（Td） | 5.55 | 3.35 | 0.0044 | -8.727 |  |
| 1.4 V | Vo-Co3O4 | Co-O | 4.55 | 1.91 | 0.00265 | -6.386 | 0.007 |
|  |  | Co-Co（Oh） | 3.79 | 2.84 | 0.00365 | -9.037 |  |
|  |  | Co-Co（Td） | 8.56 | 3.34 | 0.00808 | -9.921 |  |
| 1.45 V | Vo-Co3O4 | Co-O | 4.82 | 1.91 | 0.00308 | -7.013 | 0.009 |
|  |  | Co-Co（Oh） | 3.64 | 2.83 | 0.00329 | -11.684 |  |
|  |  | Co-Co（Td） | 11.43 | 3.35 | 0.01119 | -8.936 |  |
| 1.6 V | Vo-Co3O4 | Co-O | 4.799 | 1.91 | 0.00261 | -8.065 | 0.011 |
|  |  | Co-Co（Oh） | 3.768 | 2.83 | 0.00336 | -12.435 |  |
|  |  | Co-Co（Td） | 12.92 | 3.36 | 0.01227 | -9.099 |  |

S02 is the amolitude reduction factor (obtained by the fitting of Co foil). CN is the coordination number; R is interatomic distance (the bond length between Co central atoms and surrounding coordination atoms); σ2 is Debye-Waller factor (a measure of thermal and static disorder in absorber-scatterer distances); ∆E0 is potential correction.

Supplementary Table 2. The comparison of adsorption energies between two adsorption model.

| Vo Adsorption site | HMF* | OH- |
| --- | --- | --- |
| -CHO | -3.00 eV | -0.24 eV |
| OH- | -3.21 eV | -1.33 eV |

Supplementary Table 3. The resistance of each component for Vo-Co3O4 in 1 M KOH.

| Potential | Rs | Rct | Y0 | N0 | Rp | Y1 | N1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 4.5531 |  |  |  | 4319.2 | 4.2541E-05 | 0.77029 |
| 1.05 | 4.8511 |  |  |  | 383.01 | 2.6153E-05 | 0.86639 |
| 1.1 | 4.5531 |  |  |  | 316.41 | 0.0001092 | 0.69822 |
| 1.15 | 4.5128 |  |  |  | 212.62 | 0.00024728 | 0.60872 |
| 1.2 | 4.7279 |  |  |  | 85.752 | 0.00040032 | 0.5733 |
| 1.25 | 4.4627 |  |  |  | 51.38 | 0.00104 | 0.4856 |
| 1.3 | 4.5531 |  |  |  | 19.045 | 0.00096195 | 0.51581 |
| 1.35 | 4.484 |  |  |  | 17.951 | 0.0043287 | 0.37496 |
| 1.4 | 3.4529 |  |  |  | 45.294 | 0.032046 | 0.18818 |
| 1.45 | 4.5531 |  |  |  | 20.67 | 0.06545 | 0.17678 |
| 1.5 | 4.5531 | 9462.8 | 0.036668 | 0.66331 | 1.6809 | 0.00058461 | 0.55235 |
| 1.55 | 4.5531 | 490.4 | 0.022644 | 0.79625 | 1.6582 | 0.011368 | 0.34548 |
| 1.6 | 5.6065 | 191.57 | 0.016195 | 0.83409 | 1.7944 | 0.011869 | 0.44616 |
| 1.65 | 6.1552 | 27.935 | 0.010071 | 0.92731 | 2.121 | 0.073323 | 0.38994 |

Supplementary Table 4. The resistance of each component for Vo-Co3O4 in 1 M KOH with 50 mM HMF.

| Potential | Rs | Rct | Y0 | N0 | Rp | Y1 | N1 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 6.3982 | 7866.9 | 0.000062961 | 0.79652 | 579.51 | 1.5377E-05 | 0.90874 |
| 1.05 | 6.1457 | 4643 | 0.00013259 | 0.72791 | 512.93 | 2.0343E-05 | 0.87291 |
| 1.1 | 5.6953 | 4564.2 | 0.00052393 | 0.65114 | 457.98 | 4.4222E-05 | 0.77114 |
| 1.15 | 5.5957 | 4590.3 | 0.001313 | 0.60068 | 211.53 | 0.00014403 | 0.66835 |
| 1.2 | 5.876 | 4542.44 | 0.0029965 | 0.59547 | 63.212 | 0.0003626 | 0.59624 |
| 1.25 | 6.0369 | 4564.9 | 0.0021135 | 0.59796 | 36.415 | 0.00062666 | 0.5528 |
| 1.3 | 5.496 | 2395.6 | 0.0027978 | 0.87155 | 28.928 | 0.0026245 | 0.41665 |
| 1.35 | 5.2759 | 323.49 | 0.0033116 | 0.90213 | 21.067 | 0.0067033 | 0.33806 |
| 1.4 | 6.3065 | 126.37 | 0.0062422 | 0.84321 | 9.6614 | 0.0063179 | 0.39173 |
| 1.45 | 6.7097 | 180.35 | 0.018319 | 0.72891 | 3.851 | 0.0072371 | 0.43217 |
| 1.5 | 6.4371 | 132.16 | 0.028949 | 0.70019 | 1.3361 | 0.02811 | 0.33507 |
| 1.55 | 6.5755 | 65.495 | 0.014339 | 0.86624 | 2.1294 | 0.085371 | 0.32432 |
| 1.6 | 6.6457 | 69.181 | 0.014408 | 0.853 | 1.5041 | 0.045657 | 0.40565 |
| 1.65 | 8.2706 | 21.213 | 0.010227 | 0.86726 | 2.0908 | 0.0091548 | 0.52672 |

Supplementary Table 5. The resistance of each component for Co3O4 in 1 M KOH.

| Potential | Rs | Rp | Y1 | N1 | Rct | Y0 | N0 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 5.3258 | 3845.5 | 0.000027345 | 0.83109 |  |  |  |
| 1.05 | 5.2351 | 2418.9 | 0.000032173 | 0.81692 |  |  |  |
| 1.1 | 5.2203 | 1285.3 | 0.00012932 | 0.70239 |  |  |  |
| 1.15 | 5.2805 | 532.26 | 0.00020556 | 0.67624 |  |  |  |
| 1.2 | 5.261 | 224.61 | 0.00023756 | 0.66254 |  |  |  |
| 1.25 | 5.2893 | 93.214 | 0.00020384 | 0.67299 |  |  |  |
| 1.3 | 5.2419 | 51.247 | 0.00027685 | 0.63857 |  |  |  |
| 1.35 | 5.5834 | 26.659 | 0.00022247 | 0.67436 |  |  |  |
| 1.4 | 5.5913 | 17 | 0.00037106 | 0.63367 |  |  |  |
| 1.45 | 4.7031 | 13.49 | 0.0033527 | 0.40421 |  |  |  |
| 1.5 | 4.75 | 4.5889 | 0.000044367 | 0.60023 | 11000 | 0.024836 | 0.59101 |
| 1.55 | 4.76 | 4.88 | 0.000077332 | 0.4798 | 934 | 0.017851 | 0.66484 |
| 1.6 | 4.93 | 3.83 | 0.00024286 | 0.44242 | 435 | 0.014252 | 0.75035 |
| 1.65 | 6.3009 | 5.7863 | 0.060348 | 0.43874 | 23.223 | 0.010851 | 0.94078 |

Supplementary Table 6. The resistance of each component for Co3O4 in 1 M KOH with 50 mM HMF.

| Potential | Rs | Rp | Y1 | N1 | Rct | Y0 | N0 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 5.5497 | 3872.7 | 0.000040807 | 0.76928 |  |  |  |
| 1.05 | 5.9134 | 1571.7 | 0.000035319 | 0.84144 |  |  |  |
| 1.1 | 5.7462 | 755.53 | 0.000098613 | 0.75438 | 22369 | 0.0001386 | 0.73558 |
| 1.15 | 5.7915 | 638.19 | 0.00016017 | 0.70528 | 28141 | 0.00024087 | 0.7125 |
| 1.2 | 5.7994 | 494.3 | 0.00017841 | 0.69803 | 35002 | 0.00033942 | 0.69 |
| 1.25 | 5.823 | 269.55 | 0.00016545 | 0.71008 | 119910 | 0.00044387 | 0.66603 |
| 1.3 | 5.8632 | 143.84 | 0.00017104 | 0.71011 | 118760 | 0.00054098 | 0.65965 |
| 1.35 | 5.8805 | 96.268 | 0.00023158 | 0.66647 | 4864.7 | 0.00059479 | 0.70039 |
| 1.4 | 5.8148 | 71.384 | 0.00034795 | 0.62204 | 1329.3 | 0.00072704 | 0.73765 |
| 1.45 | 5.7923 | 39.878 | 0.00051219 | 0.5955 | 1095.2 | 0.0014978 | 0.6496 |
| 1.5 | 6.0525 | 9.8872 | 0.00023711 | 0.67773 | 1471 | 0.0042636 | 0.56021 |
| 1.55 | 5.9461 | 7.6788 | 0.0004433 | 0.61212 | 1334 | 0.0041954 | 0.59762 |
| 1.6 | 5.9263 | 8.0541 | 0.0004349 | 0.61242 | 913.83 | 0.0034057 | 0.61593 |
| 1.65 | 5.9096 | 8.9649 | 0.00048884 | 0.60014 | 213.73 | 0.002574 | 0.66109 |

Supplementary Table 7. The comparison of activity for Vo-Co3O4 and Co3O4 and other reported catalysts.

| Electrode Materials | Potential and current | FDCA yield | Faradaic efficiency | Ref. |
| --- | --- | --- | --- | --- |
| Vo-Co3O4 | 1.37 V (10 mA cm-2) | 91.90% | 95% | This work |
| Co3O4 | 1.44 V (10 mA cm-2) | 86.7% | 94.8% | This work |
| NiCo2O4 | 1.43 V (14.83 mA cm-2) | 90.80% | 87.50% | (1) |
| NiB | 1.45 V (100 mA cm-2) | 98.50% | 100% | (2) |
| NiFe LDH | 1.43 V (100 mA cm-2) | 98% | 97% | (3) |
| Ni2P | 1.423 V (>200 mA cm-2) | 100% | ~100% | (4) |
| Ni2S3 | 1.423 V (>200 mA cm-2) | 100% | 98% | (5) |
| CoNiFe LDH | 1.55 V (30 mA cm-2) | 84.90% | ~90% | (6) |
| hp-Ni | 1.423 V (>200 mA cm-2) | ~100% | ~95% | (7) |
| Ni3N@C | 1.38 V (50 mA cm-2) | 98% | 99% | (8) |

Reference

(1) Appl. Catal. B- Environ. 2019, 242,85.

(2) Angew. Chem. Int. Ed. 2018, 57, 11460.

(3) ACS Catal. 2018, 8, 5533.

(4) Angew. Chem. Int. Ed. 2016, 55, 9913.

(5) J. Am. Chem. Soc. 2016, 138, 13639.

(6) ACS Catal. 2020, 10, 5179.

(7) ACS Catal. 2017, 7, 4564.

(8) Angew. Chem. Int. Ed. 2019, 58, 15895.