Appendix A.

The constitutive relationships of the UHPFRC from DBJ43T325-2017 are shown as followes.

σc=fc1-1-εcεc0n  0≤εc≤εc0  (A-1)

n=2-160(fcu,k-50) (A-2)

σc=fc=const    εc0≤εc≤εcu  (A-3)

σt=ftεtεt0  0≤εt≤εt0  (A-4)

σt=ft=const    εt0≤εt≤εtu  (A-5)

where σc is the compressive stress of concrete, fc is the compressive strength of concrete, fcu,k is the compressive strength of specimen with dimension of 150 × 150 × 150 mm3, σt the tensile stress of the concrete, ft is the tensile strength of the concrete, εc is the compressive strain of the concrete, εc0 is the compressive strain when compressive stress reaches up to fc, εt is the tensile strain of the concrete, εt0 is the tensile strain when tensile stress reaches up to ft εcu is the ultimate compressive strain of the concrete and εtu is the

Figure A-1 shows the stress-strain response of concrete with steel fibres according to equation A-1 to A-5.

Fig A-1. Stress-strain response of concrete with steel fibre.

Thus, from Fig 10 and Fig A-1, the equation set (9) can be rewritten as follow.

α1fc bβxc=0εc0εcuxcfc1-1-εcεc0nbdy+εc0εcuxcxcfcbdyα2ftbh-xc=0εt0εtu(h-xc)ftεtεt0bdy+εt0εtu(h-xc)h-xcftbdyα1fc bβxcxc-12βxc =0εc0εcuxcfc1-1-εcεc0nbydy+εc0εcuxcxcfcbydyfyAs+α2ftbh-xc-fy'As'+α1fc bβxc=0  (A-6)

According to Fig 10, the relationship of the compressive strain of concrete and the depth is as follows.

εc=εcuyxc  (A-7)

εt=εsyh-xc  (A-8)

Table A-1 gives the properties of the concrete beams which have been determined in the main body of this study. To solve the equation set (9), the value of εc0, εt0, εcu,  εtu and n are determined as follows.

The cube compressive strength obtained in this study is from specimens with dimension of 100 × 100 × 100 mm3 while the dimension for the value of fcu,k is 150 × 150 × 150 mm3. According to GB50081-2010, fcu,k can be 0.95 times of the cube compressive strength of specimens with dimension of 100 × 100 × 100 mm3.

Thus, the value of fcu,k can be obtained as follow.

fcu,k=0.95×102.90=97.96 MPa

n=2-160fcu,k-50=1.2

The value of εc0 and εcu can be obtained from the compression test of prismatic specimens. As shown in Fig A-2,  εc0=2600 με and εcu=6400 με in this study.

The value of εt0 and εtu can be obtained from tension tests of dog-bone shaped specimen. As shown in Fig A-3,  εt0=1923 με and εtu=3142 με in this study.

Table A-2 lists the value of εc0, εcu, εt0, εtu and n.

According to Table A-1 and A-2, the value of α1, α2, β and xc can be obtained by substituting the parameters in equation set (9). Table A-3 shows the value of α1, α2, β and xc for all the concrete beams.

Table A-1. Properties of the concrete beams.

| Beam no. |  | NR | R12-1 | R18-1 | R18-2 | R20-2 | R22-2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| fy (MPa) |  | 0 | 360 | 360 | 360 | 360 | 360 |
| fy' (MPa) |  | 0 | 300 | 300 | 300 | 300 | 300 |
| As (mm2) |  | 0 | 227 | 509 | 1018 | 1256 | 1520 |
| As' (mm2) |  | 0 | 101 | 101 | 101 | 101 | 101 |
| ft (MPa) |  | 8.38 | 8.38 | 8.38 | 8.38 | 8.38 | 8.38 |
| fc (MPa) | 100 × 100 × 100 (mm3) | 102.90 | 102.90 | 102.90 | 102.90 | 102.90 | 102.90 |
|  | 100 × 100 ×300 (mm3) | 79.08 | 79.08 | 79.08 | 79.08 | 79.08 | 79.08 |
| b (mm) |  | 100 | 100 | 100 | 100 | 100 | 100 |
| h (mm) |  | 200 | 200 | 200 | 200 | 200 | 200 |
| h0 (mm) |  | 185 | 184 | 181 | 172 | 170 | 168 |
| as' (mm) |  | 15 | 16 | 19 | 28 | 30 | 32 |

Table A-2. Value of UHPFRC parameters

| Parameters | εc0 | εt0 | εcu | εtu | n |
| --- | --- | --- | --- | --- | --- |
| Value | 2600με | 1923με | 6400με | 3142με | 1.2 |

Table A-3. The value of parameters for concrete beams

| α1 | α2 | β | xc (mm) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | NR | R12-1 | R18-1 | R18-2 | R20-2 | R22-2 |
| 0.98 | 0.78 | 0.83 | 23.7 | 30.9 | 45.2 | 71.1 | 83.2 | 96.6 |

Fig A-2. Compression test result of prismatic specimen

Fig A-3. Tension test results of dog-bone shaped specimen