Table 1. Screening of Hydrogenation Protocol in batch reactor a

| entry | Temp. (⁰C) | Pressure H2 (MPa) | Conversion b (%) | Yield (%)b |  | dr % c 3a':3a'' |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | THQ(2a) | DHQ(3a'+3a'') |  |
| 1 | 150 | 5 | ˃99 | 71 | 29 | 68:32 |
| 2 | 175 | 5 | ˃99 | 41 | 59 | 73:27 |
| 3 | 200 | 5 | ˃99 | 0 | ˃99 | 80:20 |
| 4 | 200 | 4 | ˃99 | 12 | 88 | 78:22 |
| 5 | 200 | 3 | 95.3 | 20.7 | 74.9 | 72:28 |

a unless to otherwise noted, a mixture of 1a (10 g, 77.3 mmol), 5 wt% Pd/C catalyst (20% w/w), under H2 gas pressure in 50 ml autoclave for 12 h.   b conversion and yield determined by GC using DMF as the internal standard. c product distribution determined by GC.

Table 2. Substrate scope for hydrogenation of N- aromatic heterocycles a

| Entry | Starting Material | Product | Yield b % | Product distribution % c | H2 Capacity d (wt %) |
| --- | --- | --- | --- | --- | --- |
| 1 |  |  | ˃99 | (80:20) | 7.1 |
| 2e |  |  | ˃99 | (100:0) | 6.4 |
| 3 |  |  | ˃99 | (24:48:28) | 6.4 |

a unless to otherwise noted, a mixture of 1 (77.3 mmol), 5 wt% Pd/C (20% w/w) with 5 MPa H2 gas stirred at 200⁰C in 50 ml autoclave for 12 hour time.  b yield determined by GC using DMF as the internal standard. c product distribution determined by GC. d Theoretical amount of gain H2 in grams divided by the weight of hydrogenated compound in grams. e    reaction time 14 hrs.

Table 3. Screening of dehydrogenation Protocol in batch a

| Sr. No. | Temp. (⁰C) | Time (Hrs.) | Conversionb 3a (%) | Selectivityb 1a (%) |
| --- | --- | --- | --- | --- |
| 1 | 200 | 12 | 84 | 73 |
| 2 | 225 | 12 | 88 | 81 |
| 3 | 250 | 12 | 92 | 96 |
| 4 | 250 | 14 | 96 | 99 |

a Unless to otherwise noted, a mixture of 3a (5 mmol), 5 wt% Pd/C Catalyst (20 % w/w). b Conversion and selectivity determined by GC using DMF as the internal standard.

Table 4. Substrate scope for dehydrogenation of N-heterocycles a

| Entry | Reagent | Product | Yield b | H2 Capacity c | H2 Recovery d |
| --- | --- | --- | --- | --- | --- |
| 1 |  |  | 94.6 | 6.7 wt. % | 94% |
| 2 |  |  | 92.6 | 5.8 wt. % | 91% |
| 3 |  |  | ˃99 | 6.4 wt. % | 100% |

a unless to otherwise noted, a mixture of 3 (5 mmol), 5 wt.% Pd/C (20% w/w) at 250⁰C for 14 h time. b yield determined by GC using DMF as the internal standard.  c Theoretical amount of release H2 in grams divided by the weight of hydrogenated compound in gram. d Amount of H2 released in the experiment