Table 1. Optimizing of the reaction conditions in the synthesis of 2-amino-4H-pyran derivatives.

| Entry |  | Catalyst | Catalyst amount (mg) | Solvent | Temp (°C) | Time (min) | Yield |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | - | - | - | 100 | 120 | <5 |
| 2 | ND | 10 | EtOH | Reflux | 20 | 45 |
| 3 | Pectin | 10 | EtOH | Reflux | 20 | 31 |
| 4 | Fe3O4 | 10 | EtOH | Reflux | 20 | 56 |
| 5 | Ag | 10 | EtOH | Reflux | 20 | 29 |
| 6 | ND/Fe3O4/Pectin-Ag | 10 | EtOH | r.t | 10 | 98 |
| 7 | ND/Fe3O4/Pectin-Ag | 10 | EtOH/ H2O | r.t | 70 | 72 |
| 8 | ND/Fe3O4/Pectin-Ag | 10 | H2O | r.t | 80 | 39 |
| 9 | ND/Fe3O4/Pectin-Ag | 10 | Toluene | Reflux | 30 | 42 |
| 10 | ND/Fe3O4/Pectin-Ag | 10 | CH3CN | Reflux | 30 | 47 |
| 11 | ND/Fe3O4/Pectin-Ag | 10 | - | rt | 10 | 98 |
| 12 | ND/Fe3O4/Pectin-Ag | 5 | - | rt | 10 | 74 |
| 13 | ND/Fe3O4/Pectin-Ag | 20 | - | rt | 10 | 98 |