Ultrasound-Assisted Green Synthesis of 1,4-Disubstituted 1,2,3-Triazoles Using Natural Polymer Supports

Khatereh Haseli1, Maryam Esmkhani1, Shahrzad Javanshir1*

1Pharmaceutical and Heterocyclic Compounds Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran, 16846-13114, Iran.

Figure S 1. FTIR spectrum of Shilajit, Cs-Sh, and Cs-Sh@Cu ..................................................................2

Figure S 2. XRD pattern of Cs-Sh@Cu and reused catalyst........................................................................3

Figure S 3. BET analysis of Cs-Sh@Cu......................................................................................................3

Table S 1. Investigation of the prepared CS-Sh@Cu catalyst in different conditions in model reaction…4

Table S 2. Optimization the type of the catalyst…………………………………………………………...4

Figure S 1. FTIR spectrum of Shilajit, Cs-Sh, Cs-Sh@Cu, and the reused catalyst.

Figure S  2. XRD pattern of a) Cs-Sh@Cu and b) reused Cs-Sh@Cu.

Figure S 3. BET analysis of Cs-Sh@Cu.

Table S 1. Investigation of the prepared CS-Sh@Cu catalyst in different conditions in model reaction.

| Time | Yield (%) | Condition | Catalyst (mg) | Solvent |
| --- | --- | --- | --- | --- |
| 90min | 19 | Reflux | 10 | (1:1)MeOH: H2O |
|  | 15 |  | 10 | Ethanol |
|  | 84 |  | 10 | Water |
|  | Trace |  | 10 | Toluene |
|  | 5 |  | 10 | Acetonitrile |
|  | 5 |  | 10 | Chloroform |
|  | 16 |  | 10 | (1:1) Ethanol: H2O |
| 25min | 59 | Sonication, r.t. | 10 | (1:1) Ethanol: H2O |
|  | 50 |  | 10 | Ethanol |
|  | 93 |  | 10 | H2O |
|  | 79 |  | 10 | (2:1) Ethanol: H2O |
|  | - |  | - | H2O |
|  | 34 |  | 5 | H2O |
|  | 93 |  | 10 | H2O |
|  | 74 |  | 15 | H2O |
|  | 51 |  | 20 | H2O |
|  | 29 |  | 30 | H2O |

Table S 2. Optimization the type of the catalyst.

| Yield | Time (min) | Dosage (mg) | Catalyst |
| --- | --- | --- | --- |
| 0 | 25 | 10 | Chitosan |
| ≤10 | 25 | 10 | Shilajit |
| ≤10 | 25 | 10 | Cs-Sh |
| 93 | 25 | 10 | Cs-Sh@Cu |