Supplementary Information for

Low-voltage and fully flexible analogue/digital mixed-signal circuits based on carbon nanotubes for epidermal sensor applications

Taiga Kashima1, Shigeru Kishimoto1, Jun Hirotani1, Hiromichi Kataura2, and Yutaka Ohno1,3,*

1 Department of Electronics, Nagoya University, Furo-cho, Chikusa-ku, Nagoya 464-8603, Japan

2 Nanomaterials Research Institute, National Institute of Advanced Industrial Science and Technology, Tsukuba, Ibaraki, 305-8565, Japan

3 Institute of Materials and Systems for Sustainability, Nagoya University, Furo-cho, Chikusa-ku, Nagoya 464-8601, Japan

* Corresponding author e-mail: yohno@nagoya-u.jp

Contents:

- Modeling of CNT TFT

- AC and DC gains of the proposed op-amp

- Supplemental descriptions on fabricated circuits.

- Parameters of CNT TFTs and passive elements in each circuit

- Performance comparison of TFT-based differential amplifiers and op-amps

- Measurement of CMRR of instrumentation amplifier

- Evaluation of ENOB and energy efficiency

- Performance comparison of flexible ADCs

- Continuous operation of AFE

- Modeling of CNT TFT

The equivalent circuit model for a CNT TFT developed in this study is shown in Fig. S1. The device model was fundamentally based on the previous study,S1 which was modified to exhibit ambipolar characteristics of CNT TFTs to obtain more accurate frequency characteristics. The equations for the current and voltage are shown below,S1

IDSp=-μpCoxWLfpVG, VSγ+2-fpVG, VDγ+2γ+21+λVDS,#S1

IDSn=μnCoxWLfnVG,VDγ+2-fnVG, VSγ+2γ+21+λVDS,#S2

fpVG, V=VSS×ln1+exp-VG-VTp-VVSS,#S3

fnVG, V=VSS×ln1+expVG-VTn-VVSS,#S4

where VG, VS, and VD are the gate, source, and drain potentials relative to ground, respectively. VSS is subthreshold voltage that represents the steepness of SS. m is mobility, COX is oxide capacitance per unit area, W is channel width, L is channel length, g is mobility enhancement factor and l is channel length modulation factor.

Table S1 shows the mean value and standard deviation of parameters extracted by fitting above equations to experimentally measured I-V and C-V characteristics as following procedure,

- Extraction of g from measured ID-VGS characteristics by using HVG function.S2

- Extraction of l from the saturation slope of measured ID-VDS characteristics.

- Extraction of RC from measured ID-VGS characteristics using Y-function method.S3

- Extraction of VSS from logarithmic subthreshold slope of measured ID-VGS characteristics.

- Extraction of COX and overlap capacitance per unit area (COV) by using L dependence of measured gate capacitance (CG = COXLW + 2COVW).

- Extraction of mp, mn, VTp and VTn from measured ID-VGS characteristics by fitting to Eqs. S1 and S2.

Fig. S1 | Equivalent circuit of the CNT-TFT model.

Table S1 | Extracted parameters of the fabricated CNT-TFTs.

- AC and DC gains of the proposed op-amp

The AC gain AAC and DC gain ADC of the proposed op-amp circuit are given by

AAC=gm21ro2+1ro4+1ro6-1gm71ro7+1ro8-1,	(S5)

ADC=gm21ro2+gm4+1ro6-1gm71ro7+gm8-1≤gm2gm4gm7gm8=W2L2W7L7W4L4W8L8,	(S6)

where gm and ro are the transconductance and output resistance, respectively, of a transistor; W and L are the channel width and length, respectively, of a transistor; and the subscript indicates the number of the transistor.

The proposed op-amp can achieve an AAC comparable to that of the two-stage CMOS-based op-amp (gm21ro2+1ro4-1gm61ro5+1ro6-1), even though it comprises single-polarity transistors. In contrast, ADC can be controlled to be less than unity by adjusting the W/L ratio of the transistors. For instance, ADC < 0 dB can be achieved by setting W2 = W4 and W7 = W8 with a constant L. The transistors M3, M4, and M8 are biased under the condition VOUT < VB < VDD to operate in the saturation region through R1, R2, and R3. Thus, their ro values are sufficiently high to obtain a high AAC.

In the circuit simulation, the optimal VB for maximising AAC was derived at VB/VDD = 0.7 as can be seen in Fig. S2. The optimal VB should realise a high AAC = 48 dB and small ADC = -4.8 dB.

Fig. S2 | Simulated gain characteristics of the proposed op-amp circuit as a function of VB/VDD.

- Supplemental descriptions on fabricated circuits

Op-amp circuit

The AC-coupled load comprised a CNT TFT and capacitor (e.g. M9 and C1 in Fig. 3b in the main text) and the cut-off frequency was set as lower than 1 Hz by tuning W/L of the TFT. The bias voltage VB, which was applied to the load TFTs (M9, M10, and M22), was carefully determined by the five TFTs (M1–M5) in the bias circuit to realise the optimal condition VB/VDD = 0.625. The source follower output stage was used to reduce the output impedance of the op-amp by a magnitude of ten to a few hundred kiloohms. This reduction in the output impedance was essential to configure the negative-feedback circuit with the op-amp. The detailed circuit parameters are shown in Table S2.

Non-inverting amplifier

A 20-nm-thick nichrome thin film was used for resistors R1 and R2 of the non-inverting amplifier. The dimensions of the resistors were designed to obtain R2/R1 = 8, which would achieve an ideal gain of 19.1 dB for the non-inverting amplifier. The resistors exhibited good ohmic I–V characteristics and linear dependence on the length as shown in Fig. S3.

a                           b

Fig. S3 | Electrical characteristics of nichrome thin film resistors. a, I-V characteristics of nichrome resistance for various length of nichrome thin film resistors. Inset shows a micrograph of a resistor. b, Resistance as a function of length of nichrome thin film resistor.

Delta-sigma ADC

The non-overlapping clock generator generates the clock phases 1 and 2, which are distributed to the SC  ADC. The SC integrator consists of capacitors C1 and C2 and switches M1–M4. When 1 = VDD and 2 =VSS, M1 and M2 are closed so that C1 is charged by C1VIN. After half a clock, 1 (2) turns to VSS (VDD), and M3 and M4 are closed. Then, the charge of C1VIN  C1Q2 is integrated into C2, where Q2 is the output of the RS latch and equal to VDD or VSS. The op-amp outputs the voltage gain of C1/C2 to the latched comparator. When 1 = VDD and 2 =VSS, the output of the latched comparator Q1 is determined by the relation between the input voltage V1 and ground (GND). The latched comparator is reset after half a clock (i.e. at1 = VSS and 2 =VDD) (The operation of the latched comparator is described below). The following RS latch maintains the output Q1 for one clock and then provides feedback to the SC integrator through C1. Thus, the  ADC outputs a 1-bit pulse density modulation signal that depends on the input voltage.

Latched comparator

A latched comparator operates in comparison mode and in reset mode during one clock cycle. The two pairs of pseudo-CMOS inverters, composed of four TFTs (M4, M6, M8, M10, or M5, M7, M9, M11) were used for the latch as shown in Fig. S4a. When f1 = VSS and f2 = VDD, the circuit operates in the reset mode, where M12 and M13 are turned on to set the inverters’ input and output voltage to be VDD as can be seen in Fig. S4b. After a half clock, f1 and f2 respectively turns to VDD and VSS, and the circuit operates in the comparison mode. In this mode, M1 is turned on, so that, currents begin to flow through M2 and M3. Here, if VIN < GND, reaches VSS faster than Q, and positive feedback will further accelerate the imbalance between Q and , so that, the output state Q = VSS and = VDD are determined.

a                      b

Fig. S4 | Operation of latched comparator. a, Circuit diagram. b, simulation result.

AFE

The gains were designed to be 26.5 dB for the instrumentation amplifier, -6.1 dB for the bandpass filter, and 18.7 dB for the non-inversion amplifier for an overall gain of 39.1 dB. The detailed parameters are given in Table S2. The AFE had a circuit area of 8.84 mm2 and used 187 transistors.

- Parameters of CNT TFTs and passive elements in each circuit

The parameters of CNT TFTs and passive elements for each circuit simulated or fabricated in this work are summarized in Table S2.

Table S2 | Parameters of CNT TFTs and passive elements for each circuit.

- Performance comparison of TFT-based differential amplifiers and op-amps

The detailed performance indices of TFT-based differential amplifiers and op-amps reported previously and that of op-amp fabricated in this work are summarized in Table S3.

Table S3 | Performance comparison of TFT-based differential amplifiers.

- Measurement of CMRR of instrumentation amplifier

To evaluate common-mode rejection ration (CMRR) of the instrumentation amplifier, we measured both differential-mode gain and common-mode gain of the circuit as shown in Fig. S5. For differential mode gain, a sinusoidal voltage was applied to the positive input terminal and the negative terminal was grounded. The input and output voltage waveforms were measured by an oscilloscope. The differential gain ADM was measured to be 28.6 dB from the voltage waveforms. For the common-monde gain, a sinusoidal voltage is applied to both positive and negative input terminals. The common-mode gain ACM was measured to be -18.1 dB. Thus, CMRR (= ADM / ACM) was evaluated to be 46.7 dB.

a                             b

Fig. S5 | Measurement setups (upper) and transient characteristics (bottom) to measure (a) differential-mode and (b) common-mode gains of an instrumentation amplifier.

- Evaluation of ENOB and energy efficiency

ENOB was evaluated as,

ENOB bit= SNDR dB-1.766.02#S7

The Walden figure of meritS4 (FoM) that commonly used to evaluate the energy efficiency of ADC is described as follows,

FoM Jconv.step.=Power W2ENOB bit∙2∙Bandwidth Hz#S8

- Performance comparison of flexible ADCs

The detailed performance indices of flexible ADCs are summarized in Table S4 for comparison of the CNT-based flexible ADC realized in this work to those reported in previous works.

Table S4 | Performance comparison of flexible ADCs.S5–S9

- Continuous operation of AFE

To demonstrate the stability of the present AFE circuit, ECG was continuously measured through the AFE. The methods for the measurement and reconstruction of the digital data are same as described in the main text. Figure S6 shows the ECG waveforms reconstructed from the digital data in the beginning of the continuous measurement and after 1 h. The ECG was observable even after 1 h.

Fig. S6 | ECG waveforms at the beginning (upper) after 1 h (bottom).

References

S1.	Shao, L. et al. Compact modeling of thin film transistors for flexible hybrid IoT design. IEEE Design and Test 36, 6-14 (2019).

S2.	Deen, M. J., Marinov, O., Zschieschang, U. & Klauk, H. Organic thin-film transistors: Part II-parameter extraction. IEEE Trans. Electron Devices 56, 2962–2968 (2009).

S3.	Diouf, C. et al. ‘y function’ method applied to saturation regime: Apparent saturation mobility and saturation velocity extraction. Solid. State. Electron. 85, 12–14 (2013).

S4.	Walden, R. H. Analog-to-digital converter survey and analysis. IEEE J. Sel. Areas Commun. 17, 539–550 (1999).

S5.	Marien, H., Steyaert, M. S. J., van Veenendaal, E. & Heremans, P. A fully integrated DS ADC in organic thin-film transistor technology on flexible plastic foil. IEEE J. Solid-State Circuits 46, 276–284 (2011).

S6.	Raiteri, D., Lieshout, P. Van, Roermund, A. Van & Cantatore, E. An organic VCO-based ADC for quasi-static signals achieving 1LSB INL at 6b resolution. Dig. Tech. Pap. - IEEE Int. Solid-State Circuits Conf. 56, 108–109 (2013).

S7.	Garripoli, C. et al. An a-IGZO asynchronous delta-sigma modulator on foil achieving up to 43dB SNR and 40dB SNDR in 300Hz bandwidth. Dig. Tech. Pap. - IEEE Int. Solid-State Circuits Conf. 60, 260–261 (2017).

S8.	Papadopoulos, N. et al. Flexible selfbiased 66.7nJ/c.s. 6bit 26S/s successive-approximation C-2C ADC with offset cancellation using unipolar Metal-Oxide TFTs. Proc. Cust. Integr. Circuits Conf., 7–10 (2017).

S9.	Papadopoulos, N. P. et al. Toward temperature tracking with unipolar metal-oxide thin-film SAR C-2C ADC on Plastic. IEEE J. Solid-State Circuits 53, 2263–2272 (2018).