List of Tables:

Table S1. Response surface methodology (RSM) experimental table.

Table S2. Variance analysis of regression model for ip.

Table S3. Fitted electrochemical parameters of the pure copper bare and pre-passivation samples during corrosion tests.

Table S4. Fitted electrochemical parameters of the B30 alloy bare and pre-passivation samples during corrosion tests.

List of Figure:

Fig. S1. Potentiodynamic polarization curves of the pre-passivation samples formed under the environmental conditions listed in RSM table.

Table S1. Response surface methodology (RSM) experimental table.

| Order number | BTA (g/L) | SSA (g/L) | H2O2 (ml/L) | Temperature (℃) | Epit (Ω·cm2) | ip (μA/cm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 12 | 1 | 30 | 50 | 0.225 | 30.179 |
| 2 | 12 | 1 | 10 | 50 | 0.263 | 3.871 |
| 3 | 4 | 1 | 20 | 37.5 | - | - |
| 4 | 12 | 3 | 20 | 25 | 0.248 | 16.904 |
| 5 | 20 | 3 | 20 | 25 | 0.246 | 0.712 |
| 6 | 20 | 3 | 10 | 37.5 | 0.265 | 0.704 |
| 7 | 12 | 3 | 20 | 25 | 0.260 | 1.212 |
| 8 | 20 | 3 | 20 | 25 | 0.237 | 0.388 |
| 9 | 12 | 5 | 10 | 37.5 | 0.217 | 1.178 |
| 10 | 12 | 3 | 20 | 50 | 0.260 | 4.005 |
| 11 | 4 | 5 | 20 | 37.5 | - | - |
| 12 | 20 | 3 | 20 | 50 | 0.246 | 0.350 |
| 13 | 12 | 3 | 20 | 25 | 0.250 | 11.072 |
| 14 | 4 | 3 | 20 | 25 | - | - |
| 15 | 4 | 3 | 10 | 37.5 | - | - |
| 16 | 4 | 3 | 20 | 50 | 0.115 | 64.003 |
| 17 | 12 | 3 | 20 | 37.5 | 0.215 | 4.263 |
| 18 | 4 | 3 | 10 | 37.5 | 0.158 | 7.267 |
| 19 | 12 | 3 | 20 | 37.5 | 0.197 | 0.462 |
| 20 | 12 | 1 | 10 | 37.5 | 0.250 | 0.255 |
| 21 | 12 | 1 | 30 | 25 | 0.250 | 1.434 |
| 22 | 20 | 5 | 20 | 37.5 | 0.210 | 0.546 |
| 23 | 4 | 3 | 20 | 50 | 0.123 | 72.750 |
| 24 | 20 | 1 | 20 | 37.5 | 0.171 | 0.298 |
| 25 | 12 | 5 | 10 | 25 | 0.212 | 3.445 |
| 26 | 4 | 3 | 30 | 37.5 | - | - |
| 27 | 20 | 3 | 10 | 37.5 | 0.262 | 4.221 |
| 28 | 12 | 5 | 30 | 37.5 | 0.154 | 0.249 |
| 29 | 12 | 3 | 20 | 37.5 | 0.221 | 1.510 |
| 30 | 12 | 1 | 30 | 37.5 | 0.240 | 1.158 |
| 31 | 12 | 1 | 10 | 37.5 | 0.261 | 15.616 |
| 32 | 12 | 5 | 10 | 37.5 | 0.168 | 0.745 |
| 33 | 4 | 3 | 20 | 25 | - | - |
| 34 | 12 | 3 | 20 | 37.5 | 0.219 | 5.872 |
| 35 | 20 | 5 | 20 | 37.5 | 0.198 | 0.250 |
| 36 | 12 | 1 | 10 | 25 | 0.265 | 1.510 |
| 37 | 20 | 3 | 30 | 37.5 | 0.213 | 1.199 |
| 38 | 12 | 3 | 20 | 50 | 0.269 | 1.618 |
| 39 | 12 | 5 | 10 | 50 | 0.223 | 0.556 |
| 40 | 20 | 3 | 20 | 50 | 0.189 | 2.834 |
| 41 | 12 | 3 | 20 | 50 | 0.234 | 0.287 |
| 42 | 12 | 5 | 30 | 25 | 0.129 | 0.377 |
| 43 | 4 | 5 | 20 | 37.5 | - | - |
| 44 | 12 | 3 | 20 | 50 | 0.246 | 8.816 |
| 45 | 20 | 1 | 20 | 37.5 | - | - |
| 46 | 4 | 3 | 30 | 37.5 | - | - |
| 47 | 12 | 5 | 30 | 50 | 0.119 | 0.163 |
| 48 | 20 | 3 | 30 | 37.5 | 0.196 | 0.173 |
| 49 | 4 | 1 | 20 | 37.5 | - | - |
| 50 | 12 | 5 | 30 | 37.5 | 0.141 | 1.828 |
| 51 | 12 | 3 | 20 | 37.5 | 0.203 | 1.283 |
| 52 | 12 | 3 | 20 | 25 | 0.229 | 14.008 |
| 53 | 12 | 1 | 30 | 37.5 | 0.181 | 8.816 |

Table S2. Variance analysis of regression model for ip

| Source | Sum of Squares | df | Mean Square | F-value | P-value |
| --- | --- | --- | --- | --- | --- |
| Model | 67846.73 | 14 | 4846.2 | 15.55 | < 0.0001 |
| A-BTA | 36219.53 | 1 | 36219.53 | 116.18 | < 0.0001 |
| B-Sulfosalicylic acid | 985.6 | 1 | 985.6 | 3.16 | 0.0834 |
| C-H2O2 | 470.01 | 1 | 470.01 | 1.51 | 0.227 |
| D-Temperature | 158.26 | 1 | 158.26 | 0.5077 | 0.4805 |
| AB | 1237.59 | 1 | 1237.59 | 3.97 | 0.0535 |
| AC | 1158.87 | 1 | 1158.87 | 3.72 | 0.0613 |
| AD | 533.51 | 1 | 533.51 | 1.71 | 0.1987 |
| BC | 34.93 | 1 | 34.93 | 0.112 | 0.7397 |
| BD | 146.29 | 1 | 146.29 | 0.4692 | 0.4975 |
| CD | 105.56 | 1 | 105.56 | 0.3386 | 0.5641 |
| A² | 20590.82 | 1 | 20590.82 | 66.05 | < 0.0001 |
| B² | 1571.79 | 1 | 1571.79 | 5.04 | 0.0306 |
| C² | 1305.24 | 1 | 1305.24 | 4.19 | 0.0477 |
| D² | 27.36 | 1 | 27.36 | 0.0878 | 0.7686 |
| Residual | 11846.42 | 38 | 311.75 |  |  |
| Lack of Fit | 2177 | 12 | 181.42 | 0.4878 | 0.9036 |
| Pure Error | 9669.42 | 26 | 371.9 |  |  |
| Cor Total | 79693.15 | 52 |  |  |  |
| R2=0.8513, Adjusted R2=0.7966, Predicted R2=0.6713 |  |  |  |  |  |

Table S3. Fitted electrochemical parameters of the pure copper bare and pre-passivation samples during corrosion tests.

|  | Corrosion time | Rs (Ω·cm2) | Rf (Ω·cm2) | Qf (μF·cm-2·sn) | nf | Rct (Ω·cm2) | Qct (μF·cm-2·sn) | nct | Rp= Rf+ Rct (Ω·cm2) |  | χ2 (×10-3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bare samples | 12 h | 8.19 | 476.2 | 113 | 0.76 | 9904 | 1598 | 0.43 |  | 10380.2 | 3.41 |
|  | 10 d | 9.98 | 80.98 | 162.5 | 0.69 | 11310 | 32.01 | 0.88 |  | 11390.98 | 0.51 |
|  | 20 d | 6.54 | 105.6 | 0.62 | 0.56 | 95310 | 67.6 | 0.83 |  | 95415.6 | 8.77 |
|  | 30 d | 9.15 | 5125 | 262.3 | 0.68 | 6902 | 203.4 | 0.87 |  | 12027 | 1.19 |
|  | 50 d | 7.41 | 290.2 | 9.42 | 0.89 | 18390 | 182.2 | 0.56 |  | 18680.2 | 2.2 |
|  | 70 d | 2.37 | 81.27 | 12.4 | 0.92 | 12640 | 359.8 | 0.65 |  | 12721.27 | 1.37 |
|  | 90 d | 3.58 | 122.3 | 1.1 | 0.96 | 33690 | 48.83 | 0.55 |  | 33812.3 | 1.72 |
| Pre-passivation samples | 12 h | 6.27 | 31110 | 5.06 | 0.74 | 140700 | 75.06 | 0.64 |  | 171810 | 1.87 |
|  | 10 d | 6.53 | 125400 | 6.18 | 0.62 | 5960 | 0.03 | 0.95 |  | 131360 | 11.3 |
|  | 20 d | 2.87 | 320900 | 10.41 | 0.66 | 651 | 0.15 | 0.80 |  | 321551 | 4.79 |
|  | 30 d | 5.26 | 79680 | 22.79 | 0.74 | 489.4 | 0.24 | 0.78 |  | 80169.4 | 1.68 |
|  | 50 d | 0.81 | 63690 | 13.13 | 0.82 | 3332 | 1.36 | 0.93 |  | 67022 | 5.02 |
|  | 70 d | 7.42 | 15090 | 29.14 | 0.93 | 72200 | 70.3 | 0.93 |  | 87290 | 3.25 |
|  | 90 d | 6.86 | 11660 | 43.61 | 0.97 | 448400 | 31.17 | 0.95 |  | 460060 | 2.06 |

Table S4. Fitted electrochemical parameters of the B30 alloy bare and pre-passivation samples during corrosion tests.

|  | Corrosion time | Rs (Ω·cm2) | Rf (Ω·cm2) | Qf (μF·cm-2·sn) | nf | Rct (Ω·cm2) | Qct (μF·cm-2·sn) | nct | Rp= Rf+ Rct (Ω·cm2) |  | χ2 (×10-3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bare samples | Static immersion |  |  |  |  |  |  |  |  |  |  |
|  | 0 d | 9.59 | 4.57 | 376.3 | 0.67 | 7377 | 75.26 | 0.89 |  | 7381.57 | 0.53 |
|  | 10 d | 14.85 | 2046 | 3802 | 0.99 | 18850 | 138.1 | 0.76 |  | 22652 | 1.02 |
|  | 20 d | 9.82 | 1.45 | 779 | 0.63 | 63120 | 386.9 | 0.76 |  | 63121.45 | 0.16 |
|  | 30 d | 8.86 | 10.67 | 35.56 | 0.72 | 112700 | 19.83 | 0.87 |  | 112710.67 | 0.54 |
| Pre-passivation samples | 0 d | 8.73 | 71930 | 2.44 | 0.83 | 558700 | 9.46 | 0.78 |  | 630630 | 4.69 |
|  | 10 d | 10.16 | 7509 | 5.09 | 0.82 | 1571000 | 14.16 | 0.51 |  | 1578509 | 0.78 |
|  | 20 d | 10.62 | 40700 | 9.33 | 0.78 | 1013000 | 9.66 | 0.54 |  | 1053700 | 3.96 |
|  | 30 d | 9.21 | 169700 | 10.35 | 0.8 | 1460000 | 5.79 | 0.52 |  | 1629700 | 2.66 |
| Bare samples | Flow accelerated corrosion |  |  |  |  |  |  |  |  |  |  |
|  | 0 d | 12.71 | 9.28 | 264.65 | 0.78 | 8039 | 341.2 | 0.74 |  | 8048.28 | 1.16 |
|  | 10 d | 9.78 | 15.26 | 38.75 | 0.75 | 45440 | 70.34 | 0.74 |  | 45478.75 | 0.68 |
|  | 20 d | 10.32 | 11.65 | 38.9 | 0.74 | 94570 | 22.7 | 0.86 |  | 94581.65 | 1.34 |
|  | 30 d | 7.15 | 22.18 | 30.49 | 0.83 | 134100 | 50.37 | 0.69 |  | 134122.18 | 0.21 |
| Pre-passivation samples | 0 d | 6.53 | 12770 | 6.04 | 0.82 | 880300 | 18.79 | 0.45 |  | 893070 | 1.12 |
|  | 10 d | 9.67 | 9068 | 10.58 | 0.79 | 292800 | 10.74 | 0.47 |  | 301868 | 0.30 |
|  | 20 d | 12.92 | 72170 | 32.79 | 0.79 | 105600 | 33.19 | 0.73 |  | 177770 | 0.92 |
|  | 30 d | 8.64 | 16.1 | 34.37 | 0.73 | 131600 | 8.69 | 0.87 |  | 131616.1 | 2.14 |

Fig. S1. Potentiodynamic polarization curves of the pre-passivation samples formed under the environmental conditions listed in RSM table.