Table 3 Contact angle and drop filtration time of untreated, hot-pressed and functionalized cellulose acetate membranes.

| MEMBRANE | CONTACT ANGLE (°) | COMPLETE FILTRATION | FIGURE |
| --- | --- | --- | --- |
| MCA | 104 ± 1 | 100 min |  |
| MCA-HP | 55 ± 2 | 5 min |  |
| MCA-1%CNC-HP | 43 ± 4 | 24 s |  |
| MCA-3%CNC-HP | 37 ± 1 | 33 s |  |
| MCA-1%CNCTEMPO-HP | 44 ± 1 | 21 s |  |
| MCA-3%CNCTEMPO-HP | 37 ± 2 | 23 s |  |