Supporting Information

Photocatalytic treatment of different types of high-concentration ammonia wastewater by Cu/TiO2 film and its mechanism study

Jianpei Feng, Guan Zhang*, Xiaolei Zhang and Ji Li*

School of Civil and Environmental Engineering, Harbin Institute of Technology, Shenzhen, Shenzhen 518055, China.

*E−mail: zhangguan@hit.edu.cn;    liji99@hit.edu.cn

List of Figures and Tables:

Fig. S1. Fitting curves of chemical kinetics of photocatalytic oxidation of ammonia at different initial pH.

Fig. S2. Fitting curves of chemical kinetics of photocatalytic oxidation of ammonia at different temperature.

Fig. S3. (a) Nitrite nitrogen and (b) nitrate nitrogen production during photocatalytic conversion of ammonia nitrogen in aqueous solution by Cu/TiO2 film with different supports.

Fig. S4. The mass change of Cu/TiO2 films with different supports before and after the reaction.

Fig. S5. The surface morphology of Cu/TiO2 films on different supports before and after the photocatalytic reaction.

Fig. S6. The mass change of Cu/TiO2@Glass with different flow rates before and after the reaction.

Fig. S7. The concentration of Cu2+ in aqueous solution by Cu/TiO2@Glass under the irradiation of Xe lamp.

Table S1 Product conversion rate of photocatalytic ammonia reaction after 6 h under different initial pH

Table S2 Product conversion rate of photocatalytic ammonia reaction after 6 h with different catalyst

Fig. S1. Fitting curves of chemical kinetics of photocatalytic oxidation of ammonia at different initial pH

Fig. S2. Fitting curves of chemical kinetics of photocatalytic oxidation of ammonia at different temperature

Fig. S3. (a) Nitrite nitrogen and (b) nitrate nitrogen production during photocatalytic conversion of ammonia nitrogen in aqueous solution by Cu/TiO2 film with different supports.

Fig. S4. The mass change of Cu/TiO2 films with different supports before and after the reaction.

d

c

b

a

h

g

f

e

Fig. S5. The surface morphology of Cu/TiO2 films on different carriers before and after the photocatalytic reaction: (a) Titanium sheet before reaction; (b) Titanium sheet after reaction; (c) Copper sheet before reaction; (d) Copper sheet after reaction; (e) Glass before reaction; (f) Glass after reaction; (g) ITO before reaction; (h) ITO after reaction.

Fig. S6. The mass change of Cu/TiO2@Glass with different flow rates before and after the reaction.

Fig. S7. The concentration of Cu2+ in aqueous solution by Cu/TiO2@Glass under the irradiation of Xe lamp.

The removal rate of ammonia nitrogen and the generation rate of various products can be calculated by the following method. The generated NO2- and NO3- were measured, and the possible generated gaseous products like N2 and N2O were estimated according to N-balance. The selective conversion efficiencies of various products as shown in Table 1 and Table 2 were calculated by the following equation.

(1)

(2)

(3)

(4)

Where C0 and C1 are the initial ammonia nitrogen concentration and the ammonia nitrogen concentration after 6 h reaction, C2 and C3 are the NO2--N concentration and NO3--N concentration after 6 h reaction, X1 is the ammonia nitrogen removal rate, X2, X3 and X4 are the conversion rates of NO2--N, NO3--N and gaseous products, respectively.

Table S1 Product conversion rate of photocatalytic ammonia reaction after 6 h under different initial pH in the reaction system Ⅰ.

| Initial pH | X1 | X2 | X3 | X4 |
| --- | --- | --- | --- | --- |
| 7.0 | 0.59% | 0.00% | 0.00% | 0.00% |
| 8.0 | 8.77% | 0.00% | 5.96% | 94.04% |
| 9.0 | 22.34% | 29.57% | 0.00% | 70.43% |
| 10.0 | 28.45% | 32.74% | 0.00% | 67.26% |
| 11.0 | 28.84% | 38.84% | 0.00% | 61.16% |

Table S2 Product conversion rate of photocatalytic ammonia reaction after 6 h with different catalyst.

| Sample | X1 | X2 | X3 | X4 |
| --- | --- | --- | --- | --- |
| Cu/TiO2 powder | 28.45% | 32.74% | 0.00% | 67.26% |
| Cu/TiO2@Glass | 62.92% | 0.00% | 0.76% | 99.24% |
| Cu/TiO2@ITO | 48.37% | 0.03% | 0.48% | 99.49% |
| Cu/TiO2@Titanium sheet | 52.67% | 0.10% | 0.00% | 99.90% |
| Cu/TiO2 @Copper sheet | 51.27% | 0.00% | 1.57% | 98.43% |