Supporting Information

Stabilization of ZnO nanoparticles using water extract of waste coconut husk and photocatalytic activity

RiuRiuWary1,SanjibBaglari1, DuluBrahma2,Ujjal K Gautam3,Pranjal Kalita2 ,*, ManasiBuzar Baruah1,*

1Department of Physics, Central Institute of Technology Kokrajhar (Deemed to be University, MHRD, Govt. of India), Kokrajhar-783370, Assam, India

2Department of Chemistry, Central Institute of Technology Kokrajhar (Deemed to be University, MHRD, Govt. of India), Kokrajhar-783370, Assam, India

3Indian Institute of Science Education and Research Mohali, Department of Chemical Sciences, Knowledge City, Sector 81, SAS Nagar, Manauli-140306.

*Corresponding author.

# Email: mbbaruah@cit.ac.in, p.kalita@cit.ac.in

Supporting information “S1”

Williamson-Hall (W-H) plot

Fig. S1W-H plot of (a) ZnO NPs-pH 8.6, (b) ZnO NPs-pH 10.4 and (c) ZnO NPs-pH 12.7 prepared at different pH value.

The crystallite size (D) and lattice strain (Ɛ) were calculated from Williamson-Hall (W-H) method from the following relation [1]-

βhklcosθ=KλD+4εsinθ

Where K, β and λ represents shape factor,full width at half maximum (FWHM) and wavelength of the radiation (0.154 nm). The crystallite size (D) and lattice strain(Ɛ) were obatined from y-axis intercept and slop inβhklcosθ vs 4sinθ  plot  shown in Fig.S1(a-c)

Supporting information “S2”

(a)

(c)

(b)

Fig. S2 EDX micrograph of (a) ZnO NPs-pH 8.6, (b) ZnO NPs-pH 10.4 and (c) ZnO NPs-pH 12.7samples with weight and atomic percentage.

Table S1. Comparison of photocatalytic activity of ZnO NPs synthesized with different precipitating or capping agent.

| Material | Precipitating or Capping agent used | Pollutant used | Time of degradation (min) | Degradation efficiency | Ref. |
| --- | --- | --- | --- | --- | --- |
| ZnO NPs | Leaves extract | Methyl Orange | 100 | 93.4% | (Saraswathi et al. 2017) |
| ZnO | Leaves Extract | Methylene Blue | 120 | 92% | (Madan et al. 2016) |
| ZnO NPs | Peel Extract | Methylene Blue | 180 | 97% | (Nava et al. 2017) |
| ZnO NPs | Peel Extract | Methylene Blue | 120 | 63% | (Madhumitha et al. 2019) |
| ZnO NPs | NaOH | Methylene Blue | 120 | 87.74% | (Akhil et al. 2016) |
| Pure ZnO | NaOH | Methylene Blue | 180 | 12.4% | (Pandimuragan et al. 2016) |
| ZnO | NaOH | Methylene Blue | 210 | 80% | (Kahsay et al. 2019) |
| ZnO NPs | Aqueous NH3 | Methylene Blue | 270 | 97.4% | (Abbas et al. 2017) |
| ZnO | Aqueous NH3 | Methylene Blue | 240 | 54% | (Velanganni et al. 2018) |
| ZnO | KOH | Methylene Blue | 120 | 79.76% | (Khokhra et al. 2015) |
| ZnO | KOH | RhodamineB | 240 | 95.53% | (Shi et al. 2015) |
| Commercial ZnO NPs |  | Methylene Blue | 120 | 37% | (Azarang et al. 2015) |
| Pure ZnO NPs | NaOH | Malachite Green | 120 | 80% | (Lavand et al. 2015) |
| ZnO NPs | CHAWE | Methylene Blue Methyl Orange | 120 120 | 97.7% 56% | Present work |

Reference

Goswami A (1996) ‘Thin film fundamentals’, New age international (p) ltd publishers New Delhi pp 411.

Saraswathi VS, Tatsugi J, Shin PK, SanthakumarK (2017) Facile biosynthesis, characterization, and solar 	assisted photocatalytic effect of ZnO nanoparticles mediated by leaves of L. Speciosa. Journal of 	Photochemistry and Photobiology B: Biology 17: 89-98. 	https://doi.org/10.1016/j.jphotobiol.2016.12.032

Madan HR,Sarma SC, et al. (2016) Facile green fabrication of nanostructures ZnO plates, bullets, flower, 	prismatic tip, closed pine cone: Their antibacterial, antioxidant, photoluminescence and 	photocatalytic properties.SpectrochimicaActa Part A: Molecular and Biomolecular Spectroscopy, 	152: 404-416. https://doi.org/10.1016/j.saa.2015.07.067

Nava OJ, Robles CAS, et al (2017) Fruit peel extract mediated green synthesis of zinc oxide 	nanoparticles. Journal of Molecular Structure 1147(5): 1-6. 	https://doi.org/10.1016/j.molstruc.2017.06.078

Madhumitha G,Fowsiya J, Gupta N, Kumar A, Singh M (2019) Green synthesis, characterization and 	antifungal and photocatalytic activity of Pithecellobiumdulce peel- mediated ZnO. Journal of 	Physics and Chemistry of Solids 127:43-51. https://doi.org/10.1016/j.jpcs.2018.12.005

Akhil K, JayakumarJ,Gayathri G, Khan SS (2016) Effect of various capping agent on photocatalytic, 	antibacterial and antibiofilmactivities of ZnO nanoparticles, Journal of Photochemistry & 	Photobiology. B:Biology 160: 32-42. https://doi.org/10.1016/j.jphotobiol.2016.03.015

Pandimuragan R, Thambidurai S (2016) Novel seaweed capped ZnOnanoparticls for effective dye 	photodegradation and antibacterial activity. Advanced Powder Technology 27: 1062-1072. 	https://doi.org/10.1016/j.apt.2016.03.014

Kahsay MH, TadasseA, Devi DR, BelachewN,Basavaish K(2019) Green synthesis of zinc oxide 	nanostructures and investigation of their photocatalytic and bactericidal applications. RSC 	Advances  9: 36967. https://doi.org/10.1039/C9RA07630A

Abbas KN, Bidin N (2017) Morphological driven photocatalytic activity of ZnO nanostructures. Applied 	Surface Science 394: 498-508. https://doi.org/10.1016/j.apsusc.2016.10.080

Velanganni S, Pravinraj S, Immanuel P, Thirunneelakandan R(2018) Nanostructures 	CdS/ZnOheterojunction configuration for photocatalytic degradation of methylene blue. Physics 	B: Condensed Matter 534: 56-62.https://doi.org/10.1016/j.physb.2018.01.027

Khokhra R, Singh RK, KumarR (2015) Effect of synthesis medium on aggregation tendencies of 	ZnOnanosheets and their superior photocatalytic performance. Journal of Material Science 50: 	819-832. https://doi.org/10.1007/s10853-014-8642-0

Shi R, Song X, Li J, Yang P (2015) Hierarchical ZnO with twinned structures: Morphology evolution, 	formation mechanism and properties. Materials Chemistry and Physics 156: 61-68. 	https://doi.org/10.1016/j.matchemphys.2015.02.020

Azarang M, Shuhaimi A, YousefiR, JahromiSP(2015) One-pot sol-gel synthesis of reduced grapheme 	oxide uniformly decorated zinc oxide nanoparticles in starch environment for highly efficient 	photodegradation of methylene blue. RSC Advances 5: 21888-21896. 	https://doi.org/10.1039/C4RA16767H

Lavand AB, MalgheYS (2015) Synthesis, characterization and visible light photocatalytic activity of 	nitrogen-doped zinc oxide nanospheres. Journal of Asian Ceramic Societies 3: 305-310. 	https://doi.org/10.1016/j.jascer.2015.06.002