Appendix 1: Parameters for Heat Conduction and Creep Damage Analyses

The heat conduction analysis parameters except the target welding parameters were determined as follows. The heat source width w and heat source depth d were defined as functions of target welding parameters, the heat input HV (J/mm) and the layer thickness DL (mm). First, real welding test were conducted using representative values of DL and HV, and the molten zone geometry, defined as the region exceeding the melting point, was identified through cross-sectional observation of weldments. Heat conduction analysis were performed while varying w and d to replicate this geometry, and the optimal values of w and d were determined accordingly. These were regressed as functions of HV and DL, yielding the following equations (1) and (2), where the coefficients Ai (i=1,2,3,4) and Bi i=1,2,3,4 were obtained:

w=A1×HV×DL+A2×HV+A3×DL+A4              (1)

d=B1×HV×DL+B2×HV+B3×DL+B4                (2)

The obtained values of coefficients Ai and Bi are shown in Table 3.

For other parameters in the heat conduction analysis, the vertical position of the heat source center was set equal to the layer thickness. The welding speed was fixed at 1.667 mm/s, and the heat source length was fixed at 2 mm. The thermal properties of the base metal and weld metal were calculated by JMatPro [21], with the chemical compositions of base metal and weld materials shown in Table 1.

The parameters used in the creep damage analysis were based on the prior study [15] and correspond to the test conditions in this study, 873 K and 100 MPa. The values used are listed in Table 4. Parameters for both the base metal and weld metal were taken from the base metal, while parameters for the HAZ were taken from the simulated HAZ. The creep deformation law was the Norton–Arrhenius law, and the creep damage model followed the time fraction law with using Huddleston stress [22].

Appendix 2. Table of welding path thickness configuration and pair numbers

| number of layers | layer thickness combination whose sum = 9 (mm) | layer thickness configuration pattern | layer thickness configuration pattern × heat input pattern | total |
| --- | --- | --- | --- | --- |
| 3 | 3 3 3 | 1 | 1×64=64 | 64 |
| 4 | 2 2 2 3 | 4C1=4 | 4×256=1024 | 4096 |
|  | 1 2 3 3 | 4C2×2C1=12 | 12×256=3072 |  |
| 5 | 1 2 2 2 2 | 5 | 5×1024=5120 | 46080 |
|  | 1 1 1 3 3 | 5C2=10 | 10×1024=10240 |  |
|  | 1 1 2 2 3 | 4C2×5=30 | 30×1024=30720 |  |
| 6 | 1 1 1 2 2 2 | 6C3=20 | 20×4096=81920 | 204800 |
|  | 1 1 1 1 2 3 | 6C2×2C1=30 | 30×4096=122880 |  |
| 7 | 1 1 1 1 1 1 3 | 7 | 7×16384=114688 | 458752 |
|  | 1 1 1 1 1 2 2 | 7C2=21 | 21×16384=344064 |  |
| 8*) | 1 1 1 1 1 1 1 2 | 8 | 8×65536=524288 | 524288 |
| 9 | 1 1 1 1 1 1 1 1 1 | 1 | 1×262144=262144 | 262144 |
| sum |  |  |  | 1500224 |
| *) divide 8 groups for each layer thickness configuration |  |  |  |  |

Appendix 3

The criteria for excluding damaged elements due to singular stress fields, as well as the method for constructing a classifier to determine whether rupture life can be computed is explained. From the creep damage analysis results obtained in the forward workflow, time-series data of the damage distribution for all elements at each time step were extracted. At each time point, the set of damaged elements (i.e. damage=1) within the HAZ was partitioned into connected components, defined as groups of elements that share edges or faces. These connected components were analyzed according to the following criteria to classify rupture types:

- If only connected components not including triple junctions were present: the time of appearance of the component was defined as the rupture life (rupture type: internal rupture).

- If the connected component including a triple junction had a spatial extent not exceeding 0.1 mm from the triple junction, and there also existed another component that did not include a triple junction (non-triple-junction component): the time at which such a non-triple-junction component appeared was defined as the rupture life (rupture type: modified internal rupture, see Fig. 4(a)).

- If no non-triple-junction components were present and a component including a triple junction exceeded 0.1 mm in size from the junction: it was judged that damage due to singular stress and other causes could not be separated, and rupture life was not determined (rupture type: boundary rupture, see Fig. 4(b)).

Based on these rules, rupture type classification and rupture life estimation were applied to the time-series damage distribution data from the creep damage analysis, and both rupture life and rupture type were recorded. If rupture life could not be determined, the data were excluded from the training dataset. However, rupture type was recorded to prevent redundant recalculation when the same condition was selected again as a candidate.

For screening purposes, a RandomForestClassifier [28] was constructed using the HAZ geometry factors as explanatory variables. The classification target was set such that “internal rupture” or “modified internal rupture” was labeled as 1, and “boundary rupture” as 0. Hyperparameter optimization was performed using GridSearchCV [29] as implemented in scikit-learn. The search space for the hyperparameters of the RandomForestClassifier is shown in Table 5. The timing of classifier training was synchronized with each update of the Bayesian linear regression training dataset.