| layer |  | number of welding parameter | number of search condition | number of initial training data |  | achieved rupture time(h) | step | round | number of added train data |  |  | ratio of the number of added train data per number of search condition (%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | set |  |  | candidate | Tr could be calculated |  |  |  | for GP | for BL |  | GP | BL |
|  |  |  |  |  |  |  |  |  |  | candidate | Tr could be calculated |  |  |
| 3 |  | 3 | 64 | 4 | 3 | 540 | 11 | 5 | 37 | 27 | 12 | 58.0 | 42.2 |
| 4 |  | 8 | 4096 | 8 | 2 | 630 | 42 | 8 | 132 | 46 | 33 | 3.22 | 1.10 |
| 5 |  | 10 | 46080 | 11 | 0 | 610 | 58 | 8 | 188 | 56 | 27 | 0.407 | 0.120 |
| 6 |  | 12 | 204800 | 12 | 1 | 430 | 100 | 10※ | 423 | 85 | 6 | 0.207 | 0.0500 |
| 7 |  | 14 | 458752 | 13 | 1 | 170 | 85 | 9 | 340 | 87 | 2 | 0.0740 | 0.0190 |
| 8 | 1 | 8 | 65536 | 10 | 0 | 270 | 82 | 10※ | 358 | 94 | 1 | 0.546 | 0.143 |
|  | 2 | 8 | 65536 | 10 | 0 | 380 | 58 | 10※ | 226 | 88 | 2 | 0.345 | 0.134 |
|  | 3 | 8 | 65536 | 10 | 0 | 270 | 90 | 10※ | 465 | 91 | 3 | 0.710 | 0.139 |
|  | 4 | 8 | 65536 | 10 | 1 | - | 3 | 2 | 20 | 10 | 0 | 0.0305 | 0.0153 |
|  | 5 | 8 | 65536 | 10 | 1 | 280 | 130 | 10※ | 548 | 97 | 22 | 0.836 | 0.148 |
|  | 6 | 8 | 65536 | 10 | 0 | 250 | 5 | 3 | 21 | 12 | 1 | 0.0320 | 0.0183 |
|  | 7 | 8 | 65536 | 10 | 1 | - | 5 | 2 | 20 | 10 | 0 | 0.0305 | 0.0153 |
|  | 8 | 8 | 65536 | 10 | 0 | 98 | 3 | 2 | 20 | 10 | 1 | 0.0305 | 0.0153 |
| 9 |  | 9 | 262144 | 12 | 0 | - | 6 | 3 | 42 | 8 | 0 | 0.0160 | 0.00305 |
| summary |  |  | 1500224 | 140 | 10 | 630(max) |  |  | 2840 | 721 | 110 | 0.189 | 0.0481 |
|  |  |  |  |  |  |  |  | ※ terminated at 10 round |  |  |  |  |  |

Table.2 Number of input variables, number of conditions, number of initial conditions, achieved maximum rupture life, number of rounds and steps, number of added learning data, and search efficiency, for each number of layers.

|  | minimal creep rate |  |  | rupture time |  |  | elastic constants |  | misc. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | log⁡Aε | nε | Qε(J) | log⁡ATER | nTER | QTER(J) | Young’s module (MPa) | Poisson’s ratio | T=873(K) R=8.314 b=0.34 |
| base metal | 2.94×101 | 2.72 | 3.79×105 | -2.84×101 | -2.23 | -3.36×105 | 1.56695×105 | 2.74×10-1 |  |
| simulated HAZ | 1.88 | 4.62 | 3.41×105 | -1.87×101 | -5.49 | -3.55×105 | 1.06890×105 |  |  |

Table 4. Parameters for creep damage analysis, minimal creep rate for Norton-Arrhenius law, rupture time and elastic constants.

Table 6. Welding conditions, obtained rupture times for forward calculation, creep test, full-forward and creep only, shape factors for the real HAZ shape and full-forward, for Long, Normal and Short testing conditions.