Supplementary Information

Synthesis of stable zinc-phosphate micro/nanoparticles under acid and alkaline conditions

Journal of Nanoparticle Research

Benjamín Valdez-Salas1*†, Karen Guillén-Carvajal1*†, Ernesto Beltrán-Partida1, Jorge Salvador-Carlos1, Mario Alberto Curiel-Álvarez2, Nicola Nedev2

*Correspondence: benval@uabc.edu.mx, kguillen@uabc.edu.mx

†These authors contributed equally to this work.

1Core Facility- Química y materiales avanzados, Instituto de Ingeniería, Universidad Autónoma de Baja California, Blvd. Benito Juárez and Normal s/n., 21280 Mexicali, Baja California, México

2Core Facility- Semiconductores y manufactura avanzada, Instituto de Ingeniería, Universidad Autónoma de Baja California, Blvd. Benito Juárez and Normal s/n., 21280 Mexicali, Baja California, México

Table S1 Composition of chemical synthesis tests for ZnP in both acidic and alkaline media using droplets as a measure. A= acid, B= alkaline, HCl= hydrochloric acid, citric acid= AC, ascorbic acid= AA, and CC= Cocobetaine

| Medium | Name | NH4OH | HCl | AC | AA | CC |
| --- | --- | --- | --- | --- | --- | --- |
|  | Preliminar |  |  |  |  |  |
| B | ZnPB | 13 | - | - | - | 1% |
| A | ZnPA | - | 2 | - | - | 1% |
|  | Trial |  |  |  |  |  |
| B | 1BHCl | 13 / - | - | - | - | 1% |
| B | 2BHCl | 13 / 15 | - | - | - | 0.5% |
| B | 3BHCl | 15 / - | - | - | - | 0.1% |
| B | 1BAC | 20 / 19 | - | - | - | 1% |
| B | 2BAC | 13 / - | - | - | - | 0.5% |
| B | 3BAC | 14 / 14 | - | - | - | 0.1% |
| B | 1BAA | 10 / - | - | - | - | 1% |
| B | 2BAA | 12 / - | - | - | - | 0.5% |
| B | 3BAA | 10 / - | - | - | - | 0.1% |
| A | 1HCl | - | 3 / 4 | - | - | 1% |
| A | 2HCl | - | 3 / - | - | - | 0.5% |
| A | 3HCl | - | 2 / - | - | - | 0.1% |
| A | 1AC | - | - | 14 / - | - | 1% |
| A | 2AC | - | - | 18 / - | - | 0.5% |
| A | 3AC | - | - | 10 / 14 | - | 0.1% |
| A | 1AA | - | - | - | 40 / - | 1% |
| A | 2AA | - | - | - | 30 / - | 0.5% |
| A | 3AA | - | - | - | 20 / - | 0.1% |

Table S2 Preliminary resuspension tests in ZnP in a chemical medium. HCl = hydrochloric acid, citric acid = AC, ascorbic acid = AA, and CC = Cocobetaine

| Name | HCl | AC | AA | CC | Alkaline medium |
| --- | --- | --- | --- | --- | --- |
| 1BHCl | YES | X | X | X | X |
| 2BHCl | YES | X | X | X | X |
| 3BHCl | YES | X | X | X | X |
| 1BAC | YES | YES | X | X | X |
| 2BAC | YES | YES | YES | X | X |
| 3BAC | YES | YES | X | X | X |
| 1BAA | YES | YES | YES | X | X |
| 2BAA | YES | YES | YES | X | X |
| 3BAA | YES | YES | YES | X | X |

Table S3 Yield and quantity of each acid used for the resuspension of 10 mL of ZnP synthesis solution in a basic medium. The quantity is in drops. A= acid, B= alkaline, HCl= hydrochloric acid, citric acid= AC, ascorbic acid= AA, and CC= Cocobetaine

| Name | HCl | AC | AA | CC | Yield (%) |
| --- | --- | --- | --- | --- | --- |
| 1BHCl | 15 | - | - | 1% | 53.9083 |
| 2BHCl | 20 | - | - | 0.5% | 57.6405 |
| 3BHCl | 20 | - | - | 0.1% | 78.3744 |
| 1BAC | 25 | 12 | - | 1% | 66.7634 |
| 2BAC | 20 | - | - | 0.5% | 52.2496 |
| 3BAC | 8 | - | - | 0.1% | 62.2019 |
| 1BAA | - | - | 60 | 1% | 50.1762 |
| 2BAA | - | - | 60 | 0.5% | 41.0533 |
| 3BAA | - | - | 40 | 0.1% | 2.9028 |

Table S4 DLS response for the presence of MCPs and NPs upon resuspension. + Positive result, - Negative result. HCl = hydrochloric acid, citric acid = AC, ascorbic acid = AA, and CC = Cocobetaine

| C | Acid medium |  |  | Alkaline medium |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| CC | 1% | 0.5% | 0.1% | 1% | 0.5% | 0.1% |
| AC | - | - | + | + | - | + |
| HCl | + | - | - | - | + | - |
| AA | + | + | - | + | - | - |

Fig. S1 Analysis of the chemical composition by EDS of ZnP in alkaline medium

Fig. S2 Size distribution of MCPs obtained in acidic and alkaline media using ascorbic acid (AA). 1AA corresponds to 1% cocobetaine (CC), 2AA corresponds to 0.5% CC, and 1BAA is in alkaline media using 1% CC