B4-engine as the rotational driver of the B₁₃⁺ Cluster: Study based on BOMD and AdNDP analysis

Sourav Ranjan Ghosha,b , Sasthi Charan Haldera,cand Atish Dipankar Janaa,d,*

a Center for Research in Nanoscience and Crystal Engineering , Sibani Mandal Mahavidyalaya,

Namkhana, South 24 Parganas, 743357, India

b Department of Physics, Heritage Institute of Technology, Kolkata, 700107, India

cDepartment of Physics, Behala College, Parnasree, Kolkata, 700060, India

dInstitute of Astronomy Space and Earth Science, P-177, CIT Road, Scheme 7m, Ultadanga Station,

Kolkata, 700054, India.

*E-mail: atishdipankarjana@yahoo.in

Supplementary Information

TOC for supplementary materials

Fig.S1.a) Snapshots from the BOMD simulation at different time frames for B4 GS cluster

b) time evolution of diagonal B(1)-B(3) atom distance

c) time evolution of diagonal B(2)-B(4) atom distance

Fig.S2.Time evolution of two corner distances for B4GS cluster at 300K

Fig.S3. Canonical Molecular Orbital (CMO) of B4 TS and GS cluster

Fig.S4. Energy levels of LUMO and HOMO to HOMO -5 for the B4TS and GS

configuration

Fig. S5. AdNDP orbital of B13+ GS forming its square (S) and diamond (D1 and D2) motifs

Table S1.Optimized bond length of the B13+ TS and GS cluster

Table S2.Occupation Number and energy of the AdNDP Orbitals

Table S3.NAO composition of the AdNDP 2c-2e Orbitals

Table S4. NAO composition of the AdNDP 4c-2e Orbitals

Fig.S1.a)Snapshots from the BOMD simulation at different time frames for B4 GS cluster

b)time evolution of diagonal B(1)-B(3) distance

c) time evolution of diagonal B(2)-B(4)distance

Fig.S2.Time evolution of two corner distancesfor B4GS in comparison with optimized corner distance for GS (i), with their difference and TS (ii) corner distance

Fig. S3. Canonical Molecular Orbital (CMO) of B4 TS and GS cluster

Fig.S4. Energy levels of LUMO and HOMO to HOMO-5 for the B4 TS and GS

Fig. S5. AdNDP orbital in the forming of B13+ GS square (S) and diamond (D1 and D2) units

Table S1. Optimized bond length of the B13+ TS and GS cluster

| Bond | Bond length in Å |  |
| --- | --- | --- |
|  | B13+(TS) | B13+(GS) |
| B(1)-B(2) | 1.757 | 1.790 |
| B(1)-B(3) | 1.757 | 1.712 |
| B(1)-B(4) | 1.696 | 1.689 |
| B(1)-B(5) | 1.792 | 1.827 |
| B(1)-B(13) | 1.792 | 1.742 |
| B(2)-B(3) | 1.696 | 1.712 |
| B(2)-B(6) | 1.819 | 1.827 |
| B(2)-B(7) | 1.676 | 1.689 |
| B(2)-B(8) | 1.702 | 1.742 |
| B(2)-B(9) | 1.855 | 1.951 |
| B(3)-B(9) | 1.855 | 1.814 |
| B(3)-B(10) | 1.702 | 1.678 |
| B(3)-B(11) | 1.676 | 1.678 |
| B(3)-B(12) | 1.819 | 1.814 |
| B(4)-B(5) | 1.537 | 1.547 |
| B(4)-B(13) | 1.537 | 1.536 |
| B(5)-B(6) | 1.585 | 1.587 |
| B(6)-B(7) | 1.570 | 1.547 |
| B(7)-B(8) | 1.539 | 1.536 |
| B(8)-B(9) | 1.594 | 1.588 |
| B(9)-B(10) | 1.591 | 1.594 |
| B(10)-B(11) | 1.540 | 1.539 |
| B(11)-B(12) | 1.591 | 1.570 |
| B(12)-B(13) | 1.588 | 1.585 |

Table S2. Occupation Number and energy of the AdNDP Orbitals

| AdNDP Orbital No. | Occupation No. |  | Energy (eV) |  |
| --- | --- | --- | --- | --- |
|  | TS | GS | TS | GS |
| 1 | 1.9971 | 1.9800 | -13.1727 | -12.9292 |
| 2 | 1.9971 | 1.9800 | -13.1727 | -12.9292 |
| 3 | 1.9971 | 1.9800 | -13.1727 | -12.9292 |
| 4 | 1.9971 | 1.9800 | -13.1727 | -12.9292 |
| 5 | 2.0000 | 2.0000 | -14.2369 | -14.5843 |
| 6 | 2.0000 | 2.0000 | -8.2919 | -8.3602 |

Table S3. NAO composition of the AdNDP 2c-2e Orbitals

| B4 TS Orbital | (i) | (ii) | (iii) | (iv) |
| --- | --- | --- | --- | --- |
| NAO terms to shells | B(1) 2s 25.872% B(1) 2px 23.704% B(2) 2s 25.872% B(2) 2py23.704% | B(2) 2s 25.872% B(2) 2py23.704% B(3) 2s 25.872% B(3) 2px23.704% | B(3) 2s 25.872% B(3) 2px 23.704% B(4) 2s 25.872% B(4) 2py23.704% | B(4) 2s 25.872% B(4) 2py23.704% B(1) 2s 25.872% B(1) 2px23.704% |
| NAO terms to atoms | B(1) 50.00% B(2) 50.00% | B(2) 50.00% B(3) 50.00% | B(3) 50.00% B(4) 50.00% | B(4) 50.00% B(1) 50.00% |
| B4 GS Orbital | (i) | (ii) | (iii) | (iv) |
| NAO terms to shells | B(1) 2s 21.861% B(1) 2px 27.320% B(1) 2py 1.000% B(2) 2s 27.776% B(2) 2py 21.796% | B(2) 2s 27.776% B(2) 2py 21.796% B(3) 2s 21.861% B(3) 2px 27.320% B(3) 2py 1.000% | B(3) 2s 21.861% B(3) 2px 27.320% B(3) 2py 1.000% B(4) 2s 27.776% B(4) 2py 21.796% | B(4) 2s 27.776% B(4) 2py 21.796% B(1) 2s 21.861% B(1) 2px 27.320% B(1) 2py 1.000% |
| NAO terms to atoms | B(1) 50.333% B(2) 49.667% | B(2) 49.667% B(3) 50.333% | B(3) 50.333% B(4) 49.667% | B(4) 49.667% B(1) 50.333% |

Table S4. NAO composition of the AdNDP 4c-2e Orbitals

| B4 TS |  |  | B4 GS |  |
| --- | --- | --- | --- | --- |
| Orbital | (v) | (vi) | (v) | (vi) |
| NAO terms to shells | B(1) 2py 24.170% B(2) 2px 24.170% B(3) 2py 24.170% B(4) 2px 24.170% | B(1) 2pz 24.846% B(2) 2pz 24.846 % B(3) 2pz 24.846 % B(4) 2pz 24.846 % | B(1) 2s 1.850% B(1) 2py 23.454% B(2) 2px 23.577% B(3) 2s 1.850% B(3) 2py 23.454% B(4) 2px 23.577% | B(1) 2pz 28.740% B(2) 2pz20.955% B(3) 2pz28.740% B(4) 2pz20.955% |
| NAO terms to atoms | B(1) 25.00% B(2) 25.00% B(3) 25.00% B(4) 25.00% | B(1) 25.00% B(2) 25.00% B(3) 25.00% B(4) 25.00% | B(1) 25.833% B(2) 24.167 % B(3) 25.833% B(4) 24.167 % | B(1) 28.945% B(2) 21.055% B(3) 28.945% B(4) 21.055% |