Supporting Information

Magnetic recyclable Cu/ZnFe2O4 for catalytic reduction of nitroarenes and C-N bond formation reactions

Ruike Zhang1, Tian Chen1, Gongshu Wang1, Yuqiu Guan1, Guiyang Yan2* Zhangpei Chen,1* and Jianshe Hu1

1Center for Molecular Science and Engineering, College of Sciences, Northeastern University, Shenyang 110819, P. R. China

2Fujian Province University Key Laboratory of Green Energy and Environment Catalysis, Fujian Provincial Key Laboratory of Featured Biochemical and Chemical Materials, Ningde Normal University, Ningde, Fujian 352100, P. R. China

E-mail: chenzhangpei@mail.neu.edu.cn; ygyfjnu@163.com

Table of Contents

1. General information	2

2. Cu/ZnFe2O4 catalyzed reduction of nitroarenes	2

3. Cu/ZnFe2O4 catalyzed C-N bond forming reactions	3

4. References	6

5. Spectral data for representative compounds	6

1. General information

All reagents and solvents used in this work were obtained from commercial sources and were used without further purification. Thin-layer chromatography (TLC) was performed on silica gel GF254 (0.25 mm thickness) plates and visualized under UV light. Organic solutions were concentrated under reduced pressure at 40 °C (water bath temperature) using a Büchi rotary evaporator, unless otherwise noted. Column chromatography was performed on silica gel (200-300 mesh). 1H, 13C and 19F NMR spectra were recorded with Bruker Avance III HD 400 MHz or 600 MHz spectrometers. NMR spectra are reported as follows: chemical shift, multiplicity (s = singlet, d = doublet, t = triplet, q = quarter, m = multiplet, br = broad), coupling (J) constant and integration. The morphology of all samples was determined with scanning electronmicroscopy (SEM, JEOL 6500F) and transmission electron microscopy (TEM, JEM-2000EX). The absorption wavelength was measured using a UV-Vis spectrophotometer (TU-1901, Beijing Purkinje General Instrument Co., Ltd. China). Other instruments are listed as follows: TGA was performed with a Diamond instrument, FT-IR spectra were measured with samples pressed into KBr pellets on a PerkinElmer spectrum One (B) spectrometer, X-ray diffraction (XRD) patterns of samples were detected by a Rigaku DX-2500 X-ray diffractometer.

2. Cu/ZnFe2O4 catalyzed reduction of nitroarenes

Table 1. Catalytic reduction of nitroarenes with Cu/ZnFe2O4 under optimized conditions.

| Entrya | Product | Yield (%)b |
| --- | --- | --- |
| 1 |  | 98 |
| 2 |  | 98 |
| 3 |  | 98 |
| 4 |  | 97 |
| 5 |  | 98 |
| 6 |  | 98 |
| 7 |  | 98 |
| 8 |  | 97 |
| 9 |  | 98 |
| aReaction conditions : nitrobenzene 1 mmol; Sodium borohydride 2 mmol; solvent 3 mL; Cu/ZnFe2O4 100 mg; ambient temperature. bIsolated yield. |  |  |

A mixture of Cu-ZnFe2O4 (100 mg, 4.8 mol%) and nitrobenzene (0.1231 g, 1.0 mmol) was added to a round-bottom flask.H2O (3.0 mL) was added with a syringe, followed by NaBH4 (0.0757 g, 2.0 mmol). The reaction mixture was reacted at 25 oC for 1 h. After the reaction, the organic phase was extracted with ethyl acetate, dried on anhydrous sodium sulfate, and concentrated by rotary evaporation. The crude product was purified by column chromatography (petroleum ether: ethyl acetate = 1:1) to obtain 0.0913 g with 98% yield.

3. Cu/ZnFe2O4 catalyzed C-N bond forming reactions

phenyl-1H-imidazole (3a): known compound1a, 135.6 mg, 94% yield, colorless oil, Rf = 0.3 (PE: EA = 1:2); 1H NMR (400 MHz, Chloroform-d) δ 7.84 (s, 1H), 7.48 – 7.41 (m, 2H), 7.35 (d, J = 8.4 Hz, 3H), 7.27 (s, 1H), 7.20 (s, 1H);13C NMR (101 MHz, Chloroform-d) δ 137.3, 130.4, 129.8, 127.4, 121.4, 118.2.

- (o-tolyl)-1H-imidazole (3b): known compound1b, 140.5 mg, 88% yield, colorless oil, Rf = 0.25 (PE: EA = 2:1); 1H NMR (400 MHz, Chloroform-d) δ 7.57 (s, 1H), 7.31 (d, J = 1.2 Hz, 3H), 7.19 (d, J = 8.2 Hz, 2H), 7.03 (s, 1H), 2.15 (s, 3H);13C NMR (101 MHz, Chloroform-d) δ 137.5, 136.6, 133.8, 131.3, 129.2, 128.8, 126.9, 126.5, 120.5, 17.6.

(m-tolyl)-1H-imidazole (3c): known compound1c, 144.0 mg, 91% yield, colorless oil, Rf = 0.25 (PE: EA = 2:1); 1H NMR (400 MHz, Chloroform-d) δ 7.83 (s, 1H), 7.34 (s, 1H), 7.26 (t, J = 1.3 Hz, 1H), 7.19 (s, 4H), 2.42 (s, 3H);13C NMR (101 MHz, Chloroform-d) δ 140.0, 137.3, 135.6, 130.3, 129.7, 128.2, 122.1, 118.6, 118.3, 21.4.

1-(p-tolyl)-1H-imidazole (3d): known compound1a, 139.2 mg, 88% yield, yellow solid, Rf = 0.25 (PE: EA = 1:1);1H NMR (400 MHz, Chloroform-d) δ 7.82 (s, 1H), 7.25 (d, J = 7.0 Hz, 5H), 7.19 (s, 1H), 2.39 (s, 6H);13C NMR (101 MHz, Chloroform-d) δ 137.5, 135.6, 134.9, 130.4, 130.1, 121.4, 118.3, 20.9.

1-(4-methoxyphenyl)-1H-imidazole (3e): known compound1b, 151.4 mg, 87% yield, yellow solid, Rf = 0.20 (PE: EA = 5:1);1H NMR (400 MHz, Chloroform-d) δ 7.76 (s, 1H), 7.32 – 7.24 (m, 2H), 7.20 (s, 2H), 7.01 – 6.93 (m, 2H), 3.83 (s, 3H).

13C NMR (101 MHz, chloroform-d) δ 158.9, 135.9, 130.7, 130.1, 123.1, 118.8, 114.9, 55.6.

1-(4-bromophenyl)-1H-imidazole (3f): known compound1a, 196.3 mg, 88% yield, pale yellow solid, Rf = 0.25 (PE: EA = 1:1); 1H NMR (600 MHz, Chloroform-d) δ 7.84 (s, 2H), 7.63 – 7.58 (m, 4H), 7.30 – 7.24 (m, 6H), 2.51 (s, 0H); 13C NMR (151 MHz, chloroform-d) δ 136.4, 135.5, 133.0, 130.8, 123.0, 120.9, 118.1.

1-(4-nitrophenyl)-1H-imidazole (3g): known compound1a, 168.4 mg, 89% yield, pale yellow solid, Rf = 0.25 (PE: EA = 5:1); 1H NMR (400 MHz, Chloroform-d) δ 8.43 – 8.34 (m, 2H), 8.00 (s, 1H), 7.64 – 7.56 (m, 2H), 7.40 (d, J = 1.6 Hz, 1H); 13C NMR (101 MHz, chloroform-d) δ 146.2, 142.0, 135.4, 131.8, 125.8, 121.1, 117.7.

4-(1H-imidazol-1-yl)benzonitrile (3h): known compound1b, 143.5 mg, 85% yield, white solid, Rf = 0.10 (PE: EA = 1:1);1H NMR (400 MHz, Chloroform-d) δ 7.97 (s, 1H), 7.86 – 7.79 (m, 2H), 7.59 – 7.51 (m, 2H), 7.36 (s, 1H);13C NMR (101 MHz, Chloroform-d) δ 140.5, 135.3, 134.2, 131.6, 121.4, 117.9, 117.6, 111.1.

(4-(trifluoromethyl)phenyl)-1H-imidazole (3i): known compound1b, 176.3 mg, 83% yield, white solid, Rf = 0.20 (PE: EA = 2:1);1H NMR (400 MHz, Chloroform-d) δ 7.92 (s, 2H), 7.74 (d, J = 8.2 Hz, 4H), 7.51 (d, J = 8.3 Hz, 5H), 7.33 (s, 3H), 6.33 (s, 1H);13C NMR (101 MHz, Chloroform-d) δ 140.0, 131.17, 129.65, 129.32, 127.29, 127.25, 127.22, 127.18, 122.26, 121.26. 19F NMR (376 MHz, Chloroform-d) δ -62.54.

2-methyl-1-phenyl-1H-imidazole (3j): known compound2, 136.1 mg, 86% yield, colorless oil, Rf = 0.15 (PE: EA = 1:2);1H NMR (400 MHz, Chloroform-d) δ 7.48 – 7.38 (m, 1H), 7.42 – 7.32 (m, 0H), 7.28 – 7.19 (m, 1H), 7.02 – 6.92 (m, 1H), 2.31 (s, 1H); 13C NMR (101 MHz, chloroform-d) δ 144.6, 138.0, 129.4, 128.1, 127.7, 125.5, 120.6, 13.8.

1-phenyl-1H-benzo[d]imidazole (3k): known compound1a, 155.4 mg, 80% yield, colorless oil, Rf = 0.40 (PE: EA = 1:1);1H NMR (400 MHz, Chloroform-d) δ 8.10 (s, 1H), 7.93 – 7.84 (m, 1H), 7.60 – 7.45 (m, 5H), 7.49 – 7.40 (m, 1H), 7.38 – 7.27 (m, 2H); 13C NMR (101 MHz, chloroform-d) δ 144.0, 142.3, 136.4, 133.7, 130.1, 128.1, 124.1, 123.7, 122.8, 120.6, 110.5.

5-nitro-1-phenyl-1H-benzo[d]imidazole (3l): known compound3, 200.9 mg, 84% yield, colorless oil, Rf = 0.25 (PE: EA = 1:1); 1H NMR (400 MHz, Chloroform-d) δ 8.80 (d, J = 2.1 Hz, 1H), 8.32 – 8.24 (m, 2H), 7.71 – 7.60 (m, 2H), 7.64 – 7.49 (m, 4H); 13C NMR (101 MHz, chloroform-d) δ 145.7, 144.1, 135.3, 130.5, 130.4, 129.2, 124.3, 119.5, 118.6, 117.4, 110.6.

1-phenyl-1H-pyrrole (3m): known compound4, 134.3 mg, 94% yield, white solid, Rf = 0.45 (PE: EA = 20:1); 1H NMR (400 MHz, Chloroform-d) δ 7.59 – 7.46 (m, 4H), 7.35 (tt, J = 7.0, 2.2 Hz, 1H), 7.25 – 7.19 (m, 2H), 6.49 (t, J = 2.3 Hz, 2H); 13C NMR (101 MHz, chloroform-d) δ 140.9, 129.7, 125.7, 120.6, 119.4, 110.6.

1-phenyl-1H-pyrazole (3n): known compound2, 134.2 mg, 94% yield, colorless oil, Rf = 0.50 (PE: EA = 2:1); 1H NMR (400 MHz, Chloroform-d) δ 7.92 (dd, J = 2.5, 0.7 Hz, 1H), 7.76 (d, J = 1.9 Hz, 1H), 7.75 – 7.68 (m, 2H), 7.49 – 7.40 (m, 2H), 7.33 – 7.24 (m, 1H), 6.46 (dd, J = 2.5, 1.8 Hz, 1H); 13C NMR (101 MHz, chloroform-d) δ 141.1, 140.2, 129.5, 126.8, 126.5, 119.2, 107.7.

- phenyl-1H-benzo[d][1,2,3]triazole (3o): known compound5, 146.4 mg, 75% yield, pale yellow solid, Rf = 0.45 (PE:EA = 3:1); 1H NMR (400 MHz, Chloroform-d) δ 8.17 (dt, J = 8.4, 1.0 Hz, 1H), 7.85 – 7.79 (m, 1H), 7.83 – 7.74 (m, 2H), 7.69 – 7.60 (m, 2H), 7.64 – 7.49 (m, 2H), 7.46 (ddd, J = 8.1, 6.9, 1.0 Hz, 1H); 13C NMR (101 MHz, chloroform-d) δ 146.5, 137.0, 132.3, 129.9, 128.7, 128.3, 124.4, 122.9, 120.4, 110.4.

Diphenylamine (3p): known compound4, 130.3 mg, 77% yield, yellow solid, Rf = 0.25 (PE: EA = 50:1);1H NMR (400 MHz, Chloroform-d) δ 7.29 – 7.20 (m, 4H), 7.07 – 7.00 (m, 4H), 6.91 (tt, J = 7.3, 1.2 Hz, 2H), 5.63 (s, 1H); 13C NMR (101 MHz, chloroform-d) δ 143.2, 129.4, 121.1, 117.9.

2,6-dimethyl-N-phenylaniline (3q): known compound6, 128.3 mg, 65% yield, yellow solid, Rf = 0.40 (PE: EA = 10:1); 1H NMR (400 MHz, Chloroform-d) δ 7.29 – 7.02 (m, 5H), 6.73 (ddd, J = 8.4, 6.7, 1.0 Hz, 1H), 6.52 – 6.45 (m, 2H), 5.14 (s, 1H), 2.20 (s, 6H); 13C NMR (101 MHz, chloroform-d) δ 146.4, 138.3, 136.0, 129.3, 128.6, 125.8, 118.2, 113.6, 18.4.

1-phenylpiperidine (3r): known compound2, 148.4 mg, 92% yield, colorless oil, Rf = 0.25 (PE:EA = 15:1);1H NMR (400 MHz, Chloroform-d) δ 7.40 (dtd, J = 10.3, 7.4, 2.3 Hz, 2H), 7.10 (d, J = 8.4 Hz, 2H), 6.97 (dt, J = 10.3, 7.1 Hz, 1H), 3.29 (dt, J = 9.1, 5.2 Hz, 4H), 1.91 – 1.79 (m, 4H), 1.72 (pd, J = 6.0, 3.2 Hz, 2H); 13C NMR (101 MHz, chloroform-d) δ 152.4, 129.2, 119.3, 116.7, 50.8, 26.1, 24.5.

4-phenylmorpholine (3s): known compound2, 143.6 mg, 88% yield, pale yellow solid, Rf = 0.40 (PE: EA = 30:1);1H NMR (400 MHz, Chloroform-d) δ 7.33 (tq, J = 7.0, 2.0 Hz, 2H), 6.96 (td, J = 8.7, 3.6 Hz, 3H), 3.94 – 3.87 (m, 4H), 3.20 (dq, J = 4.9, 2.0 Hz, 4H); 13C NMR (101 MHz, chloroform-d) δ 151.3, 129.2, 120.1, 115.8, 67.0, 49.4.

1-(4-nitrophenyl)-4-phenylpiperazine (3t): known compound7, 170.1 mg, 60% yield, yellow solid, Rf = 0.45 (PE: EA = 5:1); 1H NMR (400 MHz, Chloroform-d) δ 8.19 – 8.11 (m, 1H), 7.35 – 7.26 (m, 1H), 7.01 – 6.83 (m, 3H), 3.63 – 3.56 (m, 2H), 3.39 – 3.32 (m, 2H); 13C NMR (101 MHz, chloroform-d) δ 154.7, 150.7, 138.7, 129.4, 126.0, 120.5, 116.3, 112.8, 48.9, 47.1.

4. References

1. a) H. Yang, C. Xi, Z. Miao, R. Chen, Eur, Cross-Coupling Reactions of Aryl Halides with Amines, Phenols, and Thiols Catalyzed by an N,N′-Dioxide–Copper(I) Catalytic System, J. Org. Chem. 2011, 3353-3360 (2011). https://doi.org/10.1002/ejoc.201100274; b) N Devarajan, P Suresh, Framework‐Copper‐Catalyzed C−N Cross‐Coupling of Arylboronic Acids with Imidazole: Convenient and Ligand‐Free Synthesis of N‐Arylimidazoles, Chem Cat Chem. 8, 2953 –2960 (2016). https://doi.org/10.1002/cctc.201600480; c) H Li, W Zhao, H Li, Z Xu, W Wang, J Lang, [Cu30I16(mtpmt)12(μ10-S4)]: an unusual 30-membered copper(i) cluster derived from the C–S bond cleavage and its use in heterogeneous catalysis, Chem. Commun. 49, 4259-4261 (2013). https://doi.org/10.1039/C2CC36736J

2. S Rina, S Suman, C Gargi, D Siuli, P Nicolaas, D Nanda, C−N Cross-Coupling Reactions Under Mild Conditions Using Singlet Di-Radical Nickel(II)-Complexes as Catalyst: N-Arylation and Quinazoline Synthesis, Adv. Synth. Catal. 361, 4342-4353 (2019).

https://doi.org/10.1002/adsc.201900545

3. C Zhu, E Gras, C Duhayon, F Lacassin, X Cui, R Chauvin, The Forgotten Nitroaromatic Phosphines as Weakly Donating P-ligands: An N-Aryl-benzimidazolyl Series in RhCl(CO) Complexes, Chem Asian J. 12, 2845-2856 (2017). https://doi.org/10.1002/asia.201701078

4. Z. Ding, N. Nie, T. Chen, L. Meng, G. Wang, Z. Chen, J. Hu, l-Proline N-oxide dihydrazides as an efficient ligand for cross-coupling reactions of aryl iodides and bromides with amines and phenols, Tetrahedron Lett. 79, 131826 (2021). https://doi.org/10.1016/j.tet.2020.131826

5. X Jia, P Peng, N-(4-Thiazolylmethyl)Morpholine N-Oxide as N,O-Bidentate Ligand for Copper-Catalyzed Ullmann-Type N-Arylation of Azoles/Amines with Aryl Halides, Asian J. Org. Chem. 8, 1548-1554 (2019). https://doi.org/10.1002/ajoc.201900273

6. M Topchiy, P Dzhevakov, M Rubina, O Morozov, A Asachenko, M Nechaev, Solvent-Free Buchwald–Hartwig (Hetero)arylation of Anilines, Diarylamines, and Dialkylamines Mediated by Expanded-Ring N-Heterocyclic Carbene Palladium Complexes, Eur. J. Org. Chem. 2016, 1908-1914 (2016). https://doi.org/10.1002/ejoc.201501616

7. C Yang, F Zhang, G Deng, H Gong, Amination of Aromatic Halides and Exploration of the Reactivity Sequence of Aromatic Halides, J. Org. Chem. 84, 181-190 (2019). https://doi.org/10.1021/acs.joc.8b02588

5. Spectral data for representative compounds