Supplemental Information for “Magnesium sub-silicates in exoplanetary interiors”

Yanlei Geng1,2, Fangfei Li1*, Ho-kwang Mao2, Qingyang Hu1,2*

1. Synergetic Extreme Condition High-Pressure Science Center, State Key Laboratory of High Pressure and Superhard Materials, College of Physics, Jilin University, Changchun, 130012, China

2. Center for High Pressure Science and Technology Advanced Research, Beijing, 100193, China

Fig. S1 The crystal structures of the stable Mg-Si-O compounds at high pressure. (A), P4/mmm phase for Mg3SiO3, (B), P4/nmm phase for Mg4SiO3, (C), P4/mmm phase for Mg5SiO3, (D), I4mm phase for Mg6SiO3, (E), Pmm2 phase for Mg5SiO4, (F), P42/mnm phase for Mg4Si2O5.

Fig. S2 The phonon spectrum at the corresponding pressure. (A), Cmmm phase for Mg2SiO3 at 1000 GPa, (B), Cmmm phase for Mg4SiO3 at 1500 GPa, (C), P4/mmm phase for Mg3SiO3 at 300 GPa, (D), P4/nmm phase for Mg4SiO3 at 300 GPa, (E), P4/mmm phase for Mg5SiO3 at 1000 GPa, (F), I4mm phase for Mg6SiO3 at 300 GPa, (G), Cmmm phase for Mg3SiO4 at 1000 GPa, (H), Pmm2 phase for Mg5SiO4 at 1000 GPa, (I), P42/mnm phase for Mg4Si2O5 at 800 GPa.

Fig. S3 The density of several sub-Mg-silicates as a function of pressure.

Fig. S4 Pressure-dependent relative enthalpies of Mg2SiO3 and its aggregation of possible dissociation products. Mg2SiO3 is more stable than combinations such as MgSi2O5 + Mg5SiO4 and Mg4Si2O5 + Mg2SiO4 above 400 GPa.

Fig. S5 Bader charge of Si as a function of pressure in MgSiO3 (PPv phase), Mg2SiO3 (Cmmm phase), Mg3SiO4 (Cmmm phase), and Mg4SiO3 (Cmmm phase).

Fig. S6 Free energy calculation as a function of pressure. (A), Formation Gibbs free energy (ΔG) of Mg2SiO3 (Cmmm phase) relative to MgSiO3 and Mg at 10000 K. (B), Formation Gibbs free energy (ΔG) of Mg4SiO3 (Cmmm phase) relative to MgSiO3 and Mg at 10000 K. (C), Formation Gibbs free energy (ΔG) of Mg3SiO4 (Cmmm phase) relative to Mg2SiO4 and Mg at 10000 K.

Fig. S7 Generalized average conductivity curve of silicate mantle, sub-silicate mantle and conductive mantle.

Fig. S8 Relationship between thickness of conductive mantle layer and Mg4SiO3 fraction in CMB layer. The curves correspond to the angular frequencies (ω) of the time-varying magnetic field at 10−8 rad/s, 10−7 rad/s, and 10−6 rad/s, respectively, and illustrate the conditions for achieving > 95% magnetic shielding efficiency.

Fig. S9 Plot of thickness as a function of super-Earth mass (M/M⊕), for sub-silicate mantle (purple dots) and conductive mantle layer (orange dots), respectively.

Fig. S10 Generalized average conductivity curve of Mg2SiO3 (Cmmm phase), Mg3SiO4 (Cmmm phase), and Mg4SiO3 (Cmmm phase) with temperature varying from 1000 K to 7000 K under a pressure of 1000 GPa.

Table

Table S1 The parameters of predicted structures.

| Space group | Pressure (GPa) | Lattice parameter (Å) |  | Atom site |  | Wyckoff position |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mg2SiO3 (Cmmm) | 1000 | a=2.8067 b=8.2251 c=1.9299 | α=90.00 β=90.00 γ=90.00 | Mg Si O1 O2 | 4i 2d 4j 2c | 0.0000 0.0000 0.0000 0.5000 | 0.3399 0.0000 0.1768 0.0000 | 0.0000 0.5000 0.5000 0.5000 |
| Mg3SiO3 (P4/mmm) | 300 | a=2.4550 b=2.4550 c=6.5844 | α=90.00 β=90.00 γ=90.00 | Mg1 Mg2 Si O1 O2 | 2h 1b 1a 2g 1d | 0.5000 0.0000 0.0000 0.0000 0.5000 | 0.5000 0.0000 0.0000 0.0000 0.5000 | 0.2164 0.5000 0.0000 0.2455 0.5000 |
| Mg4SiO3 (P4/nmm) | 300 | a=2.4593 b=2.4593 c=15.6632 | α=90.00 β=90.00 γ=90.00 | Mg1 Mg2 Mg3 Mg4 Si O1 O2 | 2c 2c 2c 2c 2c 2c 2c | 0.0000 0.0000 0.5000 0.5000 0.5000 0.5000 0.5000 | 0.5000 0.5000 0.0000 0.0000 0.0000 0.0000 0.0000 | 0.2280 0.4458 0.3281 0.9362 0.1547 0.0485 0.6642 |
| Mg4SiO3 (Cmmm) | 1500 | a=6.6533 b=4.4014 c=1.8366 | α=90.00 β=90.00 γ=90.00 | Mg Si O1 O2 | 8p 2d 4h 2c | 0.1371 0.0000 0.2201 0.0000 | 0.2934 0.0000 0.0000 0.5000 | 0.0000 0.5000 0.5000 0.5000 |
| Mg5SiO3 (P4/mmm) | 500 | a=2.3293 b=2.3293 c=8.7693 | α=90.00 β=90.00 γ=90.00 | Mg1 Mg2 Mg3 Si O1 O2 | 2g 1b 2h 1c 2g 1d | 0.0000 0.0000 0.5000 0.5000 0.0000 0.5000 | 0.0000 0.0000 0.5000 0.5000 0.0000 0.5000 | 0.8686 0.5000 0.3009 0.0000 0.3148 0.5000 |
| Mg6SiO3 (I4mm) | 300 | a=2.4427 b=2.4427 c=21.2432 | α=90.00 β=90.00 γ=90.00 | Mg1 Mg2 Mg3 Mg4 Mg5 Mg6 Si O1 O2 O3 | 2a 2a 2a 2a 2a 2a 2a 2a 2a 2a | 0.5000 0.5000 0.5000 0.0000 0.0000 0.0000 0.0000 0.5000 0.5000 0.0000 | 0.5000 0.5000 0.5000 0.0000 0.0000 0.0000 0.0000 0.5000 0.5000 0.0000 | 0.1365 0.9762 0.8580 0.7969 0.0513 0.2221 0.9182 0.2169 0.0556 0.1363 |
| Mg3SiO4 (Cmmm) | 1000 | a=3.9044 b=7.7477 c=1.9415 | α=90.00 β=90.00 γ=90.00 | Mg1 Mg2 Si O | 4j 2c 2a 8p | 0.5000 0.5000 0.0000 0.7316 | 0.2624 0.0000 0.0000 0.1309 | 0.5000 0.5000 0.0000 0.0000 |
| Mg5SiO4 (Pmm2) | 1000 | a=2.6696 b=1.9164 c=7.5720 | α=90.00 β=90.00 γ=90.00 | Mg1 Mg2 Mg3 Mg4 Mg5 Si O1 O2 O3 O4 | 1a 1a 1a 1c 1c 1d 1d 1d 1b 1b | 0.0000 0.0000 0.0000 0.5000 0.5000 0.5000 0.5000 0.5000 0.0000 0.0000 | 0.0000 0.0000 0.0000 0.0000 0.0000 0.5000 0.5000 0.5000 0.5000 0.5000 | 0.2674 0.6156 0.9895 0.7891 0.4232 0.1534 0.6083 0.9640 0.4354 0.7973 |
| Mg4Si2O5 (P42/mnm) | 800 | a=3.2468 b=3.2468 c=8.7027 | α=90.00 β=90.00 γ=90.00 | Mg1 Si1 O1 O2 | 8j 4g 8j 2b | 0.7309 0.8000 0.2709 0.0000 | 0.7309 0.2000 0.2709 0.0000 | 0.8556 0.0000 0.6738 0.5000 |