Fig. E1 Further details on the methanol synthesis mechanism.  a Methanol formation rates at 1 bar, 135 ℃ and at 20 bar, 260 ℃ (H2/CO2 = 4/1) as a function of the Cu surface area of the samples. b TOF for methanol synthesis with unsupported Cu and Cu/ZnO/Al2O3. H2/CO2 = 4/1, 20 bar. c Infrared spectra of Cu/ZnO/Al2O3 as a function of time on stream in CO/CO2/H2:0.33/10/40 at 135 °C and 2 bar. The coincident displacement of CO from Cu and emergence of adsorbed formate shows that formate is present on Cu during reaction. d Infrared spectra of Cu/ZnO/Al2O3 when switching from a CO2/H2 feed to a CO2/D2 feed. 135 °C, 1 bar, X/CO2 = 4/1 (X = H2 or D2). The results show that formates are converted in the methanol synthesis. e Comparison of TOFs at 135 ℃ for methanol synthesis and formaldehyde hydrogenation measured here to H2 and CO2 activation rates from the literature47. f Methanol synthesis rate vs hydrogen pressure (220 ℃ 40 bar, feed flow = 270 NmL/min, pCO2 = 1.2 bar, balance Ar, 3.83·106 NmL/gcat/h for Cu/ZnO/Al2O3 and 6.48·104 NmL/gcat/h for unsupported Cu). g Steady state methanol reaction rate (135 ℃, 1 bar, H2/CO2 = 3/1) on Cu/ZnO/Al2O3 catalyst as a function of time including the introduction of a pulse of formaldehyde (CH2O) into the feed.

Fig. E2 Mechanistic implications of the absence of H2/D2 effect in formic acid conversion. Illustration of how rate-limiting steps10,22,23 (RLS) via H2COO, H2COOH or COOH would depend on the presence of H2 or D2, whereas the direct formic acid dissociation does not. The absence of H2/D2 effect in formic acid conversion (Fig. 1d) is therefore most consistent with HCOOH dissociation as the rate-limiting step. The routes via H2COO and H2COOH add 3 protons before/during the rate-limiting step and are also ruled out by the 1. order hydrogen dependence in Fig. E1f.

Fig. E3 Further characterization of charge transfer effects. a O 1s XPS spectra for Cu/ZnO/Al2O3 after exposure to 1 bar, 175 ℃ and after subsequent heating in vacuum to 250 ℃. Dotted lines show deconvolutions into O and OH and their sum. b Cu 2p XPS spectra of Cu/ZnO/Al2O3 and unsupported Cu in 14 mbar H2 at 250 ℃. c H2 TPD spectra for different samples after pre-reduction and exposure to 1 bar H2 at 175 ℃. d Normalized IR absorbance from H/D-modifications of lattice vibrations (see inserted Cu/ZnO/Al2O3 spectra for location) during a switch from H2 to D2 at 1 bar and 135 ℃. e Hydrogen adsorption on pure ZnO as a function of time and the calculated stable adsorption configuration of two H on ZnO(1010). Zn: light blue, O: red, H: white. f Calculated structure of Cu54 on ZnO(1010) with H absorbed in the oxide below the Cu particle. The absorption is exothermic in the presence of Cu. Note how the Zn atoms above the H atom are shifted towards the Cu particle due to the attractive H+(ZnO)-e-(Cu) interaction created between the phases.  Cu: tan, Zn: light blue, O: red, H: white.

Fig. E4 Deconvolution of the infrared spectrum of CO on Pt/ZnO into the different sites. a DFT Calculated C-O stretch vibration frequencies CO adsorption on (red) a (111) microfacet, (black) a (111) microfacet close to the support, (green) and (orange) at the interface b Deconvolution of the measured IR spectrum into two groups of sites at the interface and two groups of sites on the wider Pt surface. Colours: Pt: dark blue, Zn: light blue, O: red, C: grey.

Fig. E5 The stability of high coverages at the Cu-ZnO interface. a The adsorption energy of formate on Cu(111) from calorimetry48 and DFT49 as well as interpolation by an isotherm model50 taking into account adsorbate interactions, compared to our calculated HCOO adsorption energies at the Cu-ZnO interface. Notice how high coverages are very stable at the Cu-ZnO interface. b Structure of adsorbed formate at a high coverage (HCOO:Cusurf = 0.4) right at the interface. Cu: tan, Zn: light blue, O: red, H: white. Notice from the transition and final states in the rate-limiting step in Fig. 4 how the dissociation products need to be shifted into bridge sites with no adjacent neighbours and notice how this is impossible at the highly covered interface.