Supplementary Information

In vivo activation of pH-responsive oxidase-like graphitic-nanozymes for selective killing of Helicobacter pylori

Lufeng Zhang1, Liang Zhang1, Hui Deng1, Huan Li2, Wentao Tang1, Luyao Guan1, Ye Qiu1, Michael J Donovan1, Zhuo Chen1 & Weihong Tan1,3

1Molecular Science and Biomedicine Laboratory, State Key Laboratory of Chemo/Bio-Sensing and Chemometrics, College of Chemistry and Chemical Engineering, College of Biology, Hunan Provincial Key Laboratory of Biomacromolecular Chemical Biology, Hunan University, Changsha, 410082, China

2Department of Gastroenterology, the Third Xiangya Hospital of Central South University, Changsha, 410013, China

3The Cancer Hospital of the University of Chinese Academy of Sciences, Institute of Basic Medicine and Cancer (IBMC), Chinese Academy of Sciences, Hangzhou, Zhejiang, 310022, China

These authors contributed equally: Lufeng Zhang, Liang Zhang.

*E-mail: zhuochen@hnu.edu.cn

Supplementary Figures

Supplementary Figure 1. TEM image of PtCo@G.

Supplementary Figure 2. UV-Vis absorbance of PtCo@G solution.

Supplementary Figure 3. (a) Hydrodynamic diameter and (b) Zeta potential of PtCo@G characterized by dynamic light scattering.

Supplementary Figure 4. Hydrodynamic diameter of PtCo@G in H2O, PBS (pH 1.0), and SGF after 12 h incubation.

Supplementary Figure 5. Time-dependent absorbance spectra of TMB catalyzed by PtCo@G.

Supplementary Figure 6. The oxidase-like activity of PtCo@G is dependent on pH and temperature. The data indicate the means and SD from three parallel experiments.

Supplementary Figure 7. Peroxidase-like activity of PtCo@G nanocrystals. (a) The UV-Vis absorbance spectra and visual color changes of TMB in different reaction systems: (1) PtCo@G, (2) TMB, (3) TMB+H2O2, (4) PtCo@G+TMB, and (5) PtCo@G+TMB+H2O2 in a pH 4.0 PBS buffer after 10 min incubation. (b) PtCo@G catalyzes oxidation of various peroxidase substrates in the presence of H2O2 to produce different color reactions. (1) TMB, (2) ABTS, (3) OPD. Insert images show corresponding visual color changes. (c) Time-dependent absorbance spectra of TMB catalyzed by PtCo@G in the presence of H2O2. Data are presented as means ± standard deviation (s.d.). Error bars were based on s.d. of three independent experiments.

Supplementary Figure 8. Peroxidase-like activity of PtCo@G nanocrystals. (a) and (b) show that the peroxidase-like activity of PtCo@G is dependent on pH and temperature. Data are presented as means ± s.d. Error bars were taken from three independent experiments.

Supplementary Figure 9. Oxidase-like activity of the PtCo@G nanocrystals in PBS (pH 1.0) buffer: (1) PtCo@G, (2) TMB, (3) PtCo@G+TMB. Insert images show corresponding visual color changes.

Supplementary Figure 10. (a) Fluorescence spectra of hydroethidine (HE) in different reaction systems: (1) PtCo@G+HE, (2) HE, (Excitation: 370 nm) (3) PtCo@G+HE, (4) HE, (5) PtCo@G (Excitation: 535 nm) in pH 1.0 PBS buffer after 30 min incubation. Insert shows the reaction of HE as a fluorescence probe for trapping the superoxide radical (O2•-). (b) Fluorescence spectra of hydroethidine (HE) before and after the addition of PtCo@G nanocrystals. (c) Histograms of FL intensity show the fluorescence product ethidium catalyzed by PtCo@G nanocrystals. P values were calculated by the Student’s t test: ****p < 0.0001. Data are presented as means ± s.d. Error bars were taken from three independent experiments.

Supplementary Figure 11. (a) The reaction between terephthalic acid (TA) and hydroxyl radical (•OH). The fluorescence product is 2-hydroxy terephthalic acid (TAOH). (b) Fluorescence spectra of the PBS (pH 1.0) solution include only TA; TA and PtCo@G; TA and H2O2; TA, PtCo@G and H2O2. (c) Histograms of ΔFL intensity show the fluorescence product, 2-hydroxy terephthalic acid (TAOH) catalyzed by PtCo@G nanocrystals. P values were calculated by the Student’s t test: ****p < 0.0001. Data are presented as means ± s.d. Error bars were taken from three independent experiments.

Supplementary Figure 12. (a) The reaction of DEPMPO trapping hydroxyl radical (•OH). (b) EPR spectra of DEPMPO-OH obtained by trapping •OH with the spin-trap agent DEPMPO in different reaction systems: (1) Fe2++H2O2, (2) Fe2++H2O2+DEPMPO, (3) PtCo@G+H2O2, (4) PtCo@G+H2O2+DEPMPO in pH 1.0 PBS buffer.

Supplementary Figure 13. 1H-NMR characterization of C18-PEGn-Benzeneboronic acid (CPB) with MQ 400 MHz.

Supplementary Figure 14. Raman spectra characterization of CPB functionalized PtCo@G.

Supplementary Figure 15. The oxidase-like property comparison of PtCo@G and PtCo@G@CPB in SGF: (1) TMB, (2) PtCo@G+TMB, (3) PtCo@G@CPB+TMB. Insert images show corresponding visual color changes.

Supplementary Figure 16. Characterization of H. pylori-infected mouse model. (a) Photographs of H. pylori colonies after gastric mucosa reculture. (b) Quantification of bacterial burden in the stomach of H. pylori-infected mouse. (c) The gram staining of a slice from the gastric mucosa of H. pylori-infected mouse. Slice thickness, 5 μm.

Supplementary Figure 17. Raman imaging and spectra of slice from the gastric mucosa. Scale bar: 20 μm, Slice thickness, 5 μm.

Supplementary Figure 18. (a) H&E staining of slice from the gastric mucosa after treatment with PBS, PtCo@G@CPB and OAC. Slice thickness, 5 μm. The inflammation score (b) and injury score (c) of gastric mucosa, according to the images of H&E staining.

Supplementary Figure 19. The distribution of PtCo@G@CPB in organs (72 h) after treatment (n=4).