Supplementary Materials for:

High-density inclined polar skyrmions with giant piezoelectricity

Xiang-Wei Guo1,†, Hui-Mei Li1,2,†, Yun-Long Tang1, Yin-Lian Zhu3,4, Xiu-Liang Ma3,5,6, Yu-Jia Wang1,2,*

1Shenyang National Laboratory for Materials Science, Institute of Metal Research, Chinese Academy of Sciences, Shenyang, 110016, China.

2School of Materials Science and Engineering, University of Science and Technology of China, Shenyang, 110016, China.

3Bay Area Center for Electron Microscopy, Songshan Lake Materials Laboratory, Dongguan, 523808, China.

4Hunan University of Science and Technology, Xiangtan, 411201, China.

5Institute of Physics, Chinese Academy of Sciences, Beijing, 100190, China.

6Quantum Science Center of Guangdong-HongKong-Macau Greater Bay Area (Guangdong), Shenzhen, 510290, China.

†These authors contributed equally: Xiang-Wei Guo, Hui-Mei Li

*Email: yjwang@imr.ac.cn.

This file includes:

Supplementary Fig. 1 to 4

Supplementary Note 1

Tables S1 and S2

Supplementary Figures:

Supplementary Fig. 1. Topological charge analysis of polar skyrmions under anisotropic epitaxial strain modulation in the PTO/STO superlattices. (a, d, g) Planar views of the topological charge distribution corresponding to polar skyrmions shown in Fig. 2(a, d, g) under εyy = -1.5%, -1.2%, and -0.9%, respectively, with a fixed εxx = -1.5%. (b, e, h) Enlarged planar views of the topological charge distribution for the three polar topological states in (a), (d), and (g) at the top surface of the PTO layer highlighted by black boxes, respectively. (c, f, i) Enlarged planar views of the topological charge distribution for the three polar topological states in (a), (d), and (g) at the bottom surface of the PTO layer highlighted by black boxes, respectively.

Supplementary Fig. 2. More typical polar topological states in the phase diagram. (a, d, g) Planar view of the ferroelectric polarization magnitude for three representative polar topological states: (a) a mixed state of polar skyrmions and vortex tubes under εxx = -1.5% and εyy =-1.9%; (d) a pure polar vortex tube state under εxx = -1.5% and εyy = -2.5%; (g) a mixed state of inclined skyrmions and vortex tubes under εxx = -2.0% and εyy = -1.0%. (b, e, h) Enlarged planar views of the polarization vector distributions for the three polar topological states highlighted by black boxes in (a), (d), and (g), respectively. (c, f, i) Corresponding enlarged cross-sectional views of the polarization vector distributions in the PTO/STO superlattices. The positions of the vortex cores are indicated by red and green dots.

Supplementary Fig. 3. Local piezoelectric response of polar skyrmions under different anisotropic epitaxial strains. (a-c) Planar distribution of the local piezoelectric coefficient d33 and polarization vectors for inclined skyrmions at the top, middle, and bottom of the PTO layer under εxx = -1.5% and εyy = -0.8%. (d-f) Corresponding results for a transitional state between upright and inclined skyrmions under εxx = -1.5% and εyy = -1.0%. (g-i) Corresponding results for upright skyrmions under εxx = -1.5% and εyy = -1.5%.

Supplementary Fig. 4. Schematic of geometric transformation from the (001)-oriented coordinate system (x', y', z') to the (111)-oriented coordinate system (x, y, z).

Supplementary Note 1. The expressions for the different energy density terms

The total free energy F of the entire system contains contributions from the bulk, gradient, elastic, and electrostatic energies:

F=fbulkT,Pi+fgrad(Pi,j)+felecEi,Pi+felasεij,PidV    (S1)

The first term is the bulk energy density:

fbulk=α1P12+P22+P32+α11P14+P24+α12P12P22+α13P12P32+P22P32+α14P12P2P3+α24P23P3+α33P34+α111P16+α222P26+α333P36+α112P14P22+α122P24P12+α113P14P32+P24P32+α133P34P12+P34P22+α123P12P22P32+α243P23P33+α143P12P2P33+α224P25P3+α124P12P23P3+α114P14P2P3          (S2)

where αi, αij, and αijk are the Landau expansion coefficients. Here, α1=α0T-Tc, with Tc being the Curie temperature.

The second term is the gradient energy density:

fgrad=12G11P1,12+P2,22+12G33P3,32+G12P1,1P2,2+G13P1,1P3,3+P2,2P3,3+G14P1,1P3,2+P1,1P2,3-P2,2P3,2-P2,2P2,3+P2,1P3,1+P3,1P1,2+P2,1P1,3+P1,2P1,3+12G44P2,3+P3,22+P3,1+P1,32+12G66P1,2+P2,12+12G44'P2,3-P3,22+P3,1-P1,32+P1,2-P2,12                     (S3)

where Gij is the gradient energy coefficients and Pi,j is the spatial differentiation of the polarization components.

The third term is the elastic energy density:

felas=12C11e112+e222+12C33e332+C12e11e22+C13e11e33+e22e33+2C44e232+e312+2C66e122+2C14e11e23+2C24e22e23+4C56e31e12        (S4)

where Cij denotes the elastic stiffness tensor, and eij is the elastic strain. The elastic strain is defined as the difference between the total strain εij and eigenstrain the εij0, i.e., eij=εij-εij0. The eigenstrain εij0 is associated with spontaneous polarizations through the electrostrictive coefficient Qij:

ε110=Q11P12+Q12P22+Q13P32+Q14P2P3

ε220=Q12P12+Q22P22+Q23P32+Q24P2P3

ε330=Q13P12+Q23P22+Q33P32

ε230=Q14P12+Q24P22+Q44P2P3

ε310=Q55P1P3+Q56P1P2

ε120=Q56P1P3+Q66P1P2                        (S5)

The last term is the electrostatic energy density:

felec=-12κ0κbEiEj-EiPi                    (S6)

where κ0 is the vacuum permittivity, κb is the background dielectric constant, and Ei is the ith component of the total electric field. The electric field is the sum of the applied electric field Eiapp and the depolarization field Eid.

It is assumed that the equilibrium of mechanical stress and electrical field is much faster than the relaxation of domain structures. Accordingly, the following mechanical and electrical equilibrium equations are solved for each polarization configuration to obtain the corresponding elastic and electrostatic driving forces:

σij,j=0                            (S7)

Di,i=0                            (S8)

Table S1. Relationships between energy coefficients in the global (x, y, z) and local (x', y', z') coordinate systems. A superscript “#” is used to indicate coefficients defined in the local system.

| Landau energy coefficients αi, αij, αijk | α1=α1#, α11=12α11#+14α12#, α33=13α11#+13α12#, |
| --- | --- |
|  | α12=α11#+12α12#, α13=2α11#, |
|  | α24=-223α11#+23α12#, α14=22α11#-2α12#, |
|  | α111=14α111#+14α112#, α222=1136α111#+736α112#+154α123#, |
|  | α333=19α111#+29α112#+127α123#, α112=54α111#+14α112#+16α123#, |
|  | α122=512α111#+1312α112#-19α123#, α113=52α111#+112α123#, |
|  | α133=53α111#+23α112#-19α123#, α123=5α111#+16α123#, |
|  | α243=-1029α111#+429α112#-227α123#, |
|  | α143=1023α111#-423α112#+29α123#, |
|  | α224=-526α111#+26α112#+218α123#, |
|  | α124=523α111#-23α112#-29α123#, |
|  | α114=522α111#-22α112#-26α123#. |
| Gradient energy coefficients Gij | G11=12G11#+12G12#+G44#, G33=13G11#+23G12#+43G44#, |
|  | G12=16G11#+56G12#-13G44#, G13=13G11#+23G12#-23G44#, |
|  | G44=13G11#-13G12#+13G44#, G66=16G11#-16G12#+23G44#, |
|  | G44'=G44'#, G14=26G11#-26G12#-23G44#. |
| Elastic stiffness coefficients Cij | C11=12C11#+12C12#+C44#, C33=13C11#+23C12#+43C44#, |
|  | C12=16C11#+56C12#-13C44#, C13=13C11#+23C12#-23C44#, |
|  | C44=13C11#-13C12#+13C44#, C66=16C11#-16C12#+23C44#, |
|  | C14=26C11#-26C12#-23C44#, C24=-C14, C56=C14. |
| Electrostrictive coefficients Qij | Q11=12Q11#+12Q12#+14Q44#, Q22=Q11, Q12=16Q11#+56Q12#-112Q44#, |
|  | Q13=13Q11#+23Q12#-16Q44#, Q23=Q13, Q14=23Q11#-23Q12#-26Q44#, Q24=-Q14, |
|  | Q33=13Q11#+23Q12#+13Q44#, Q44=43Q11#-43Q12#+13Q44#, |
|  | Q55=Q44, Q56=223Q11#-223Q12#+23Q44#, Q66=23Q11#-23Q12#+23Q44#. |

Table S2. Material parameters used for the PTO/STO superlattice in the local (x', y', z') coordinate system.

| Parameter (SI units) | PTO | STO |
| --- | --- | --- |
| α11# (C-2∙m2∙N) | −1.73×108 | 1.85×108 |
| α11# (C-4∙m6∙N) | −7.3×107 | 1.7×109 |
| α12# (C-4∙m6∙N) | 7.5×108 | 1.37×109 |
| α111# (C-6∙m10∙N) | 2.6×108 | 0 |
| α112# (C-6∙m10∙N) | 6.1×108 | 0 |
| α123# (C-6∙m10∙N) | −3.7×109 | 0 |
| Q11# (C-2∙m4) | 0.089 | 0.089 |
| Q12# (C-2∙m4) | −0.026 | −0.026 |
| Q44# (C-2∙m4) | 0.0675 | 0.0675 |
| C11# (m-2∙N) | 1.746×1011 | 1.746×1011 |
| C12# (m-2∙N) | 7.937×1010 | 7.937×1010 |
| C44# (m-2∙N) | 1.111×1011 | 1.111×1011 |
| G11# (C-2∙m4∙N) | 1.035×10-10 | 1.035×10-10 |
| G12# (C-2∙m4∙N) | −1.035×10-10 | −1.035×10-10 |
| G44# (C-2∙m4∙N) | 1.035×10-10 | 1.035×10-10 |
| G110# (C-2∙m4∙N) | 1.73×10-10 | 1.73×10-10 |
| κb | 40 | 40 |