SUPPLEMENTARY MATERIAL

AlN PEALD Development

The dose and exposure-saturation behavior of the binary PEALD AlN films were determined in real-time by in situ multi-wavelength ellipsometry. The modeled thickness and index of the evolving AlN film grown on untreated 150 mm Si (100) substrates at a 215 °C substrate temperature are shown in Fig. S1. Here, we define the TMA dose time as the length of time the ALD valve between the TMA ampoule and the chamber remained open. The exposure time is defined by the amount of time the TMA resided in the chamber, which was controlled by fully opening and closing a downstream throttle valve. For this investigation, the TMA and N2-H2 plasma purge times remained fixed at 30 and 10 s, respectively. These extended purge times ensured the complete removal of any remaining precursor and/or reaction byproducts during the purge steps.

Fig. S1.  AlN growth-per-cycle (GPC) vs. (a) TMA dose time, (b) TMA exposure time and (c) N2-H2 plasma dose time determined in situ for AlN PEALD on Si (100) at a 215 °C substrate temperature.

TMA dose and exposure saturation curves are presented in Fig. S1(a) and Fig. S1(b), respectively, where the N2-H2 plasma dose time remained constant at 20 s.  For the TMA dose saturation curve [Fig. S1(a)] does not include an exposure step.  As observed in Fig. S1(a), the GPC increases from ~0.8 Å/cycle to ~1.0 Å/cycle after increasing the TMA dose time significantly from 0.1–0.5 s. To reach full saturation, we implemented and systematically varied an exposure step with a fixed TMA dose time of 0.3 s, which is shown in Fig S1(b).  With the added exposure step, we observe a saturating GPC of ~1.1 Å/cycle between 3-6 s exposure time.  We note, however, that if we significantly increased the TMA dose (≥0.5 s) and exposure time (≥5 s) we observed a slight further increase of the GPC (GPC >~1.2 Å/cycle), which indicates some non-ideal behavior of the TMA at extremely large doses.  We intend to pursue this TMA behavior in future work.

The N2-H2 plasma dose saturation curve presented in Fig. S1(c) shows an increase in the GPC from 1.01 Å/cycle at 15 s plasma dose to 1.08 Å/cycle at 30 s plasma dose time.  TMA dose and exposure times remained fixed at 0.3 and 3 s, respectively. We performed ellipsometry measurements ex-situ across 150 mm Si substrates, which revealed only a small increase in the average GPC from 0.9–0.92 Å/cycle (<3%) from 10–30 s plasma dose time, respectively, where the AlN thickness nonuniformity (NU) remained below 1.6% (Fig. S2). The refractive index increased from 1.83 to 1.88 (<3%) over the same range of plasma dose times (Fig. S3). The corresponding index NU decreased from 1.1% to 0.5% at 10 s and 15 s plasma dose time, respectively, and remained unchanged as the dose time increased from 15 to 30 s.  Based on these results, we utilized a 15 s N2-H2 plasma dose for all subsequent Al(1-x)ScxN depositions. We also performed in-situ ellipsometry measurements to investigate TMA and N2-H2 plasma purge behavior, which demonstrated essentially no change in the AlN GPC down to 3 s TMA and N2-H2 plasma purge time (Fig. S4). Due to non-linear behavior during the initial stages of AlN growth on Si (100), the average GPC values determined ex situ (Fig. S2) are lower than the in-situ values (Fig. S4).

Fig. S2 AlN GPC and thickness NU versus N2-H2 plasma dose time determined ex-situ across 150 mm Si (100) substrates.

Fig. S3 AlN refractive index average and index NU versus N2-H2 plasma dose time determined ex-situ across 150 mm Si (100) substrates.

Fig. S4 GPC versus (a) TMA and (b) N2-H2 plasma purge times determined in-situ for AlN PEALD on Si (100) at 215°C substrate temperature.  TMA purge results show only a slight 1% increase in GPC with decreasing purge time from 20–3 s.  For the N2-H2 plasma purge data, the GPC remains constant over the full range of purge times investigated.

ClSc(EtCp)2 dose saturation behavior

We previously reported some anomalous behavior of the ClSc(EtCp)2 precursor after aging and thermal cycling.SR1  Further investigation revealed dose saturation of the Sc precursor occurred at significantly shorter dose times indicative of improved ClSc(EtCp)2 delivery after the thermal cycling event (Fig. S5).  We concluded that at least one of the manual isolation valves on the flow-through ampoule was in a partially closed position prior to thermally cycling, thereby limiting the conductance through the ampoule.

Fig. S5.  GPC versus ClSc(EtCp)2 dose and purge time determined in situ for ScN PEALD on Si (100) at a 215°C substrate temperature.  Sc precursor dose saturation at ~0.15 Å/cycle is observed over the full range of dose times from 0.25–1.75 s.  GPC also remains constant at ~0.15 Å/cycle above 20 s ClSc(EtCp)2 purge time.

It was previously reported that a higher value was observed for the refractive index at the center versus the edge positions of a 150 mm Si (100) substrate.SR1 We investigated this phenomenon and determined that the index NU correlated with continuous H2 flow through the ICP source during ScN growth. After limiting the H2 flow to the N2-H2 plasma dose step only, the index NU significantly improved; therefore, in this work, we limited H2 flow to the plasma dose step only.

Supplemental Reference

SR1 Gilbert B. Rayner, Jr., Noel O’Toole, Bangzhi Liu, Jeffrey Shallenberger, Jiadi Zhu, Tomás

Palacios, Piush Behera, Suraj Cheema, Blaine Johs and Nicholas A. Strnad, J. Vac. Sci.

Technol. A 43, 020401 (2025).