Extended Data

Table EI.  Summary of Al(1-x)ScxN film thickness, refractive index and composition.

| ScN: AlN | Temp. (°C) | Thick. (nm) | Index (633nm) | Al (at.%) | Sc (at.%) | N (at.%) | N: Al+Sc | x | Cl (at.%) | C (at.%) | O (at.%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0:1 | 215 | 39.2 ± 1.7% | 1.88 ± 1.2% | 52.4 ± 0.3 | 0.0 | 45.6 ± 0.4 | 0.87 ± 0.01 | 0.0 | 0.0 | 1.9 ± 0.5 | 0.2 ± 0.1 |
| 1:1 | 215 | 35.4 ± 1.2% | 2.04 ± 0.8% | 46.0 ± 0.3 | 7.5 ± 0.1 | 44.6 ± 0.3 | 0.84 ± 0.01 | 0.14 ± 0.01 | 0.9 ± 0.1 | 0.6 ± 0.2 | 0.4 ± 0.3 |
| 1.5:1 | 215 | 41.1 ± 1.7% | 2.12 ± 0.6% | 41.1 ± 0.4 | 11.2 ± 0.1 | 45.8 ± 0.2 | 0.88 ± 0.02 | 0.21 ± 0.01 | 1.2 ± 0.1 | 0.6 ± 0.3 | 0.2 ± 0.2 |
| 2:1 | 215 | 36.5 ± 3.0% | 2.12 ± 0.7% | 37.1 ± 0.7 | 15.4 ± 0.3 | 44.2 ± 0.5 | 0.84 ± 0.02 | 0.29 ± 0.01 | 1.9 ± 0.1 | 1.2 ± 0.7 | 0.3 ± 0.4 |
| 3:1 | 215 | 34.7 ± 2.5% | 2.19 ± 0.9% | 27.7 ± 0.3 | 23.0 ± 0.1 | 46.1 ± 0.4 | 0.91 ± 0.01 | 0.45 ± 0.01 | 2.3 ± 0.1 | 0.7 ± 0.2 | 0.2 ± 0.2 |
| 0:1 | 300 | 40.5 ± 2.7% | 1.99 ± 0.4% | 52.2 ± 0.1 | 0.0 | 47.1 ± 0.2 | 0.90 ± 0.01 | 0.0 | 0.0 | 0.7 ± 0.1 | 0.1 ± 0.1 |
| 1.5:1 | 300 | 36.4 ± 2.3% | 2.11 ± 0.6% | 47.6 ± 0.3 | 6.6 ± 0.3 | 45.3 ± 0.3 | 0.84 ± 0.01 | 0.12 ± 0.01 | 0.2 ± 0.1 | 0.0 | 0.4 ± 0.2 |
| 3:1 | 300 | 30.9 ± 6.4% | 2.16 ± 1.4% | 35.9 ± 0.6 | 15.3 ± 0.3 | 47.4 ± 0.3 | 0.93 ± 0.02 | 0.30 ± 0.01 | 0.6 ± 0.1 | 0.5 ± 0.3 | 0.3 ± 0.2 |

Fig. E1.  Sc concentration versus # of ScN cycles per AlN cycle for Al(1-x)ScxN PEALD on Si (100) at a 215°C substrate temperature.

Fig. E2.  Al(1-x)ScxN-coated trenches with a 5:1 aspect ratio imaged by FESEM showing a bottom-to-top thickness ratio of 86%.

Fig. E3.  Close-up of the Al(1-x)ScxN Goniometer 2θ XRD scan of (0002) peaks shown in Fig. 4(a) with the fit peak center values (2-theta) labeled for convenience.

Fig. E4.  XRD patterns of Al0.79Sc0.21N thin films grown with a ScN:AlN cycle ratio of 1.5:1 on {111}-oriented Pt substrates at a substrate temperature of 215° C. (a) Goniometer 2θ scan showing a very small (0002) Al0.79Sc0.21N peak, (b) a closeup of the same, and (c) omega rocking curve scan along the (0002) Al0.79Sc0.21N peak.

Fig. E5.  Full-sized Phi scans aligned to the (103) plane of PEALD Al0.88Sc0.12N (40.2 nm-thick with a 5nm-thick AlN nucleation layer) (a) and epitaxial GaN (b) films on a c-plane sapphire substrate.