| Figure 1: chalcopyrite 1 | Figure 2: chalcopyrite 1 |
| --- | --- |
| Figure 3: chalcopyrite 2 | Figure 4: chalcopyrite 2 |
| Figure 5: chalcopyrite 3 | Figure 6: chalcopyrite 3 |
| Figure 7: pyrite 1 | Figure 8: pyrite 1 |

| Figure 9: pyrite 2 | Figure 10: pyrite 2 |
| --- | --- |

Table 1:Raw vs. Processed SEM Images

Table 2: Liberation Analysis Results from Image Processing

| Sample | Total Grains | Grain Area (pixels) | Image Area (pixels) | Liberation (%) |
| --- | --- | --- | --- | --- |
| Chalcopyrite1 | 1,076 | 105,638 | 228,800 | 46.17 |
| Chalcopyrite2 | 5,837 | 876,433 | 4,121,920 | 21.26 |
| Chalcopyrite3 | 2,223 | 127,014 | 512,502 | 24.78 |
| Pyrite1 | 2,888 | 168,731 | 549,950 | 30.68 |
| Pyrite2 | 2,573 | 143,481 | 504,900 | 28.42 |

Table 3: Individual Grain Size Histograms for chalcopyrite’s

Table 4: Individual Grain Size Histograms for Pyrite's and Combined Histogram