Table S1 The proximate and ultimate analysis of three types of AC

| Sample | Proximate analysis (ad, wt%) |  |  |  | Ultimate analysis (ad, wt%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | moisture | volatile | ash | fixed carbon | C | H | O* | N | S |
| AC1 | 6.74 | 6.48 | 6.38 | 80.40 | 78.53 | 4.27 | 2.86 | 0.92 | 0.39 |
| AC2 | 6.57 | 7.92 | 10.93 | 74.88 | 72.93 | 5.01 | 1.98 | 1.03 | 1.55 |
| AC3 | 6.42 | 13.52 | 12.99 | 67.07 | 67.51 | 5.96 | 3.57 | 1.12 | 2.43 |

*-calculated by difference

Figure S1 Flow chart of catalyst preparation through solid-phase method

Figure S2 Schematic diagram of experimental setup for testing catalyst performance

Figure S3 Nitrogen adsorption-desorption isotherms and pore size of AC

Figure S4 High-resolution XPS spectra of Ni/AC2 and Ni/AC3: a) Ni/AC2 and Ni/AC3; b) C 1s; c) Ni 2p3/2; d) O 1s e) Cl 2p3/2

Figure S5 Nitrogen adsorption-desorption isotherms and pore sizes of the Ni/AC catalysts

Figure S6 H2 selectivity and carbon balance curves of Ni/AC on DRM at different temperatures:

a) H2 selectivity; b) carbon balance

Figure S7 H2 selectivity and carbon balance curves of Ni/AC at 900 °C:

a) H2 selectivity; b) carbon balance