Supplementary Table S1

| Trial ID | Workpiece | Wheel Type | Issue Noted | Reason for Exclusion |
| --- | --- | --- | --- | --- |
| A4 | OHNS | SiC | Erratic Ra values | Spindle vibration – confirmed via log |
| A7 | OHNS | SiC | SEM showed chatter bands | Measurement deviation > ±0.20 µm |
| B4 | EN24 | SiC | Contact profilometer error | Failed triple measurement repeatability |
| B7 | EN24 | SiC | Workpiece surface irregularity | Defective sample – pre-grinding anomaly |