1.0 Catalyst Characterization

The detailed analysis of the catalyst was conducted through a combination of sophisticated analytical methods to thoroughly assess its structural, thermal, surface, and chemical properties. The analysis involved X-ray diffraction (XRD) using a Shimadzu XRD-6000 diffractometer, which scanned at a rate of 4°/min across a 2θ range from 5° to 80°. The resulting diffractograms were then compared with files from the International Centre for Diffraction Data (ICDD) to determine the crystalline phases present in the synthesized catalyst (Adzahar et al., 2022). Thermogravimetric analysis (TGA) was performed utilizing a TGA 1000i instrument in an inert nitrogen atmosphere, with the catalyst being heated from 25 °C to 900 °C at a rate of 30 °C/min to evaluate its thermal stability and decomposition characteristics (Adzahar et al., 2022). The catalyst's specific surface area and porosity were assessed through Brunauer-Emmett-Teller (BET) and Barrett-Joyner-Halenda (BJH) methods utilizing a Thermo-Finnigan Shopmatic 1990 N2 sorption analyzer. Before analysis, samples underwent degassing at 150 °C for 12 hours to eliminate moisture and contaminants, followed by nitrogen adsorption-desorption at −196 °C to evaluate surface characteristics essential for catalytic activity (Adzahar et al., 2025). Furthermore, the acidity of the catalyst were examined through temperature-programmed desorption of ammonia (TPD-NH3) utilizing a Thermo-Finnigan TPDRO analyzer that is outfitted with a thermal conductivity detector (TCD). About 0.05 g of catalyst underwent a pre-treatment at 150°C in a nitrogen atmosphere to remove moisture. It was then exposed to NH3 for one hour at room temperature, followed by a nitrogen purge (Adzahar et al., 2025). Subsequently, the temperature was increased from 50°C to 900°C under helium flow to observe NH3 desorption, indicating the strength and quantity of acidic sites present on the catalyst surface. The combination of these characterisation techniques offers a comprehensive insight into the catalyst’s crystalline structure, thermal stability, surface morphology, and acid characteristics, all of which are crucial for enhancing its efficacy in catalytic applications.

2.0 Feedstock Saponification

This study involved the precise weighing of 2.0 g of Palm Fatty Acid Distillate (PFAD), which was then placed in a round-bottom flask to ascertain its saponification value and molecular weight, essential parameters for evaluating feedstock quality and its appropriateness for biodiesel production. To commence the saponification process, 25 mL of 0.5 M ethanolic potassium hydroxide (KOH) solution was introduced into the flask. The mixture was refluxed at 65°C with continuous stirring for one hour to ensure complete reaction between the alkali and the triglycerides or free fatty acids in the PFAD. The controlled temperature during refluxing enhances the hydrolysis of ester bonds, transforming oil components into glycerol and soap, which is crucial for precise saponification measurement. Following the reflux period, the reaction mixture was allowed to cool to room temperature, and 10 drops of phenolphthalein indicator were introduced. Phenolphthalein functions as a pH indicator, exhibiting a pink color in basic solutions and remaining colorless in acidic environments, thereby facilitating accurate endpoint determination in titration processes. The mixture was titrated with 0.5 M hydrochloric acid (HCl) until the disappearance of the pink color, signifying the neutralization of the excess alkali (Hazmi et al., 2021). This titration step measures the quantity of KOH utilized in the saponification of the PFAD sample. The saponification value (SV) of PFAD was determined using the volume of HCl consumed during titration, as outlined in equation (1). The saponification value indicates the mg of KOH needed to saponify one gramme of oil, offering insights into the average molecular weight of the fatty acids involved. The molecular weight (MW) of PFAD was subsequently calculated from the saponification value using equation (2), which establishes an inverse relationship between the saponification value and the average molecular weight of the oil components.

Saponification value, 𝑆𝑉 = Blank -Volume HCl used ×Molarity of KOH × MW of KOHW         (1)

Molecular weight of oil, MW = 56.11 ×1000SV             (2)

In this case, W represents the weight of the oil used for saponification, while MW represents the molecular weight of KOH.  The saponification value of PFAD employed in this study has been estimated and determined using equations (1) and (2) as follows:

Saponification value of PFAD, SVPFAD

= Blank -Volume HCl used ×Molarity of KOH × MW of KOHW

= 25-8.6 ×0.5M ×56.112.0166g

= 228.16 mg KOH/g

Average molecular weight of PFAD in this study, MWPFAD

= 56.11 ×1000SV

= 56.11 ×1000228.16

= 245.9 g/mol

Since the saponification value represents the fatty acid chain length and composition, which affect the feedstock's reactivity and quality during the biodiesel synthesis process, figuring out these factors is essential. Fuel characteristics like viscosity and cold flow can be impacted by shorter fatty acid chains, which are associated with lower molecular weights. As a result, this systematic method of determining the molecular weight and saponification value guarantees a thorough comprehension of PFAD's chemical properties, allowing for the optimization of subsequent biodiesel manufacturing procedures (Hazmi et al., 2022).

3.0 Acid Value Calculation

To evaluate the quality and concentration of free fatty acids in the PFAD, 2.0 g of PFAD was precisely measured into a conical flask. Subsequently, 25 mL of ethanol was introduced, and the mixture was rapidly boiled to ensure the complete solubility of the oil and to promote the acid-base interaction. Subsequent to boiling, the solution was allowed to cool to ambient temperature, and 5 to 7 drops of phenolphthalein indicator were added. Phenolphthalein, which transitions from colorless to pink under alkaline circumstances, was utilized to visually identify the endpoint during titration. The titration was conducted using 0.5 M potassium hydroxide (KOH) until the solution transitioned from colorless to a pale pink, signifying the neutralization of free fatty acids by the base (Hazmi et al., 2025). The volume of KOH utilized in the titration was documented, and the acid value (AV) was computed using equation (3) and FFA was measure using equation (4):

AV = Volume KOH used-Blank ×  Normality of KOH ×MW of KOHWeight of the oil used        (3)

FFA = AV2      (4)

FFA Conversion (%) = AVi- AVfAVi   ×100%     (5)

Where AVi is the acid value initial and AVf is the final acid value, hence the calculation for acid value and FFA for PFAD used in this study is calculated as below using equation (3) and (4) :

AVPFAD = 25.1-12 ×0.5N ×56.112.0079g

= 183.04

FFA = 183.042

= 91.52

4.0  Biodiesel confirmation analysis

The ester compositions of biodiesel were assessed using gas chromatography with a flame ionization detector (GC-FID, Agilent 7890-A) equipped with a pre-installed BPX-70 capillary column (60 m 0.25 mm 0.25 m), in accordance with the EN14103 standard procedure. The eluted esters from the synthesized biodiesel were compared with reference standards of known concentrations (C12:0, C14:0, C16:0, C18:0 and C18:2). A volume of approximately 20μL–40μL of the biodiesel sample was diluted with a gas chromatography solvent consisting of 1000 ppm methyl heptadecanoate (internal standard) dissolved in hexane. 1 μL of diluted biodiesel was injected into the injector port at 250 °C. The gas chromatography oven temperature was originally established at 100 °C and incrementally increased to 250 °C at a rate of 10 °C/min, while the detector temperature was maintained at 270 °C (Hazmi et al., 2025). The PerkinElmer (PC) Spectrum 100 FTIR, with a resolution of 4 cm−1 (300–4000 cm−1), was employed to validate the identified organic functional compounds (Adzahar et al., 2022).

References

Adzahar, N. A., AbdulKareem-Alsultan, G., Mijan, N. A., Mastuli, M. S., Lee, H. V., & Taufiq-Yap, Y. H. (2025). Effect of catalyst synthesis of bimetallic nickel-cobalt supported iron-based catalysts on converting palm kernel oil into bio-jet fuel via deoxygenation reaction. Energy, 314(June 2024), 133957. https://doi.org/10.1016/j.energy.2024.133957

Adzahar, N. A., Asikin-Mijan, N., Saiman, M. I., Alsultan, G. A., Mastuli, M. S., Shamsuddin, M. R., & Taufiq-Yap, Y. H. (2022). Chemoselective decarboxylation of ceiba oil to diesel-range alkanes over a red mud based catalyst under H2-free conditions. RSC Advances, 12(26), 16903–16917. https://doi.org/10.1039/d2ra00853j

Hazmi, B., Beygisangchin, M., Rashid, U., Mokhtar, W. N. A. W., Tsubota, T., Alsalme, A., & Ngamcharussrivichai, C. (2022). Glycerol-Based Retrievable Heterogeneous Catalysts for Single-Pot Esterification of Palm Fatty Acid Distillate to Biodiesel. Molecules, 27(20). https://doi.org/10.3390/molecules27207142

Hazmi, B., Rashid, U., Akhlisah, Z. N., Chaowamalee, S., Ngamcharussrivichai, C., & Sabater, M. J. (2025). Productive esterification of palm fatty acid distillate under lignocellulosic biomass char of rambutan seeds waste-supported sulfonated catalyst. Biomass and Bioenergy, 194, 107607. https://doi.org/https://doi.org/10.1016/j.biombioe.2025.107607

Hazmi, B., Rashid, U., Ibrahim, M. L., Nehdi, I. A., Azam, M., & Al-Resayes, S. I. (2021). Synthesis and characterization of bifunctional magnetic nano-catalyst from rice husk for production of biodiesel. Environmental Technology & Innovation, 21, 101296. https://doi.org/https://doi.org/10.1016/j.eti.2020.101296