| Table 1. Optimizing of different parameters for the model reaction in the synthesis of 5a catalysed by the CS-g-PAN/Fe3O4 nanoparticles (1)a |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Catalyst loading (mg) | Solvent | Temp (oC) | Time (min) | Yieldb(%) |
| 1 | - | - | - | r.t. | 120 | Trace |
| 2 | - | - | - | 80 | 120 | Trace |
| 3 | - | - | CH3CN | Reflux | 120 | Trace |
| 4 | CS-g-PAN/Fe3O4 | 10 | - | r.t. | 30 | <50 |
| 5 | CS-g-PAN/Fe3O4 | 10 | EtOH | r.t. | 20 | 72 |
| 6 | CS-g-PAN/Fe3O4 | 10 | EtOH | 80 | 20 | 88 |
| 7 | CS-g-PAN/Fe3O4 | 10 | H2O | Reflux | 20 | <60 |
| 8 | CS-g-PAN/Fe3O4 | 10 | EtOH/H2O (1:1) | 80 | 10 | 97 |
| 9 | CS-g-PAN/Fe3O4 | 5 | EtOH/H2O (1:1) | 80 | 15 | 85 |
| 10 | CS-g-PAN/Fe3O4 | 8 | EtOH/H2O (1:1) | 80 | 10 | 92 |
| 11 | CS-g-PAN/Fe3O4 | 10 | EtOH/H2O (1:1) | r.t. | 10 | 74 |
| 12 | CS-g-PAN/Fe3O4 | 10 | EtOH/H2O (1:1) | Reflux | 10 | 90 |
| 13 | Fe3O4 | 10 | EtOH/H2O (1:1) | 80 | 20 | N.R. |
| 14 | Chitosan | 10 | EtOH/H2O (1:1) | 80 | 20 | 48 |
| aReaction conditions: ethyl acetoacetate (2, 1.0 mmol), hydrazine hydrate (3, 1.0 mmol), aldehyde (5a, 1.0 mmol) and malononirile (4, 1.0 mmol), in the presence of CS-g-PAN/Fe3O4 nanomaterial (1) were added to the solvent (3.0 ml) unless otherwise stated. bIsolated yields. |  |  |  |  |  |  |

| Table 2. The synthesis of DHPPs derivatives in optimized conditions using CS-g-PAN/Fe3O4 nanocatalyst.a |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Entry | R | Productb | Time (min) | Yieldc (%) | M.p. (oC) | M.p. (oC) (Lit.) | Ref |
| 1 | 4-Cl | 6a | 10 | 95 | 216-218 | 216-219 | 74 |
| 2 | 2-Cl | 6b | 10 | 95 | 243-245 | 245-246 | 75 |
| 3 | 2,4-Cl2 | 6c | 10 | 95 | 230-234 | 231-233 | 76 |
| 4 | 4-Me | 6d | 25 | 95 | 195-200 | 196-198 | 77 |
| 5 | 4-OMe | 6e | 20 | 91 | 210-212 | 209-212 | 50 |
| 6 | 2-OMe | 6f | 20 | 90 | 249-253 | 251-253 | 10 |
| 7 | 3-OH | 6g | 20 | 89 | 254-256 | 253-256 | 78 |
| 8 | 4-OH | 6h | 20 | 91 | 225-226 | 224-226 | 79 |
| 9 | 4-Br | 6i | 20 | 92 | 217-220 | 218-220 | 80 |
| 10 | 4-F | 6j | 20 | 94 | 170-172 | 168-170 | 81 |
| 11 | 3-NO2 | 6k | 30 | 89 | 214-215 | 213-215 | 82 |
| 12 | 4-NO2 | 6l | 35 | 89 | 251-253 | 250-252 | 83 |
| 13 | 4-CN | 6m | 32 | 90 | 213-215 | 212-214 | 84 |
| 14 | 2-Furyl | 6n | 36 | 79 | 227-229 | 227-229 | 85 |
| 15 | 2-Thienyl | 6o | 36 | 79 | 250-252 | 251-253 | 76 |
| 16 | 3-Pyridyl | 6p | 39 | 84 | 214-215 | 216-217 | 86 |
| aReaction conditions: ethyl acetoacetate (2, 1.0 mmol), hydrazine hydrate (3, 1.0 mmol), aldehyde (5a, 1.0 mmol) and malononitrile (4, 1.0 mmol), in the presence of CS-g-PAN/Fe3O4 nanomaterial (1) were added to the solvent (3.0 ml) unless otherwise stated. bIsolated yields. Scope of the synthesis of DHPPs derivatives 6a-p catalyzed by CS-g-PAN/Fe3O4 (1) under optimized reaction conditions. All compounds are known and their structures were established from their spectral data and melting points as compared with literature values. cYields refer to the isolated products. |  |  |  |  |  |  |  |

| Table 3. Optimizing of different parameters for the model reaction in the synthesis of 5i catalysed by the CS-g-PAN/Fe3O4 nanoparticles (1)a |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Catalyst loading (mg) | Solvent | Temp (oC) | Time (min) | Yieldb(%) |
| 1 | - | - | - | 80 | 120 | Trace |
| 2 | - | - | - | 100 | 120 | Trace |
| 3 | - | - | EtOH | Reflux | 120 | 20 |
| 4 | Chitosan | 10 | EtOH | Reflux | 20 | 48 |
| 5 | CS-g-PAN/Fe3O4 | 5 | EtOH | r.t. | 20 | 68 |
| 6 | CS-g-PAN/Fe3O4 | 7 | EtOH | r.t. | 20 | 81 |
| 7 | CS-g-PAN/Fe3O4 | 10 | EtOH | Reflux | 10 | 97 |
| 8 | CS-g-PAN/Fe3O4 | 10 | Acetone | Reflux | 10 | 96 |
| 9 | CS-g-PAN/Fe3O4 | 10 | H2O | Reflux | 20 | 65 |
| 10 | CS-g-PAN/Fe3O4 | 10 | EtOH/H2O (1:1) | Reflux | 10 | 81 |
| 11 | CS-g-PAN/Fe3O4 | 15 | EtOH | Reflux | 10 | 96 |
| 12 | CS-g-PAN/Fe3O4 | 10 | MeCN | Reflux | 20 | 50 |
| 13 | CS-g-PAN/Fe3O4 | 10 | EtOH | r.t. | 20 | 89 |
| 14 | Fe3O4 | 10 | EtOH/H2O (1:1) | 80 | 20 | N.R. |
| aReaction conditions: 2-nitrobezaldehyde (5i, 1.0 mmol), malononitrile (4, 1.0 mmol), dimedone (6, 1.0 mmol), and the CS-g-PAN/Fe3O4 catalyst. |  |  |  |  |  |  |

| Table 4. Synthesis of different derivatives of 4H-pyran 7a-j through the MCRs catalyzed by CS-g-PAN/Fe3O4 nanocatalyst (1) under the optimized conditions.a |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Entry | R | Productb | Time (min) | Yieldc (%) | M.p. (oC) | M.p. (oC) (Lit.) | Ref |
| 1 | 4-Cl | 7a | 15 | 94 | 235-237 | 234-236 | 87 |
| 2 | 2-Cl | 7b | 15 | 92 | 211-214 | 213-215 | 88 |
| 3 | 4-F | 7c | 15 | 93 | 242-244 | 244-246 | 64 |
| 4 | 4-OH | 7d | 20 | 93 | 250-252 | 252-254 | 64 |
| 5 | 4-OMe | 7e | 20 | 91 | 197-199 | 197-199 | 89 |
| 6 | 2-OMe | 7f | 20 | 90 | 197-199 | 198-199 | 90 |
| 7 | 4-Me | 7g | 25 | 90 | 173-175 | 173-175 | 91 |
| 8 | 3-NO2 | 7h | 10 | 95 | 188-190 | 187-188 | 92 |
| 9 | 2-NO2 | 7i | 10 | 95 | 182-184 | 180-182 | 93 |
| 10 | 4-CN | 7j | 10 | 97 | 229-230 | 227-229 | 94 |
| aReaction conditions: aldehyde (5a-j, 1.0 mmol), malononirile (4, 1.2 mmol), dimedone (6, 1.0 mmol) and in the presence of CS-g-PAN/Fe3O4 nanomaterial (1) were added to the solvent (3.0 ml) unless otherwise stated. bIsolated yields. Scope of the synthesis of 2‐amino‐3-cyano-4H‐pyran derivatives (7a-j) catalyzed by CS-g-PAN/Fe3O4 (1) under optimized reaction conditionsa.a Reaction conditions: ethyl acetoacetate (2, 1.0 mmol), aldehyde (5a-j, 1.0 mmol) and malononirile (4, 1.0 mmol) in the presence of CS-g-PAN/Fe3O4 nanomaterial (1, 0.01 g) was added to the EtOH (3.0 ml) at room temperature. cAll compounds are known and their structures were established from their spectral data and melting points as compared with literature values. dYields refer to the isolated products. |  |  |  |  |  |  |  |

| Table 5. Comparison of the catalytic efficiency of CS-g-PAN/ Fe3O4 nanocatalyst with some previously reported heterogeneous catalysts |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Entry | Catalyst | Catalyst loading (mg) | Solvent | Temp (oC) | Time (min) | Yield (%) | product | Ref |
| 1 | Fe-MCM-22 zeolite | 10 | H2O/EtOH | 60 | 50 | 94 | 6a | 96 |
| 2 | CMC-SO3H | 30 | EtOH | 60 | 40 | 90 | 6a | 97 |
| 3 | Fe3O4@PDA/CuCl2 | 50 | H2O | 70 | 30 | 94 | 6a | 98 |
| 4 | CS-g-PAN/Fe3O4 | 10 | H2O/EtOH | 80 | 10 | 97 | 6a | This work |
| 5 | CuFe2O4@starch | 30 | EtOH | r.t | 20 | 96 | 5a | 99 |
| 6 | Fe3O4@CS–TDI–Titriplex V | 20 | EtOH | Reflux | 30 | 30 | 5a | 100 |
| 7 | NiFe2O4 | 11.7 | EtOH | 40 | 35 | 90 | 5a | 101 |
| 8 | Fe3O4@Ph-SO3H | 0.2 mol % | H2O | 50 | 25 | 88 | 5a | 102 |
| 9 | DAHP | 10 mol % | H2O/EtOH | 25 | 240 | 85 | 5a | 103 |
| 10 | CS-g-PAN/Fe3O4 | 10 | EtOH | Reflux | 10 | 97 | 5a | This work |