Electronic Supporting Information

Preparation of magnetic decorated polyacrylonitrile grafted chitosan as a new bio-inspired nanocatalyst for the synthesis of dihydropyrano [2,3-c]pyrazoles and 2-amino-3-cyano-4H-pyran derivatives

Niloufar Nashibi1, Mohammad G. Dekamin1, Ali Maleki1

1Pharmaceutical and Biologically-Active Compounds Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran 16846-13114, Iran

Tel: +98-21-77240640-50; fax: +98-21-73021584; e-mail: mdekamin@iust.ac.ir

| Page | Contents |
| --- | --- |
| S1 | Title page |
| S3 | Fig. S1. Structure of selected examples of biologically- and pharmacologically-active dihydropyrano [2,3-c] pyrazole and 4H-pyrans.derivatives |
| S3 | Fig. S2. Schematic representation for the preparation of CS-g-PAN/Fe3O4 nanoparticles (1) |
| S4 | Fig. S3. One-pot three-component synthesis of highly substituted dihydropyrano [2,3-c] pyrazole (DHPPs) and 4H-pyrans derivatives catalyzed by the magnetic CS-g-PAN/Fe3O4 nanoparticles. |
| S4 | Fig. S4. FTIR spectra of (a) PAN, (b) CS, (c) CS-g-PAN and (d) the CS-g-PAN/Fe3O4 |
| S5 | Fig. S5. FESEM images of the CS-g-PAN nanoparticles (1). |
| S5 | Fig. S6. XRD patterns of the CS-g-PAN/Fe3O4 nanoparticles (1), CS-g-PAN and CS |
| S6 | Fig. S7. EDX spectra of the CS-g-PAN/Fe3O4 nanoparticles (1), along with its elemental mapping for a fresh sample. |
| S6 | Fig. S8. Hysteresis diagram of the CS-g-PAN/Fe3O4 nanoparticles (1) |
| S7 | Fig. S9. (a) The N2 adsorption–desorption isotherm of CS-g-PAN catalyst (1) and (b) its pore width. |
| S7 | Fig. S10. TGA patterns of the CS-g-PAN/Fe3O4 nanoparticles (1) |
| S8 | Fig. S11. FTIR spectra of the recycled CS-g-PAN/Fe3O4 MNPs (1) after the first run (Down, blue curve); and five run (Top, red curve) in the model reaction for the synthesis of 6k. |
| S9 | Fig. S12. 1H NMR spectrum of compound (6a) |
| S10 | Fig. S13. 1H NMR spectrum of compound (6k) |
| S11 | Fig. S14. 1H NMR spectroscopy of the 4H-Pyran (7a) |
| S12 | Fig. S15. 1H NMR spectroscopy of the 4H-Pyran (7j) |
| S13 | Fig. S16. 1H NMR spectroscopy of the 4H-Pyran (7i) |

(Anticancer activity) A

(Inhibitor of human CHK1 kinase) C

(Antibacterial) B

(Antifungal) E

(Anti-tumor agent) D

Fig. S1. Structure of selected examples of biologically- and pharmacologically-active dihydropyrano [2,3-c] pyrazole and 4H-pyran derivatives.

(Tumor vascular-disrupting agent) F

(Antiproliferative agent) G

(Anticancer agent) H

Fig. S2. Schematic representation for the preparation of CS-g-PAN/Fe3O4 nanoparticles (1).

Fig. S3. One-pot three-component synthesis of highly substituted dihydropyrano [2,3-c] pyrazole (DHPPs) and 4H-pyrans derivatives catalyzed by the magnetic CS-g-PAN/Fe3O4 nanoparticles.

a)

b)

Fig. S4. FTIR spectra of (a) PAN, (b) CS, (c) CS-g-PAN and (d) the CS-g-PAN/Fe3O4.

|  | (a) |  | (b) |  |
| --- | --- | --- | --- | --- |
|  | (c) |  | (d) |  |
| Fig. S5. FESEM images of the CS-g-PAN (a-b) and CS-g-PAN/Fe3O4 (c-d) nanoparticles (1). |  |  |  |  |

Fig. S6. XRD patterns of the CS-g-PAN/Fe3O4 nanoparticles (1), CS-g-PAN and CS.

Fig. S7. EDX spectra of the CS-g-PAN/Fe3O4 nanoparticles (1), along with its elemental mapping for a fresh sample.

a

b

Fig. S8. Hysteresis diagram of the CS-g-PAN/Fe3O4 nanoparticles (1).

Fig. S10. TGA patterns of the CS-g-PAN/Fe3O4 nanoparticles (1).

Fig. S9. (a) The N2 adsorption–desorption isotherm of CS-g-PAN catalyst (1) and (b) its pore width.

a

b

Fig. S11. FTIR spectra of the recycled CS-g-PAN/Fe3O4 MNPs (1) after the first run (Down, blue curve); and five run (Top, red curve) in the model reaction for the synthesis of 6k.

Fig. S12. 1H NMR spectrum of compound (6a).

Fig. S13. 1H NMR spectrum of compound (6k).

Fig. S14. 1H NMR spectroscopy of the 4H-pyran (7a).

Fig. S15. 1H NMR spectroscopy of the 4H-pyran (7j).

Fig. S16. 1H NMR spectroscopy of the 4H-pyran (7i).