Table 1. Surface physical characteristics of MSA-SB@Ni

| Properties | MSA-SB@Ni |
| --- | --- |
| BET surface area (m2 g-1) | 16.829 |
| Micropore surface area (m2 g-1) | 12.150 |

| External surface area (m2 g-1) | 21.12 |
| --- | --- |
| Langmuir surface area (m2 g-1) | 42.012 |
| Total pore volume (cm3 g-1) | 0.0865 |
| Average pore diameter (nm) | 4.61 |

Table 2. Optimization and evaluation of catalyst, reactant and reaction conditions.

| Yield (%) | Temp (˚C) | Time (h) | cat (mg) [mol %] | Catalyst | Ra | Entry |
| --- | --- | --- | --- | --- | --- | --- |
| 92 | 100 | 4 | 15[1.50] | MSA-SB@Ni b | H- | 1 |
| 82 | 100 | 4 | 10[0.66] | MSA-SB@Ni | -H | 2 |
| 71 | 80 | 4 | " | MSA-SB@Ni | -H | 3 |
| 86 | 70 | 4 | 15[1.50] | MSA-SB@Ni | -H | 4 |
| 87 | 100 | 4 | " | MSA-SB@Ni | CH3- | 5 |
| 81 | 100 | 4 | " | MSA-SB@Ni | CH3 -di | 6 |
| 95 | 90 | 4 | " | MSA-SB@Ni | NO2- | 7 |
| 93 | 90 | 4 | " | MSA-SB@Ni | Cl- | 8 |
| 88 | 100 | 4 | " | MSA-SB@Ni | OH- | 9 |
| 40 | 100 | 4 | " | MSA-SB@Cuc | H- | 10 |
| 36 | 100 | 4 | " | MSA-SB@Mnd | H- | 11 |
| 38 | 100 | 4 | " | MSA-SB@Zne | -H | 12 |
| 90 | 90 | 4 | " | MSA-SB@Ni | -H | 13 |
| 81 | 100 | 3 | " | MSA-SB@Ni | -H | 14 |
| 87 | 100 | 3 | " | MSA-SB@Ni | -NO2 | 15 |
| 15 | 110 | 8 | 0 | - | H- | 16f |

Reaction condition: reaction between aldehyde, β-naphthol, and amide with MSA-SB@Ni as nanocatalyst for green synthesis of amido alkyl naphthol.

a) Benzaldehyde derivatives.

b) MSA-SB@Ni=  Fe3O4@SiO2/APTES-Schiff base of Ni as catalyst.

c) MSA-SB@Cu= Fe3O4 @SiO2/APTES-Schiff base of Cu as catalyst.

e) MSA-SB@Zn= Fe3O4@SiO2/APTES-Schiff base of Zn as catalyst.

f) In this step the reaction performed without a catalyst.

Table 3. Model reaction and synthesis of amidoalkyl naphthol derivatives via multi-component reaction in the presence of MSA-SB@Ni nano-catalyst in solvent free conditions.

| Yield (%)f | Time (h) | TONe | TOF (h-1)d | Product c | R2 b | R1 a | Entry |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 92 | 4 | 61.3 | 15.32 |  |  |  | 1 |
| 93 | 4 | 62 | 15.5 |  |  |  | 2 |
| 95 | 3.5 | 63.3 | 18.08 |  |  |  | 3 |
| 88 | 4 | 58.66 | 14.66 |  |  |  | 4 |
| 86 | 4 | 57.33 | 14.33 |  |  |  | 5 |
| 93 | 4 | 62 | 15.5 |  |  |  | 6 |
| 90 | 4 | 60 | 15 |  |  |  | 7 |
| 94 | 4 | 62.66 | 15.66 |  |  |  | 8 |
| 89 | 4 | 59.33 | 14.8 |  |  |  | 9 |
| 88 | 4 | 58.66 | 14.66 |  |  |  | 10 |
| 92 | 4 | 61.33 | 15.33 |  |  |  | 11 |

Reaction conditions:  β naphthol (1 mmol as fix reactant), aldehyde (1 mmol) with and amide (1.5 mmol) in the presence of MSA-SB@Ni as nanocatalyst (0.015 g) at 80-100°C under solvent-free conditions. Isolated yield. Mmol of active site of catalyst =1.5×10-2

- Aldehyde derivatives as reactant 1

- Amide derivatives as reactant 2

- Amido-alkyl-2-naphthol as product

- TOF (h-1) = Turn over frequency of catalyst: (TON / time of the reaction (h))

- TON = Turn over number of catalyst: (mmol of product / mmol of active site of catalyst).

- The efficiency of product in thermal method and free solvent.

Table 4. Comparison of the catalytic efficiency of MSA-SB@Ni  nano catalyst with other reported catalysts that used for the synthesis of amidoalkyl naphthol.

| Entry | Catalyst | Solvent | Temp. (˚C) | Time (h) | Yield (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | K5CoW12O40.3H2O | (CH2)2Cl2 | 25 | 10 | 92 | [43] |
| 2 | HClO4 | - | 90 | 3 | 80 | [44] |
| 3 | I2 | - | 125 | 5.5 | 85 | [44] |
| 4 | Ce(SO4)2 | - | reflux | 36 | 72 | [44] |
| 5 | Na2SO4 | - | 100 | 4 | 12 | [45] |
| 6 | CuO | - | 100 | 4.3 | 69 | [45] |
| 7 | Fe2O3 | - | 100 | 5 | 20 | [45] |
| 8 | CaO | - | 100 | 4.1 | 71 | [45] |
| 9a | MSA-SB@Ni | - | 100 | 4 | 92 | This work |

a) reaction between benzaldehyde, β-naphthol and acetamide with MSA-SB@Ni as catalyst for green synthesis of amidoalkyl naphthol ( Table 3.entry 1)