Research Highlights

👉 A novel biocomposite combining DEAE-cellulose fiber and fish scale-derived hydroxyapatite (Hap) was synthesized for Pb(II) removal from water.

👉 The composite exhibited high adsorption capacity (147.7 mg/g) for Pb(II) under optimized conditions, following the Langmuir isotherm model.

👉 FTIR, XRD, SEM-EDS, TGA, and BET analyses confirmed strong interactions and successful incorporation of DEAE-C with Hap.

👉 Adsorption followed a pseudo-first-order kinetic model and was found to be endothermic and spontaneous, based on thermodynamic analysis.

👉 Ion exchange and electrostatic interactions were identified as the main mechanisms of Pb(II) removal, supported by XPS and theoretical calculations.