Supplemental Materials for

“Structural relaxation of ferroelectric phase in hard sodium lithium niobate solid solutions studied by Solid-State NMR”

Millena Logrado, Changhao Zhao, Hergen Breitzke, Jürgen Rödel, Gerd Buntkowsky

S1. Choice of delay recovery in 23Na MAS NMR

Figure S1: Normalized single pulse 23Na MAS under distinct relaxation delays for samples (a) LNN12 and (b) LNN18 aged for 8h at 800°C. A delay time of 3.8 s was used for MQMAS experiments.

S2. 23Na 3QMAS spectra

Figure S2: 23Na TQMAS results for LNNx system with x є [12, 18].

Figure S3: 23Na TQMAS results for LNN18 aged at a temperature T for 8 hours, with T є [500, 800] °C.

Figure S4: 23Na TQMAS results for LNN18 aged at 500 °C for 24 h and at 600 °C for a time t, where t є [0,6] hours.

S3. Values used for the deconvolution of the single-pulse experiments and parameters obtained from the 23Na 3QMAS spectra

Table S1: Quantitative parameters extracted from 23Na single pulse experiment. For each site or phase, the percentage, isotropic chemical shift (δ0), quadrupolar coupling constant (CQ) and asymmetry parameter (ηQ) were measured using a single pulse experiment in a quantitative regime. The letters P, Q, R represent the orthorhombic antiferroelectric phase, the orthorhombic ferroelectric and the rhombohedral phases, respectively, while Am1 and Am2 represent two amorphous sites at higher and lower frequency, respectively. The error in the percentage was estimated as 10% of the corresponding percentage value. Values for absolute error less than 2 is unrealistic, therefore ± 2% is understood as the minimum error value.

| Sample | Site/Phase | Percentage / % | δ0 / ±0.5 ppm | CQ / ±0.2 MHz | ηQ / ±0.1 |
| --- | --- | --- | --- | --- | --- |
| LNN12 | P | 3 | -4.9 | 2.3 | 0.0 |
|  | Q | 24 | -1.9 | 2.0 | 1.0 |
|  | R | 28 | -1.6 | 1.4 | 0.0 |
|  | Am1 | 45 | -5.0 | 1.0 (σ=0.49) | - |
| LNN14 | Q | 24 | -1.2 | 2.31 | 1.0 |
|  | R | 33 | -1.5 | 1.49 | 0.0 |
|  | Am1 | 41 | -4.2 | 1.2 (σ=0.63) | - |
|  | Am2 | 2 | -8.0 | 1.3 (σ=0.70) | - |
| LNN16 | Q | 23 | 0.0 | 2.2 | 1.0 |
|  | R | 42 | -1.2 | 1.4 | 0.0 |
|  | Am1 | 34 | -4.3 | 1.0 (σ=0.50) | - |
|  | Am2 | 1 | -8.4 | 1.2 (σ=0.63) | - |
| LNN18 | Q | 21 | 0.3 | 2.2 | 1.0 |
|  | R | 50 | -0.8 (0.7) | 1.6 | 0.0 |
|  | Am1 | 34 | -3.4 | 1.3 (σ=0.66) | - |
|  | Am2 | 5 | -8.7 | 1.1 (σ=0.57) | - |
| LNN18 500°C (8h) | Q | 12 | 0.3 | 2.2 | 1.0 |
|  | R | 61 | -0.8 (0.7) | 1.6 | 0.1 |
|  | Na1 | 23 | -3.7 | 1.3 (σ=0.54) | - |
|  | Am2 | 4 | -8.7 | 1.1 (σ=0.52) | - |
| LNN18 600°C(8h) | Q | 35 | 0.3 | 2.2 | 1.0 |
|  | R | 33 | -0.9 | 1.7 | 0.1 |
|  | Am1 | 27 | -3.4 | 1.2 (σ=0.65) | - |
|  | Am2 | 5 | -8.5 | 1.2 (σ=0.63) | - |
| LNN18 700°C(8h) | Q | 21 | 0.9 | 2.3 | 1.0 |
|  | R | 66 | -1.1 (0.7) | 1.6 | 0.0 |
|  | Am1 | 13 | -3.6 | 1.0 (σ=0.52) | - |
| LNN18 800°C(8h) | Q | 7 | 1.0 | 2.2 | 1.0 |
|  | R | 77 | -1.0 (0.5) | 1.6 | 0.0 |
|  | Am1 | 16 | -5.0 | 1.2 (σ=0.63) | - |
| LNN18 500°C(24h) 600°C(0h) | Q | 10 | 0.3 | 2.2 | 1.0 |
|  | R | 66 | -0.6 | 1.6 | 0.1 |
|  | Am1 | 22 | -2.8 | 1.1 (σ=0.54) | - |
|  | Am2 | 2 | -8.8 | 1.0 (σ=0.52) | - |
| LNN18 500°C(24h) 600°C(2h) | Q | 20 | 1.4 | 2.3 | 1.0 |
|  | R | 54 | -0.8 | 1.7 | 0.0 |
|  | Am1 | 24 | -3.1 | 1.2 (σ=0.63) | - |
|  | Am2 | 2 | -8.3 | 1.2 (σ=0.62) | - |
| LNN18 500°C(24h) 600°C(4h) | Q | 33 | 1.0 | 2.3 | 1.0 |
|  | R | 38 | -1.6 | 1.6 | 0.0 |
|  | Am1 | 24 | -4.3 | 1.1 (σ=0.57) | - |
|  | Am2 | 5 | -8.8 | 1.1 (σ=0.55) | - |
| LNN18 500°C(24h) 600°C(6h) | Q | 48 | 0.3 | 2.2 | 1.0 |
|  | R | 22 | -2.4 | 1.5 | 0.0 |
|  | Am1 | 23 | -4.6 | 1.0 (σ=0.50) | - |
|  | Am2 | 7 | -9.2 | 0.9 (σ=0.40) | - |

Table S2: Parameters extracted from 23Na 3QMAS experiment. For each site or phase, the isotropic chemical shift (δ0) and the quadrupolar product (PQ) were measured. The letters P, Q, R represent the orthorhombic antiferroelectric, orthorhombic ferroelectric and rhombohedral phases, respectively, while Am1 and Am2 represent two amorphous sites at higher and lower frequency, respectively. Asterisk mark (*) represents the sites with poor signal-to-noise ratio. Due that, their parameters were not able to be extracted accurately.

| Sample | Site/Phase | δ0/ ±0.5 ppm | PQ/ ±0.2 MHz |
| --- | --- | --- | --- |
| LNN12 | P | - | - |
|  | Q | -0.9 | 2.5 |
|  | R | -2.4 | 1.4 |
|  | Am1 | -4.3 | 1.0 |
| LNN18 | Q | -0.3 | 2.5 |
|  | R | -1.8 | 1.6 |
|  | Am1 | -3.9 | 1.1 |
|  | Am2 | -9.1 | 1.1 |
| LNN18 500°C (8h) | Q | * | * |
|  | R | -1.7 | 1.6 |
|  | Na1 | -4.1 | 1.1 |
|  | Am2 | -9.2 | 1.1 |
| LNN18 800°C(8h) | Q | * | * |
|  | R | -1.9 | 1.6 |
|  | Am1 | -4.5 | 1.0 |
| LNN18 500°C(24h) 600°C(0h) | Q | * | * |
|  | R | -1.6 | 1.6 |
|  | Am1 | -3.8 | 1.1 |
|  | Am2 | -8.9 | 1.2 |
| LNN18 500°C(24h) 600°C(6h) | Q | -0.6 | 2.5 |
|  | R | * | * |
|  | Am1 | -3.6 | 1.1 |
|  | Am2 | -9.0 | 1.1 |

S4. Correlation between the lattice parameter and the 23Na chemical shift of the samples

Figure S5: Lattice parameter (d200) as a function of the 23Na chemical shift for (a) LNNx samples, where x є [12,16], and (b) LNN18 for a time t, where t є [0,4] hours.

Table S3: F-value and R² from the linear models shown in Figure S5(a) and (b). An F-value greater than the critical value (Fc) indicates that the model is statistically significant at the chosen significance level. An R² value closer to 1 indicates that the model explains the variability in the data more effectively.

|  | Figure 6(a) | Figure 6(b) | Fc=F(1,1,S) |
| --- | --- | --- | --- |
| F-value | 539.01265 | 191.47748 | F(1,1, 0.027) = 539.01265 F(1,1,0.046) = 191.47748 |
| R2 | 0.998 | 0.995 | - |