Supporting Information

Growth, crystal structure, Hirshfeld surface analysis, DFT studies, physicochemical characterization and cytotoxicity assays of novel organic triphosphate

Yathreb Oueslati, Sevgi Kansız, Necmi Dege, Cristina de la Torre Paredes, Antoni Llopis-Lorente, Ramón Martínez-Máñez and Wajda Sta

Table S-1. Crystal data and refinement of (C10H15N2)2H3P3O10.

| Empirical formula | (C10H15N2)2H3P3O10 |
| --- | --- |
| Formula weight Temperature (K) Wavelength (A ˚ ) Crystal system Space group a (Å) b (Å) c (Å) α(°) β(°) γ(°) Volume (Å3) Z Dcalc (Mg cm-3) Absorption coefficient F (000) Theta range for data collection Crystal size (mm3) Limiting indices Reflections collected Reflections observed Goodness-of-fit on F2 Final R indices Largest diff. peak and hole (e Å-3) | 582.41 (g.mol-1) 293 0.71073 Triclinic P1 9.511(2) 10.622(2) 13.653(2) 84.58(2) 86.59(2) 68.78(2) 1279.5(4) 2 1.512 0.24 (mm-1) 612 2.06°- 32.78° 0.21 x 0.16 x 0.14 -14<h< 14, -12<k<12, -4<l< 18 8386 6138 1.06 R1 = 0.054 and wR2 = 0.153 0.54 and -0.63 |

Table S-2. Principal intermolecular hydrogen bonding geometry (Å, ˚).

| D-H…A | D-H(Å) | H...A(Å) | D...A(Å) | D-H...A(˚) |
| --- | --- | --- | --- | --- |
| O(9)-H(7)…O(8) | 0.75(5) | 1.89(5) | 2.624(4) | 169(5) |
| O(1)-H(8)…O(10) | 0.99(6) | 1.60(6) | 2.557(4) | 162(5) |
| O(2)-H(9)…O(6) | 0.89(4) | 1.72(4) | 2.605(3) | 173(5) |
| N(2)-H(2A)…O(6) | 0.90 | 2.04 | 2.851(3) | 150 |
| N(2)-H(2B)…O(7) | 0.90 | 1.64 | 2.478(3) | 153 |
| N(4)-H(4A)...O(8) | 0.90 | 2.22 | 2.991(3) | 143 |
| N(4)-H(4B)…O(3) | 0.90 | 1.83 | 2.700(3) | 162 |
| C(8)-H(8A) ...O(3) | 0.97 | 2.13 | 2.989(3) | 147 |
| C(9)-H(9A) ...O(7) | 0.97 | 2.55 | 3.095(3) | 116 |
| C(19)-H(19B)...O(10) | 0.97 | 2.23 | 3.190(4) | 170 |

Figure S-1. The asymmetric unit of (C10H15N2)2H3P3O10.

Figure S-2. (a) Infinite layers of [H3P3O10]2- viewed along the c axis. (b) Hydrogen bonding sired with dashed lines.

.

Figure S-3. Graphical correlation of theoretical and experimental geometric parameters (a): distances (b): angles.

Figure S-4. Graphical correlation of theoretical and experimental infrared values.

Figure S-5. UV-Vis Spectrum of (C10H15N2)2H3P3O10 in solid state.

Figure S-6. Dependence of (αhυ)2 on the photon energy and optical band gap value of (C10H15N2)2H3P3O10.

Figure S-7. Solid-state photoluminescence spectrum of (C10H15N2)2H3P3O10.