Fig. S1 Changes in the color of AgNP hydrogels in contact with braised chicken during storage.

Table S1 The solubility product constant of silver compounds in water.

| silver compounds | Ksp | silver compounds | Ksp |
| --- | --- | --- | --- |
| AgCl | 1.8*10-10 | AgNO3 | 122 g/100 mL water |
| Ag(CH3COO) | 1.02 g/100 mL water | Ag2SO4 | 1.4*10-5 |
| AgOH | 2.0*10-8 | AgNO2 | 0.34g/100 mL water |

Table S2 Effect of NaCl on the main constituents.

| Contents | zeta-potential (mV) | particle size( nm) |
| --- | --- | --- |
| NaCl-free gelatin | -1.34±0.22g | 27.37±3.86ef |
| NaCl-containing gelatin | -0.57±0.03ef | 34.27±3.59d |
| NaCl-free PVP | -0.04±0.01de | 15.87±2.41h |
| NaCl-containing PVP | -0.04±0.02de | 25.63±2.60ef |
| NaCl-free AgNO3 | 30.82±0.41a | 56.80±2.01c |
| NaCl-containing AgNO3 | 7.45±0.43c | 88.30±0.36a |
| NaCl-free gelatin and PVP | -0.54±0.55h | 23.43±1.74fg |
| NaCl-containing gelatin and PVP | -1.02±0.10fg | 31.67±5.24de |
| NaCl-free mixed group of gelatin and PVP | -0.59±0.03ef | 18.77±5.61gh |
| NaCl-containing mixed group of gelatin and PVP | -1.28±0.08g | 27.23±3.04ef |
| NaCl-free AgNP | 13.38±0.35b | 23.80±3.54fg |
| NaCl-containing AgNP | 0.56±0.50d | 64.87±0.11b |

Note：The data is expressed as mean ± SD, lowercase letters (a-f) indicate significant differences within the same column (P < 0.05).